MINERAL RESOURCES TASMANIA

Laboratory Report

LJN2021-006

# Mineralogical, Hylogger and Geochemical ANALYSES,

# Savage River

An unpublished Mineral Resources Report for:

Grange Resources

By: 	R S Bottrill, M. Torrenes, J Renaud

and L Unwin

Date:	15/02/2021

Mineral Resources Tasmania

Department of State Growth

# Summary

Thirty four samples of drill core from the Savage River Centre Pit deposit were analysed by XRD to validate results from Hylogger analyses. The main outcome helps to determine the mineralogy which helps estimate the PAF (potential acid-forming) potential and ANC (acid-neutralising capacity) of these rocks in the tailings. Most of the rocks contain little or no sulphates after cutting and cleaning of the samples, and the correlation between the XRD and Hylogger results is very good.

# Introduction

The Hylogger IR spectroscopic analyses of drill core, conducted by various Geological Surveys in Australia, routinely returns analyses indicating various minerals that often cannot be readily confirmed in the hand specimens, and require XRD (X-ray diffraction) or other methods for confirmation.

The objective of this study was to confirm the mineralogy of 34 samples of drill core from the Savage River Centre Pit deposit, Tasmania, by XRD, in order to validate the results from Hylogger analyses. The main outcome is to help estimate the amount of PAF (potential acid-forming) material and the ANC (acid-neutralising capacity) of these rocks in the tailings. The samples were HYlogged previously (Report LJN2020-098 and 099) but the results were inadequate due to oxidation and weathering of the cores post-drilling. This set of dta was most done on clean, fresh-cut core.

Sample descriptionS

The details of the drill core samples are summarised in Table 1 below. See Appendix 1 for abbreviations. Pictures are in Figs 1 – 3.

Table 1: Sample details

(Highlighted samples were not tested by XRD)

| Reg. # | Hole Number & Depth | Sample Description - Visual | Process | Litho Unit |
| --- | --- | --- | --- | --- |
| G409611 | CDDH13003/78.0 | Chl-SiSt | XRD, HyL | WWA |
| G409612 | CDDH13003/79.8 | Chl-SiSt | XRD, HyL | WWA |
| G409614 | CDDH13003/158.9 | Dol, py | XRD, HyL | WWA |
| G409615 | CDDH13003/170.1 | Chlorite-phyllite breccia | XRD, HyL | WWA |
| G409616 | CDDH13003/183.15 | Black slate | XRD, HyL | WWA |
| G409617 | CDDH13003/184.2 | Py-dol-slate | XRD, HyL | WWA |
| G409618 | CDDH13003/201.0 | Chl-SiSt | XRD, HyL | WWA |
| G409619 | CDDH13003/212.8 | Chl-SiSt | XRD, HyL | WWA |
| G409620 | CDDH13003/219.0 | Chl-SiSt | XRD, HyL | WWA |
| G409621 | CCDH13012/29.1 | Chl-SiSt | XRD, HyL | WWA |
| G409622 | CCDH13012/38.9 | Chl schist rubble | XRD, HyL | WWA |
| G409623 | CCDH13012/51.5 | Chl qtz schist rubble | XRD, HyL | WWA |
| G409624 | CCDH13012/149.1 | Chl-ab | XRD, HyL, | WWA |
| G409625 | CCDH13012/61.4 | Phyllite | XRD, HyL | WWA |
| G409626 | CCDH13012/71 | Chl schist rubble | XRD, HyL | WWA |
| G409627 | CCDH13012/77.05 | Chl-dol | XRD, HyL | WWA |
| G409628 | CCDH13012/79.6 | Chl-Ab | XRD, HyL | WWA |
| G409629 | CCDH13012/51.5 | Qtz-chl schist rubble | HyL | WWA |
| G409630 | CCDH13012/99.6 | Chl schist | XRD, HyL | WWA |
| G409631 | CCDH13012/125.45 | Chl schist rubble | XRD, HyL | WWA |
| G409632 | CCDH13012/71.0 | Chl schist rubble | HyL | WWA |
| G409633 | CCDH13012/136.02 | Ab-chl brx | XRD, HyL | WWA |
| G409634 | CCDH13012/170.4 | Ab | XRD, HyL | WWA |
| G409635 | CDDH13012/146.7 | Chl-Ab | XRD, HyL | WWA |
| G409636 | CDDH13012/149.1 | Chl-Ab | XRD, HyL | WWA |
| G409637 | CDDH13012/143.4 | Chl schist | XRD, HyL | WWA |
| G409638 | CDDH13012/144.6 | Chl-Ab | XRD, HyL | WWA |
| G409639 | CDDH13012/150.1 | Chl-Ab | XRD, HyL | WWA |
| G409640 | CDDH13012/157.1 | Albitite +am fibre vein | XRD, HyL | MHA |
| G409644 | CDDH13012/221.9 | Am-py-mt-dol | XRD, HyL | MHA |
| G409650 | CDDH13015/51.0 | Amphibolite | XRD, HyL | MHA |
| G409660 | CDDH13017/37.0 | Qtz-chl-schist | XRD, HyL | Fill |
| G409661 | CDDH13017/53.4 | Qtz-chl-schist | XRD, HyL | MHA |
| G409662 | CDDH13017/74.75 | Chl-mt-dol | XRD, HyL | MHA |

Fig. 1a: Hylogged samples.

Fig. 1b: Hylogged samples.

Fig. 1c: Hylogged samples.

# METHODS

The samples were prepared, examined and analysed by Hylogger and XRD in the Mineral Resources Tasmania (MRT) laboratories, Rosny Park and Mornington, Tasmania. Sampling in this round avoided core with abundant amphiboles, serpentine, pyrite and magnetite.

The Hylogging results are summarised in Table 2.  The full Hylogger data, including IR spectroscopy and drillcore photographic images, have been provided to Grange Resources separately.

XRD

To check the mineralogy of 2 samples, they were analysed by XRD. Every attempt was made to sample the areas of core Hylogged, and be relatively homogenous.  The samples were prepared, examined, and analysed in the MRT laboratories, Rosny Park, Tasmania. They were run on a Rigaku Miniflex 600 X-Ray Diffractometer system provided with a 600W generator 150mm goniometer with a Cu tube; 40kV/15mA, sample spinner and a Scintillation counter (SC) with Be window, and a graphite counter monochromator and a Kß Ni- filter.. The MRT validated XRD analysis procedure scans over the range 3-63° 2Theta-2Theta range, with a scanning speed of 0.05o /min, and sample rotation of 15 rpm. The raw data were processed using the Rigaku PDXL2 software linked to the ICCD database.

Quantification is largely manual, using a series of prepared standards of the more common minerals to enable some semi-quantitative analysis. Quartz, if present, is used as an internal standard; and if not present, it is often added to the sample for a supplementary scan.  Our semi-quantitative results are calculated using single-peak calibration factors derived from scans of known mixtures of minerals.

The results are shown in Appendix 2 and summarised in Table 2.

Table 5: Comparison of Hylogger and XRD Results

(discrepancies are highlighted)

| Reg. # | Hole Number & Depth | Sample Description - Visual | Hylogger -TIR Mineralogy -Round 1. Highlighted cells are very possibly invalid. | XRD – Minerals >10% | Litho Unit | uTSAS results | Round 2 CLS results | Missed |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| G409611 | CDDH13003/78.0 | Phyllite +dol | Quartz, Calcite, Magnesite, Albite, Gypsum, Dolomite | Chlorite-quartz-Albite -dolomite-calcite | WWA | dolomite | Dolomite, calcite, sid? | Chlorite-quartz-Albite |
| G409612 | CDDH13003/79.8 | Chl-SiSt | Quartz, calcite, chlorite-FeMg | Chlorite-quartz-Albite | WWA | Chl, cac, sid | Qz, ab, cac, chl |  |
| G409614 | CDDH13003/158.9 | Dol, py | Quartz, calcite, ankerite | Dolomite-siderite-pyrite | WWA | Sid, aspectral, mtm? | Dolomite, sid, cac, qz? |  |
| G409615 | CDDH13003/170.1 | Chlorite-phyllite breccia | Chlorite, Quartz, Albite, Am, Ep, CO3 | Albite-chlorite | WWA | Chl, Hb, cac | Ab, Chl, cac |  |
| G409616 | CDDH13003/183.15 | Black slate | Quartz, ankerite, dolomite, chlorite | Quartz-dolomite-chlorite | WWA | Almost aspectral | Dolomite, chl, qz |  |
| G409617 | CDDH13003/184.2 | py-dol-slate | ankerite, magnesite, quartz, calcite | Dolomite-quartz-Albite | WWA | Almost apectral | Dolomite, calcite, qz | Ab |
| G409618 | CDDH13003/201.0 | Chl-SiSt | ankerite, magnesite, quartz, calcite | Chlorite-quartz-calcite | WWA | Chl | Chl, sid | qtz? |
| G409619 | CDDH13003/212.8 | Chl-SiSt | ankerite, magnesite, calcite | Chlorite-K-feldspar-quartz-Albite | WWA | Chl, sid | Chl, ab, sid | Ksp |
| G409620 | CDDH13003/219.0 | Chl-SiSt | quartz, chlorite-Fe, calcite | Albite-chlorite-clinopyroxene-Quartz - K-feldspar-amphibole | WWA | Chl, hb | Chl, ab, qz | cpx, Ksp |
| G409621 | CCDH13012/29.1 | Chl-SiSt | Albite-chlorite-quartz-anhydrite-epidote | Albite-chlorite-quartz-amphibole | WWA | Chl, Hb, sid | Ab, Qz, chl, |  |
| G409622 | CCDH13012/38.9 | chl schist rubble | Gypsum-calcite-andesine | Albite-chlorite-amphibole | WWA | Ch, hb | Ab, Chl |  |
| G409623 | CCDH13012/51.5 | chl qtz schist rubble | Albite-calcite-anhydrite-andesine | Albite-talc-chlorite | WWA | Ch, tl?, | Chl, albite, |  |
| G409624 | CCDH13012/149.1 | Chl-ab | Qtz, albite, Am, Chl, Cal, anhydrite, gypsum | Chlorite-albite-talc-amphibole | WWA | Phl, chl | Phl, chl |  |
| G409625 | CCDH13012/61.4 | phyllite | Gypsum-calcite-montmorillonite | Amphibole-Albite-quartz | WWA | Hb, chl | Qz, ab |  |
| G409626 | CCDH13012/71 | chl schist rubble | Chlorite-FeMg, anhydrite, albite, montmorillonite | Albite-chlorite | WWA | Chl, hb? | Ab, chl, Olig? |  |
| G409627 | CCDH13012/77.05 | chl-dol | Albite, calcite, anhydrite | Albite | WWA | Chl, cac, ank, phl, sid? | Ab, chl, olig, cac |  |
| G409628 | CCDH13012/79.6 | Chl-Ab | gypsum, calcite, bytownite | Albite | WWA | Chl, phl? | Ab, chl, olig? |  |
| G409629 | CCDH13012/51.5 | qtz-chl schist rubble | albite, anhydrite, labradorite | Not analysed | WWA | Chl, phl? | Ab, chl, olig? |  |
| G409630 | CCDH13012/99.6 | chl schist | Chlorite FeMg, montmorillonite, anhydrite | Albite | WWA | Hb, chl, act | Ab, hb, andesine? |  |
| G409631 | CCDH13012/125.45 | chl schist rubble | albite, chlorite FeMg, Chlorite, anhydrite | Albite | WWA | Chl, hb | Ab, chl, act? |  |
| G409632 | CCDH13012/71.0 | chl schist rubble | muscovite, talc, gypsum | Not analysed | WWA | Chl, hb | Ab, chl, act? |  |
| G409633 | CCDH13012/136.02 | Ab-chl brx | gypsum, calcite, albite, quartz | Albite-K-feldspar-clinopyroxene | WWA | Chl, phl, ank? hb, sid? | Hb,chl, ab, olig? | cpx |
| G409634 | CCDH13012/170.4 | Ab | Albite, calcite, anhydrite | Albite-amphibole-chlorite-talc | WWA | Hb, Chl, act? cac, ank, Gyp | Ab, gyp, olig?, talc? |  |
| G409635 | CDDH13012/146.7 | Chl-Ab | albite, anhydrite, quartz | Albite-chlorite-quartz | WWA | Chl, hb, phl? | Ab, olig? Chl? |  |
| G409636 | CDDH13012/149.1 | Chl-Ab | gypsum, calcite, actinolite, anhydrite | Albite | WWA | Hb, chl | Ab, chl, act? |  |
| G409637 | CDDH13012/143.4 | Chl schist | muscovite, quartz, anhydrite | Muscovite-quartz-Albite | WWA | Phe, chl | Ms, qz, ab |  |
| G409638 | CDDH13012/144.6 | Chl-Ab | calcite, montmorillonite, quartz | Quartz-Albite | WWA | Phl? chl? | Ab, qz, chl |  |
| G409639 | CDDH13012/150.1 | Chl-Ab | calcite, quartz, muscovite | Quartz-Albite-amphibole-clinopyroxene | WWA | Hb, chl | Ab, qz, act, chl, hb | cpx |
| G409640 | CDDH13012/157.1 | Albitite +Am fibre veins | actinolite, albite, edenite | Albite | WWA | Hb | Ab, act? |  |
| G409644 | CDDH13012/221.9 | Am-py-mt-dol | albite, quartz, phengite (visual sulphide?) | Fluorapatite-pyrite-quartz | MHA | Chl, sid, dolomite, | Qz, ap, ab, chl |  |
| G409650 | CDDH13015/51.0 | amphibolite | gypsum, dolomite, albite | Albite-amphibole | WWA | Hb, Chl | Qz, ab |  |
| G409660 | CDDH13017/37.0 | qtz-chl-schist | magnesite, gypsum, montmorillonite | Albite-amphibole | WWA | Chl, hb, act | Alb, olig?, act |  |
| G409661 | CDDH13017/53.4 | qtz-chl-schist | quartz, dolomite, ankerite, calcite | Quartz-Albite-cal | WWA | Chl, ank, phe, sid? | Ab, ms, cal, dolomite? Qtz? |  |
| G409662 | CDDH13017/74.75 | chl-mt-dol | talc, siderite, calcite, chlorite-FeMg, albite | Talc-chlorite-Albite | MHA | Hb, chl, sid | Ab, chl, cac? Talc |  |

Conclusions and Discussion

The Hylogger results were generally well validated by XRD, and is better than the initial hylogging due to the clean surfaces analysed after cutting the core.  None of the new Hylogger analyses was totally invalid relative to the XRD analyses. The Hylogger missed some major minerals detected by XRD in 6 samples (mostly clinopyroxene and Kspar), and 15 of the samples have minerals reported by Hylogger that could not be validated by XRD (mostly oligoclase-andesine (7), also siderite, calcite, montmorillonite and quartz). The initial Hylogging of these same 34 samples gave 12 results which were essentially totally invalidated by XRD; 16 that reported minerals not validated by XRD (mostly sulphates), and 12 that missed major minerals shown by XRD. The initial Hylogging indicated 18 of these to have gypsum and/or anhydrite as major components, but the second round indicated sulphates in only one sample (still unconfirmed by XRD). The mineralised zones gave even worse results. Thus this second round of Hylogging is much better than that on the unaltered core. Some ongoing discrepancies could be due to inter-sample mineralogical variability, eg. sparse, small veins, especially for calcite. The reports of plagioclase, other than albite, by Hylogger seem to be very suspect, as are most reports of siderite, montmorillonite, ankerite and magnesite. Some more petrology and SEM work is planned to help with this mineralogy.

The results indicate that Hylogging the uncut core indicated abundant anhydrite and gypsum in a very large proportion of that core, however these minerals generally could not be verified on cut core samples, and none are validated at more than 1% by XRD. Much of this probably reflects thin, post-drilling sulphate alteration on the cores, especially gypsum, although anhydrite is typically difficult to determine spectrally. The Hylogger is essentially a surface analysis technique, thus very sensitive to any oxidation or coatings. As the XRD analysis is a bulk analysis and not so sensitive to the core surface, the relatively small sulphate coatings on these samples is not usually obvious in the XRD analyses.

In regards to the initial Hylogging, I think if we delete all reported sulphates, magnesite, siderite, ankerite, montmorillonite and calcic plagioclase from the initial data, we should have much more reliable results.

# R.S. Bottrill 					J Renaud and L Unwin

# Mineralogist/Petrologist 	TECHNICAL OFFICERs

# Disclaimers:

While every care has been taken in the preparation of this report, no warranty is given as to the correctness of the information and no liability is accepted for any statement or opinion or for any error or omission. No reader should act or fail to act on the basis of any material contained herein. Readers should consult professional advisers. As a result the Crown in Right of the State of Tasmania and its employees, contractors and agents expressly disclaim all and any liability (including all liability from or attributable to any negligent or wrongful act or omission) to any persons whatsoever in respect of anything done or omitted to be done by any such person in reliance whether in whole or in part upon any of the material in this report. The MRT laboratories are not NATA registered but work to similar standards. This and other data collected in MRT laboratories may enter the MRT databases but every attempt will be made to ensure it remains closed file and not be available externally, unless at your request.

Appendix 1: Abbreviations

| Abbreviations | Mineral |
| --- | --- |
| Ab, Alb | Albite |
| Act | Actinolite |
| Am- | Amphibole |
| Anh- | Anhydrite |
| Ank- | Ankerite |
| Bar | Baryte |
| Bt | Biotite |
| Cal, cac | Calcite |
| Chl | Chlorite |
| CO3 | Carbonate |
| Cpx | Clinopyroxene |
| Ep | Epidote |
| Gyp | Gypsum |
| Hb | Hornblende |
| Ksp | Kspar |
| MgSt | Magnesite |
| Mont, Mtm | Montmorillonite |
| Ms, musc | Muscovite |
| Olig | Oligoclase |
| Phe | Phengite |
| Phl | Phlogopite |
| Qz, Qtz | Quartz |
| Sid | Siderite |
| SiSt | Siltstone |
| Stp | Stilpnomelane |
| Tc | Talc |
| Wthd | Weathered |

Appendix 3: XRD Analyses: MRT Laboratory Report

# Client:  R Bottrill	Sample Source:  Savage River

MRT Job Number:  LJN2021-006	Analysis:  Approximate Mineralogy

Method:  X-Ray Diffraction		Analyst:  L Unwin

Lab Manager: R Bottrill		Date:  6/11/2018

# XRD Results-G409611repeat-LJN2020-098-QA1-11/2/21

## General Information

| ### Measurement date: | 11/02/2021 | ### Interpretative date: | 11/02/2021 |
| --- | --- | --- | --- |
| ### Job Number/Client: | LJN2020-098-Grange | ### XRD | Rigaku Miniflex 600 |
| ### Registration Number: | G409611repeat | ### Analyst: | LUnwin |
| ### Quantitative Method: | XPlot | ### Process Medium: | Wholerock |
| ### Sample Holder: | Standard | ### Speed (deg/min): | 0.5 |
| ### Comment: | Shifted -0.03 |  |  |

## Analysis Results

| ### Phase name | ### Content wt% (± error) | ### Formula |
| --- | --- | --- |
| Quartz | 18(5) | SiO2 |
| Dolomite | 59(10) | CaMg(CO3)2 |
| Calcite | 7(3) | CaCO3 |
| Plagioclase* | 10(4) | NaAlSi3O8 |
| Chlorite* | 6(3) | (Fe,Mg,Al)6(Si,Al)4O10(OH)8 |

### Notes

Peak overlap may interfere with identifications and quantitative calculations.

Amorphous minerals and minerals present in trace amounts may not be detected.

Chlorite* - probably Mg-Chamosite

Plagioclase* - probably Albite

## Peak List

| No. | 2-theta(deg) | d(ang.) | Phase name | Rel. int. I(a.u.) |
| --- | --- | --- | --- | --- |
| 1 | 6.26(2) | 14.12(5) | Chlorite(0,0,1) | 0.88 |
| 2 | 12.5181 | 7.0654 | Chlorite(0,0,2) | 1.94 |
| 3 | 13.8329 | 6.39663 | Plagioclase(1,0,-1) | 0.89 |
| 4 | 16.5542 | 5.35075 | Dolomite(0,0,3) | 0.60 |
| 5 | 18.7871 | 4.71952 | Plagioclase(1,-2,0),Chlorite(0,0,3) | 0.91 |
| 6 | 20.8565 | 4.25568 | Quartz(1,0,0),Plagioclase(0,3,0),Chlorite(1,-1,1) | 2.14 |
| 7 | 22.2546 | 3.99139 | Plagioclase(2,0,-1) | 1.20 |
| 8 | 23.1783 | 3.83437 | Calcite(0,1,2),Plagioclase(1,-1,1) | 0.78 |
| 9 | 24.035(16) | 3.700(2) | Chlorite(1,-1,2),Dolomite(0,1,2) | 5.49 |
| 10 | 25.15(4) | 3.539(5) | Plagioclase(1,0,-2),Chlorite(0,0,4) | 1.20 |
| 11 | 25.44(3) | 3.498(4) | Plagioclase(1,1,-2),Chlorite(1,1,-3) | 0.68 |
| 12 | 26.638(5) | 3.3437(6) | Quartz(0,1,1),Plagioclase(1,-1,-2),Chlorite(0,2,-3) | 13.37 |
| 13 | 27.9505 | 3.18959 | Plagioclase(1,2,-2) | 0.79 |
| 14 | 29.45(2) | 3.031(2) | Calcite(1,0,4),Plagioclase(0,1,2) | 9.37 |
| 15 | 30.6915 | 2.9107 | Plagioclase(0,2,-2) | 0.87 |
| 16 | 30.9001 | 2.89152 | Plagioclase(1,-4,0),Dolomite(1,0,4) | 100.00 |
| 17 | 33.4141 | 2.67949 | Plagioclase(3,0,-1),Chlorite(1,-3,0),Dolomite(0,0,6) | 3.94 |
| 18 | 35.21(2) | 2.5471(14) | Plagioclase(2,4,-1),Chlorite(2,0,1),Dolomite(0,1,5) | 2.94 |
| 19 | 36.1218 | 2.48461 | Calcite(1,1,0),Plagioclase(1,-1,2) | 0.47 |
| 20 | 36.521(10) | 2.4583(7) | Quartz(1,1,0),Plagioclase(1,4,-2),Chlorite(1,-3,2) | 1.64 |
| 21 | 37.261(8) | 2.4112(5) | Plagioclase(2,-4,-1),Chlorite(0,2,-5),Dolomite(1,1,0) | 7.94 |
| 22 | 39.429(8) | 2.2835(5) | Quartz(1,0,2),Calcite(1,1,3),Plagioclase(1,-4,-2),Chlorite(1,-3,3) | 2.12 |
| 23 | 41.008(6) | 2.1992(3) | Plagioclase(2,5,-1),Chlorite(0,4,2),Dolomite(1,1,3) | 17.03 |
| 24 | 42.4253 | 2.12889 | Quartz(2,0,0),Plagioclase(1,5,-2),Chlorite(2,-2,2) | 1.74 |
| 25 | 43.6915 | 2.07008 | Plagioclase(3,-1,-3),Chlorite(2,0,-5),Dolomite(0,2,1) | 2.35 |
| 26 | 44.826(8) | 2.0203(3) | Plagioclase(1,6,0),Chlorite(0,0,7),Dolomite(2,0,2) | 11.85 |
| 27 | 47.5031 | 1.91249 | Calcite(0,2,4),Plagioclase(2,-5,-2),Chlorite(2,2,-5) | 2.22 |
| 28 | 49.2005 | 1.85041 | Plagioclase(2,-5,1),Chlorite(0,2,-7),Dolomite(0,2,4) | 4.94 |
| 29 | 50.309(17) | 1.8122(6) | Quartz(1,1,2),Plagioclase(2,-3,2),Chlorite(0,4,-5),Dolomite(0,1,8) | 12.46 |
| 30 | 50.94(3) | 1.7913(9) | Quartz(0,0,3),Plagioclase(3,-3,1),Chlorite(0,4,5),Dolomite(1,1,-6) | 19.68 |
| 31 | 54.9343 | 1.67006 | Quartz(0,2,2),Plagioclase(2,-2,-4),Chlorite(1,5,-3) | 1.12 |
| 32 | 56.2741 | 1.63343 | Plagioclase(2,6,1),Chlorite(1,-5,3) | 1.23 |
| 33 | 58.791(15) | 1.5694(4) | Calcite(1,0,10),Plagioclase(5,2,-2),Chlorite(3,1,-5),Dolomite(1,2,-1) | 4.05 |
| 34 | 59.73(4) | 1.5470(9) | Quartz(1,2,1),Plagioclase(1,-3,-4),Chlorite(1,-5,4),Dolomite(1,2,2) | 6.33 |

## Phase Data Pattern

# XRD Results-G409624-LJN2021-006-Grange-QA2-18/02/21

## General Information

| ### Measurement date: | 11/02/2021 | ### Interpretative date: | 18/02/2021 |
| --- | --- | --- | --- |
| ### Job Number/Client: | LJN2021-006-Grange | ### XRD | Rigaku Miniflex 600 |
| ### Registration Number: | G409624 | ### Analyst: | LUnwin |
| ### Quantitative Method: | XPlot/PDXL Rel Height | ### Process Medium: | Wholerock |
| ### Sample Holder: | Standard | ### Speed (deg/min): | 0.5 |
| ### Comment: | Shifted -0.03 |  |  |

## Analysis Results

| ### Phase name | ### Content wt% (± error) | ### Formula |
| --- | --- | --- |
| Chlorite* | 17(5) | (Fe,Mg,Al)6(Si,Al)4O10(OH)8 |
| Mica* | 4(2) | K(Mg,Fe)3[AlSi3O10](OH)2 |
| Anatase | 1(1) | TiO2 |
| Titanite | <1 | Ca(TiO)(SiO4) |
| Plagioclase* | 21(5) | NaAlSi3O8 |
| Amphibole* | 8(3) | Ca2(Mg4Al)(Si7AlO22)(OH)2 |
| Talc | 49(10) | Mg3Si4O10(OH)2 |

### Notes

Peak overlap may interfere with identifications and quantitative calculations.

Amorphous minerals and minerals present in trace amounts may not be detected.

Plagioclase* probably Albite

Chlorite* probably Mg-Chamosite

Amphibole* probably Edenite

Mica* probably Phlogopite

## Peak List

| No. | 2-theta(deg) | d(ang.) | Phase name | Rel. int. I(a.u.) |
| --- | --- | --- | --- | --- |
| 1 | 6.208(6) | 14.225(13) | Chlorite(0,0,1) | 33.75 |
| 2 | 8.695(8) | 10.162(9) | Biotite(0,0,2) | 27.64 |
| 3 | 9.424(4) | 9.377(4) | Talc(0,0,1) | 100.00 |
| 4 | 9.75056 | 9.06369 | Amphibole(0,2,0) | 1.39 |
| 5 | 10.484(8) | 8.431(6) | Amphibole(1,1,0) | 17.84 |
| 6 | 12.451(3) | 7.1034(17) | Chlorite(0,0,2) | 54.97 |
| 7 | 13.840(6) | 6.394(3) | Albite(0,2,0) | 11.47 |
| 8 | 14.9933 | 5.90407 | Albite(1,1,-1) | 0.93 |
| 9 | 15.820(9) | 5.597(3) | Chlorite(0,1,2),Albite(1,-1,-1) | 0.97 |
| 10 | 17.70(6) | 5.007(16) | Titanite(0,1,1) | 1.73 |
| 11 | 18.728(6) | 4.7343(15) | Chlorite(1,0,1),Amphibole(2,0,0) | 33.09 |
| 12 | 19.33(3) | 4.587(7) | Chlorite(0,2,0),Biotite(0,2,0),Amphibole(0,4,0),Talc | 24.21 |
| 13 | 20.946(10) | 4.2378(19) | Chlorite(1,-1,1),Biotite(0,2,2),Amphibole(2,2,0) | 7.84 |
| 14 | 22.015(10) | 4.0344(18) | Chlorite(1,-1,-2),Albite(2,0,-1),Amphibole(2,0,-1) | 29.65 |
| 15 | 23.024(11) | 3.8597(18) | Chlorite(0,2,-2),Albite(1,-1,1),Talc(1,1,1) | 3.06 |
| 16 | 23.523(10) | 3.7789(16) | Chlorite(1,0,-3),Albite(1,1,1) | 12.04 |
| 17 | 24.260(8) | 3.6658(12) | Chlorite, Biotite(1,1,3),Titanite(1,2,0),Albite(1,3,0), Amphibole | 24.19 |
| 18 | 25.060(5) | 3.5505(7) | Chlorite(0,0,4),Biotite(1,1,-4) | 37.76 |
| 19 | 25.366(10) | 3.5084(13) | Chlorite(1,1,-3),Anatase(1,0,1),Albite(1,1,-2),Talc | 12.13 |
| 20 | 26.405(4) | 3.3726(5) | Albite(1,-1,-2),Amphibole(0,4,1) | 20.07 |
| 21 | 26.651(15) | 3.3421(19) | Chlorite(0,1,-4),Biotite(0,0,6),Albite(2,-2,-1) | 3.97 |
| 22 | 27.135(13) | 3.2836(15) | Chlorite(1,2,1),Biotite(1,1,4),Titanite(2,1,-1),Amphibole(2,4,0),Talc(0,2,-2) | 6.36 |
| 23 | 27.41(2) | 3.251(3) | Talc(0,2,2) | 3.85 |
| 24 | 27.734(18) | 3.214(2) | Chlorite(1,2,-2),Albite(2,0,-2) | 52.94 |
| 25 | 27.876(5) | 3.1980(6) | Albite(0,0,2) | 63.83 |
| 26 | 28.524(10) | 3.1268(10) | Chlorite(1,0,-4),Amphibole(3,1,0),Talc(0,0,3) | 77.55 |
| 27 | 30.052(10) | 2.9712(10) | Chlorite(0,3,-1),Albite(1,-3,1),Amphibole(1,5,-1) | 20.82 |
| 28 | 30.418(7) | 2.9362(7) | Chlorite(1,2,-3),Biotite(1,1,5),Albite(0,4,-1) | 9.81 |
| 29 | 31.20(2) | 2.8645(19) | Albite(1,3,1) | 5.59 |
| 30 | 31.479(14) | 2.8397(12) | Chlorite(0,0,5),Albite(1,3,-2) | 7.75 |
| 31 | 32.969(7) | 2.7146(6) | Chlorite(0,1,-5),Amphibole(1,5,1) | 8.72 |
| 32 | 33.92(2) | 2.6410(15) | Chlorite(2,0,-1),Biotite(1,3,1),Titanite(1,2,-2),Albite(1,-3,-2),Amphibole(1,1,-2),Talc(1,-3,0) | 10.47 |
| 33 | 34.55(4) | 2.594(3) | Chlorite(1,2,-4),Titanite(1,3,-1),Albite(2,4,-1),Amphibole(0,6,1),Talc(1,3,-1) | 28.93 |
| 34 | 35.1879 | 2.54838 | Chlorite(2,1,-1),Albite(3,1,-2),Amphibole(2,0,-2) | 3.79 |
| 35 | 36.01(3) | 2.492(2) | Chlorite(2,1,-2),Titanite(0,2,2),Albite(2,-2,1),Amphibole(1,7,0),Talc(1,-3,1) | 8.69 |
| 36 | 36.659(11) | 2.4494(7) | Chlorite(2,-1,1),Biotite(1,3,3),Albite(2,-4,-1),Amphibole(2,2,-2),Talc(2,0,-2) | 6.73 |
| 37 | 36.93(4) | 2.432(3) | Chlorite(2,1,1),Biotite(1,3,-4),Anatase(1,0,3),Albite(1,5,-1),Amphibole(1,3,-2),Talc(1,-1,3) | 6.43 |
| 38 | 37.63(2) | 2.3882(15) | Chlorite(1,-2,4),Albite(2,-4,0),Amphibole(3,5,0),Talc(1,3,-2) | 1.95 |
| 39 | 38.40(3) | 2.3422(18) | Amphibole(3,5,-1),Talc(0,0,4) | 1.79 |
| 40 | 38.8066 | 2.31867 | Chlorite(0,3,4),Biotite(1,3,4),Titanite(1,3,1),Albite(3,3,-1),Amphibole(4,2,-1) | 3.13 |
| 41 | 39.8572 | 2.25994 | Chlorite(1,-3,3),Biotite(0,4,2),Titanite(2,3,-1),Amphibole(0,8,0) | 2.39 |
| 42 | 41.23(2) | 2.1880(11) | Chlorite(2,-1,-4),Biotite(1,3,5),Albite(1,-5,1),Amphibole(1,7,1) | 4.53 |
| 43 | 41.625(6) | 2.1679(3) | Biotite(2,2,-4),Amphibole(2,6,1),Talc(2,0,-3) | 3.60 |
| 44 | 42.453(12) | 2.1276(6) | Chlorite(2,-1,3),Biotite(2,2,3),Titanite(1,1,-3),Albite(0,6,0),Amphibole(4,4,-1) | 7.26 |
| 45 | 43.3591 | 2.08518 | Biotite(1,1,-9),Titanite(2,1,-3),Albite(2,-4,1),Talc(0,2,-4) | 2.40 |
| 46 | 44.112(14) | 2.0513(6) | Chlorite(1,3,4),Biotite(1,3,6),Amphibole(2,0,2),Talc | 3.15 |
| 47 | 44.89(2) | 2.0174(10) | Chlorite(2,2,-4),Biotite(0,2,9),Titanite(3,2,-2),Albite(2,4,1),Amphibole(3,5,1) | 12.66 |
| 48 | 47.1529 | 1.92588 | Chlorite(0,4,4),Biotite(1,3,7),Albite(2,-2,2),Amphibole(4,2,1) | 2.89 |
| 49 | 47.985(18) | 1.8944(7) | Chlorite(2,-3,-3),Biotite(1,1,-10),Anatase(2,0,0),Titanite(2,3,1),Albite(4,-2,-2),Amphibole(5,1,0),Talc(2,0,-4) | 6.40 |
| 50 | 48.550(14) | 1.8737(5) | Chlorite(2,3,2),Biotite(2,2,-7),Titanite(3,1,-3),Amphibole(2,4,2),Talc(0,0,5) | 1.66 |
| 51 | 49.15(3) | 1.8522(9) | Chlorite(0,2,7),Biotite(0,2,10),Titanite(3,3,-1),Albite(4,0,-3),Amphibole(1,7,-2),Talc(0,4,-3) | 1.81 |
| 52 | 49.87(6) | 1.827(2) | Chlorite(2,-1,-6),Biotite(2,2,6),Titanite(1,4,-2),Albite(2,6,0),Amphibole(4,4,-2),Talc(0,4,3) | 11.31 |
| 53 | 50.535(19) | 1.8046(6) | Biotite(0,4,7),Albite(1,1,3),Amphibole(0,10,0) | 2.65 |
| 54 | 51.081(13) | 1.7866(4) | Chlorite(2,-1,5),Albite(2,0,-4) | 5.50 |
| 55 | 52.1723 | 1.75178 | Chlorite(1,0,-8),Biotite(3,1,-1),Titanite(2,4,-2),Albite(4,2,0),Amphibole(5,1,-2),Talc(2,2,-4) | 1.99 |
| 56 | 53.12(2) | 1.7228(6) | Chlorite(3,-1,-2),Biotite(1,5,2),Albite(0,6,2),Amphibole(2,2,-3),Talc(2,-4,-1) | 2.66 |
| 57 | 54.286(11) | 1.6885(3) | Chlorite(3,-1,-3),Titanite(0,5,1),Albite(2,-2,-4),Amphibole(2,8,-2) | 2.02 |
| 58 | 54.67(9) | 1.678(2) | Chlorite(1,5,-2),Biotite(1,5,-3),Anatase(1,0,5),Titanite(1,1,3),Albite(3,5,-3),Amphibole(0,10,1),Talc(1,-3,4) | 10.19 |
| 59 | 55.531(11) | 1.6535(3) | Chlorite(2,-4,2),Titanite(2,0,-4),Albite(3,3,-4),Amphibole(4,6,1),Talc(1,5,-2) | 1.52 |
| 60 | 56.188(15) | 1.6357(4) | Chlorite(3,1,-4),Titanite(4,0,0),Albite(1,7,1),Amphibole(6,0,-1) | 1.56 |
| 61 | 57.7754 | 1.5945 | Chlorite(1,1,8),Biotite(1,5,5),Titanite(1,5,1),Albite(0,8,0),Amphibole(4,0,-3),Talc(1,5,2) | 1.96 |
| 62 | 59.0595 | 1.56286 | Chlorite(3,1,-5),Albite(5,-1,-1),Amphibole(1,11,-1),Talc(2,4,2) | 3.84 |
| 63 | 59.97(3) | 1.5413(6) | Chlorite(2,-1,-8),Biotite(1,1,12),Albite(5,3,-2),Amphibole(6,4,-1),Talc(2,-2,-5) | 2.07 |
| 64 | 60.49(6) | 1.5293(13) | Chlorite(2,-4,-5),Biotite(1,5,6),Titanite(4,2,0),Albite(4,-2,-4),Amphibole(4,2,2),Talc(3,-1,2) | 4.34 |
| 65 | 61.52(9) | 1.506(2) | Chlorite(2,0,7),Biotite(1,5,-7),Titanite(0,0,4),Albite(1,-7,2),Amphibole(2,8,2),Talc(3,-3,0) | 7.73 |

## Phase Data Pattern

Appendix 2: MRT Laboratory Report

Client:  		Grange Resources

Sample Location:  	Savage River mine

Job Number:  		LJN2020-098,099

Analyses:  		Approximate Mineralogy

Methods: 		XRD

Analyst:  		J Renaud, L Unwin

Lab Manager: 		R Bottrill

Date:  			23/11/2020

| Sample | Quartz | Plagioclase | Chlorite | Amphibole | Biotite | Phlogopite | Muscovite | Illite | Paragonite | Antigorite | Talc | Smectite | Vermiculite | Clinopyroxene | Clinozoisite | Tourmaline | Phillipsite | Titanite | Calcite | Mg-Calcite | Dolomite | Ankerite | Siderite | Magnesite | Hydrotalcite | K-feldspar | Pyrite | Marcasite | Magnetite | Rutile | Illmenite | Anatase | Jarosite | Anhydrite | Lansfordite | Fluorapatite |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| G409601 | 32 | 31 | 16 | 1 |  |  |  |  |  |  |  |  |  | 17 |  |  |  |  |  |  |  |  |  |  |  |  |  |  | 3 |  |  |  |  |  |  |  |
| G409602 | 15 | 29 | 42 | 5 |  |  | 2 |  |  |  |  |  |  |  |  |  |  |  |  |  | 4 |  |  |  | 2 |  |  |  |  |  |  |  | 1 |  |  |  |
| G409605 | 13 | 16 | 56 | 1 |  |  | 2 |  | 5 |  |  |  |  |  |  |  |  | 7 |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| G409606 | 16 | 25 | 39 | 10 |  |  |  |  |  |  |  |  |  |  |  |  |  |  | 2 |  | 4 |  |  |  |  | 3 |  |  |  |  |  |  |  |  |  |  |
| G409607 | 13 | 29 | 57 | 1 | <1 |  |  |  |  |  |  |  |  |  |  |  |  | <1 |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| G409609 | 27 | 20 | 46 | 6 | <1 |  |  |  |  |  |  |  |  |  |  |  |  | 1 |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| G409610 | 16 | 32 | 35 | 14 |  |  |  |  |  |  |  |  |  |  |  |  | <1 |  |  |  |  |  |  |  |  |  |  |  | 2 |  |  |  |  |  |  |  |
| G409611a | 20 | 12 | 61 |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | 3 |  | 3 |  |  |  |  |  | 1 |  |  | 1 |  |  |  |  |  |  |
| G409611b | 18 | 10 | 6 |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | 7 |  | 59 |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| G409612 | 24 | 18 | 45 |  |  |  | 2 |  |  |  |  |  |  |  |  |  |  |  | 6 |  |  | 2 |  |  |  |  |  |  |  | 2 | 2 |  |  |  |  |  |
| G409614 | 2 |  |  |  |  |  | 5 |  |  |  | 4 |  |  |  |  |  |  |  | <1 |  | 43 |  | 31 |  |  |  | 15 | <1 |  |  |  |  |  |  |  |  |
| G409615 |  | 74 | 16 | 1 |  |  |  |  |  |  |  |  |  |  |  |  |  | 2 | 4 |  |  |  |  |  |  |  | 2 |  |  |  |  |  | <1 |  |  |  |
| G409616 | 47 |  | 16 | 2 |  |  | 1 |  |  |  | 1 |  |  |  |  |  |  |  | 1 |  | 28 |  |  |  |  |  | 3 |  |  |  |  |  |  |  |  |  |
| G409617 | 30 | 11 | 5 | 3 |  | 2 |  |  |  |  |  |  |  |  |  |  |  |  | 2 |  | 45 |  |  |  |  |  | 1 |  |  |  |  |  |  |  |  |  |
| G409618 | 13 |  | 71 | 2 | <1 |  |  |  |  |  |  |  |  |  |  |  |  |  | 10 |  |  |  |  |  |  | 3 |  |  |  |  |  |  |  |  |  |  |
| G409619 | 15 | 9 | 52 | <1 | <1 |  |  |  |  |  |  |  |  |  |  |  |  | <1 | 7 |  |  |  |  |  |  | 16 |  |  |  |  |  |  |  |  |  |  |
| G409620 | 11 | 28 | 25 | 13 |  |  | 5 |  |  |  |  |  |  |  |  |  |  |  | 4 |  |  |  |  |  |  | 13 |  |  |  |  |  | 1 |  |  | <1 |  |
| G409621 | 20 | 36 | 23 | 12 |  |  | 1 |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | 1 |  |  | 5 |  |  | 1 |  |  |  |  |
| Sample | Quartz | Plagioclase | Chlorite | Amphibole | Biotite | Phlogopite | Muscovite | Illite | Paragonite | Antigorite | Talc | Smectite | Vermiculite | Clinopyroxene | Clinozoisite | Tourmaline | Phillipsite | Titanite | Calcite | Mg-Calcite | Dolomite | Ankerite | Siderite | Magnesite | Hydrotalcite | K-feldspar | Pyrite | Marcasite | Magnetite | Rutile | Illmenite | Anatase | Jarosite | Anhydrite | Lansfordite | Fluorapatite |
| G409622 | 2 | 45 | 25 | 15 |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | 5 |  |  |  |  |  | 4 | 3 |  |  | 1 |  |  |  |  |  |  |
| G409623 | 2 | 43 | 19 | 9 | <1 |  |  |  |  |  | 25 |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | 1 |  |  |  |  |
| G409624 |  | 22 | 18 | 6 | 1 |  |  |  |  |  | 52 |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | 1 |  |  |  |  |
| G409625 | 19 | 27 | 9 | 27 |  |  |  |  |  |  | 7 |  |  |  |  |  |  | 2 |  |  | 2 |  |  |  |  |  | 2 |  | 5 |  |  |  |  |  |  |  |
| G409626 | 5 | 53 | 21 | 6 |  | 9 |  |  |  | 1 | 5 |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| G409627 | 4 | 91 | 4 |  |  |  | 1 |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| G409628 | 5 | 90 | 3 |  | 2 |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| G409629 |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| G409630 | 4 | 88 | 4 | 3 | 2 |  |  |  |  |  |  |  |  |  |  |  |  | <1 |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| G409631 |  | 85 | 4 | 5 | 1 |  |  |  |  |  |  |  |  |  |  |  |  | 1 | 4 |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| G409633 |  | 33 | 7 | 8 | 1 |  |  |  |  |  | <1 |  |  | 15 |  |  |  |  |  |  |  |  |  |  |  | 32 |  |  | 3 |  |  |  |  |  |  |  |
| G409634 | 2 | 34 | 20 | 25 |  |  |  |  |  |  | 12 |  |  |  |  |  |  |  | 4 |  |  |  |  |  |  |  |  |  | 3 |  |  |  |  |  |  |  |
| G409635 | 10 | 50 | 13 | 8 | 4 |  |  |  |  |  |  | 6 |  |  |  |  |  |  |  |  |  |  |  |  |  | 9 |  |  |  |  |  |  |  |  |  |  |
| G409636 | 7 | 66 | 8 | 10 |  | 6 |  |  |  |  | 4 |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | <1 |  |
| G409637 | 25 | 12 | 2 |  | 8 |  | 44 |  |  |  |  | <1 |  |  |  |  |  |  |  |  |  |  |  |  |  | 8 |  |  |  |  |  | 1 |  |  |  |  |
| G409638 | 60 | 29 | 6 | <1 |  | 2 |  |  |  |  |  |  |  |  |  |  |  |  | 4 |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| G409639 | 44 | 29 | 1 | 23 |  |  |  |  |  |  |  |  | 1 |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | 1 |  |  |
| G409640 |  | 95 |  | 4 |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| G409641 | 1 | 46 |  | 4 |  |  |  |  |  |  |  |  |  | 49 |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| G409642 | 89 | 5 |  | 6 |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| G409643 | 83 | 11 |  | 5 |  |  |  |  |  |  |  |  |  |  |  |  |  | <1 | 1 |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| G409644 | 16 |  | 5 |  |  |  |  |  |  |  |  |  |  |  |  |  |  | <1 | 4 |  |  |  |  |  |  |  | 28 |  |  |  |  |  |  |  |  | 47 |
| G409645 |  |  | 39 | 20 |  |  |  |  |  |  |  |  |  |  |  |  |  | 1 |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| G409646 |  |  | T |  |  |  |  |  |  | SD |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | T |  | M |  |  |  |  |  |  |  |
| G409647 |  |  | A | A |  |  |  |  |  | A |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | M |  | T |  |  |  |  |  |  |  |
| G409648 | 48 | 37 | 11 |  | 2 |  |  |  |  |  |  |  |  |  |  |  |  | <1 | 2 |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| G409650 |  | 72 | 9 | 15 | <1 |  |  |  |  |  |  |  |  |  |  |  |  | 1 |  |  | 2 |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| G409652 | 3 | 34 | 10 | 17 | 1 |  |  |  |  |  |  |  |  |  | 35 |  |  | 2 |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| G409653 | 2 | 22 | 6 | 23 | 3 |  |  |  |  |  |  |  |  |  | 40 |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| Sample | Quartz | Plagioclase | Chlorite | Amphibole | Biotite | Phlogopite | Muscovite | Illite | Paragonite | Antigorite | Talc | Smectite | Vermiculite | Clinopyroxene | Clinozoisite | Tourmaline | Phillipsite | Titanite | Calcite | Mg-Calcite | Dolomite | Ankerite | Siderite | Magnesite | Hydrotalcite | K-feldspar | Pyrite | Marcasite | Magnetite | Rutile | Illmenite | Anatase | Jarosite | Anhydrite | Lansfordite | Fluorapatite |
| G409654 |  |  | 7 | 13 |  |  |  |  |  |  |  |  |  |  |  |  |  | <1 | 3 |  |  |  |  |  |  |  | 77 |  |  |  |  |  |  |  |  |  |
| G409655 |  |  | 60 | 23 |  |  |  |  |  |  |  |  |  |  | 9 |  |  | <1 | 3 |  |  |  |  |  |  |  |  |  | 5 |  |  |  |  |  |  |  |
| G409657 | 4 |  | 5 |  |  |  |  |  |  | 68 |  |  |  |  |  |  |  |  | 1 |  |  |  |  |  |  |  | 6 |  | 11 |  |  |  |  |  |  | 5 |
| G409658 |  |  | 6 |  |  |  |  |  |  | 69 |  |  |  |  |  |  |  |  | 1 |  |  |  |  |  |  |  | 5 |  | 19 |  |  |  |  |  |  |  |
| G409659 | 3 | 3 | 7 | 17 |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | 57 |  |  |  |  |  |  |  |  | 13 |
| G409660 | 4 | 67 | 3 | 15 |  | 3 |  |  |  |  |  |  |  | 8 |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| G409661 | 44 | 34 | 5 |  |  |  |  | 6 |  |  |  |  |  |  |  |  |  |  |  |  | 5 |  |  |  |  |  | 6 |  |  |  |  |  |  |  |  |  |
| G409662 | 9 | 11 | 26 | 7 | 3 |  |  |  |  |  | 34 |  |  |  |  |  |  |  | 6 |  |  |  |  |  |  |  |  |  | 5 |  |  |  |  |  |  |  |
| G409663 | 2 | 92 | 1 | 4 |  |  |  |  |  |  | <1 |  |  |  |  |  |  |  |  |  | 1 |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| G409665 |  |  | 9 | 55 |  |  |  |  |  |  |  |  |  |  |  | 12 |  | 4 |  |  |  |  |  |  |  |  |  |  | 13 |  |  |  |  |  |  |  |
| G409666 |  |  | 1 | 1 |  |  |  |  |  |  |  |  |  |  |  |  |  | 1 |  |  |  |  |  |  |  |  | 16 |  | 76 |  |  |  |  |  |  | 5 |
| G409668 |  |  | 3 | 2 |  |  |  |  |  |  |  |  |  |  |  |  |  | <1 |  |  |  |  |  |  |  |  |  |  | 94 |  |  |  |  |  |  |  |
| G409670 |  | 32 | 3 | 27 |  |  |  |  |  |  |  |  |  |  | 20 |  |  | 6 |  |  |  |  |  |  |  |  |  |  | 10 |  |  |  |  | 2 |  |  |
| G409671 | 2 | 29 | 12 | 26 |  |  |  |  |  |  |  |  |  |  | 29 |  |  | 2 |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| G409672 |  |  | 62 | 36 |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | 2 |  |  |  |  |  |  |  |  |  |
| G409673 | <1 | 16 | <1 | 23 |  |  |  |  |  |  |  |  |  |  | 59 |  |  | 2 |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| G409674 | 3 | 39 |  | 14 |  |  |  |  |  |  |  |  |  |  | 41 |  |  | 2 |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| G409676 |  | 21 | 19 | 20 | 1 |  |  |  |  |  |  |  |  |  | 32 |  |  | 7 |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| G409677 | 2 | 27 | 4 | 24 |  |  |  |  |  |  |  |  |  |  | 43 |  |  | <1 |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| G409679 |  |  | 28 | 9 |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | 64 |  |  |  |  |  |  |  |
| G409680 |  | 13 | 18 | 25 |  |  |  |  |  |  |  |  |  |  | 41 |  |  | 3 |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| G409681 |  |  | 3 |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | 3 |  | 94 |  |  |  |  |  |  |  |
| G409682 |  | 63 | 16 | 17 |  |  |  |  |  |  |  |  |  |  |  |  |  | 1 | 3 |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| G409684 |  |  | 37 | 20 |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | 11 |  | 33 |  |  |  |  |  |  |  |
| G409685 |  |  | 15 | 27 |  |  |  |  |  |  |  |  |  |  | 52 |  |  | 3 |  |  |  |  |  |  |  |  | 3 |  |  |  |  |  |  |  |  |  |
| G409686 |  | 18 | 20 | 39 |  |  |  |  |  |  |  |  |  |  | 9 |  |  |  | 1 |  |  |  |  |  |  |  | 4 |  |  |  |  | 9 |  |  |  |  |
| G409687 |  | 48 | 10 | 35 |  |  |  |  |  |  |  |  |  |  |  |  |  |  | 6 |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| G409688 | 15 | 47 | 3 | 4 | 14 |  | 13 |  |  |  |  | 1 |  |  |  |  |  |  | 1 |  |  |  |  |  |  |  | 2 |  |  |  |  |  |  |  |  |  |
| Sample | Quartz | Plagioclase | Chlorite | Amphibole | Biotite | Phlogopite | Muscovite | Illite | Paragonite | Antigorite | Talc | Smectite | Vermiculite | Clinopyroxene | Clinozoisite | Tourmaline | Phillipsite | Titanite | Calcite | Mg-Calcite | Dolomite | Ankerite | Siderite | Magnesite | Hydrotalcite | K-feldspar | Pyrite | Marcasite | Magnetite | Rutile | Illmenite | Anatase | Jarosite | Anhydrite | Lansfordite | Fluorapatite |
| G409689 | 35 | 55 | <1 |  |  |  |  |  |  |  | 7 |  |  |  |  |  |  |  | 1 |  |  |  |  |  |  |  |  |  | 2 |  |  |  |  |  |  |  |
| G409690 | 6 | 84 | 1 | <1 | 3 |  | 4 |  |  |  |  | 1 |  |  |  |  |  | <1 |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| G409691 | 64 | 14 | 13 |  | 3 |  | 5 |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | 2 |  |  |  |  |  |
| G409692 | 25 | 20 | 41 |  |  |  | 9 |  |  |  |  |  |  |  |  |  |  | <1 |  |  |  |  |  |  |  |  | 5 |  |  |  |  |  |  |  |  |  |
| G409694 | 7 | 52 | 4 | 28 | 2 |  |  |  |  |  |  |  |  |  |  |  |  |  | 2 |  | 1 |  |  |  |  |  |  |  | 5 |  |  |  |  |  |  |  |
| G409695 | 32 | 14 | 41 |  |  |  | 3 |  |  |  |  |  |  |  |  |  |  |  | 6 |  |  |  |  |  |  |  | 1 |  |  |  | 3 |  |  |  |  |  |
| G409696 | 33 | 40 | 11 |  |  |  | 8 |  |  |  |  |  |  |  |  |  |  |  | 1 |  |  |  |  |  |  |  | 4 |  |  |  | 3 |  |  |  |  |  |
| G409697 | 43 | 8 | 13 |  |  |  | 31 |  |  |  |  |  |  |  |  |  |  |  | 1 |  |  |  |  |  |  |  | 1 |  |  |  | 3 |  |  |  |  |  |
| G409698 | 44 | 17 | 14 |  |  |  | 22 |  |  |  |  |  |  |  |  |  |  |  |  |  | 2 |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| G409699 | 27 | 22 | 15 |  |  |  | 36 |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| G409701 | 32 | 34 | 12 |  |  |  | 21 |  |  |  |  |  |  |  |  |  |  |  |  |  | 2 |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| G409702 | 2 | 86 | <1 |  |  |  | 1 |  |  |  |  |  |  |  |  |  |  |  |  |  | 9 |  |  |  |  |  | 2 |  |  |  |  |  |  |  |  |  |
| G409703 | 19 | 33 | 13 |  | 4 |  | 6 |  |  |  |  |  |  |  |  |  |  |  | 1 |  | 17 |  |  |  |  | 2 |  |  | 4 | 2 |  |  |  |  |  |  |
| G409704 | 1 |  |  |  |  |  |  |  |  |  |  |  |  |  |  | 1 |  |  |  |  | <1 |  |  | 96 |  |  | 2 |  |  |  |  |  |  |  |  |  |
| G409706 | 34 | 57 | 3 |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | 5 |  |  |  |  |  | 2 |  |  |  |  |  |  |  |  |  |
| G409707 | 21 | 64 | 1 |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | 14 |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| G409708 | 47 | 50 | 1 |  | <1 |  |  |  |  |  |  |  |  |  |  |  |  |  | 1 |  | 1 |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| average | 15 | 30 | 16 | 9.2 | 0.6 | 0.2 | 2.5 | 0.1 | 0.1 | 1.6 | 1.1 | 0.1 | 0 | 1 | 4.6 | 0.1 | 0 | 0.5 | 1.1 | 0.1 | 2.1 | 0 | 0.3 | 1.1 | 0 | 1 | 3 | 0 | 5.1 | 0.1 | 0.1 | 0.1 | 0 | 0 | 0 | 0.8 |

Notes:

Peak overlap may interfere with identifications and quantitative calculations.

Amorphous minerals and minerals present in trace amounts may not be detected.

Clinozoisite includes epidote.

Amphibole may be largely tremolite-actinolite.

Plagioclase is probably mostly albite.

Clinopyroxene is probably diopside.