MINERAL RESOURCES TASMANIA

LABORATORY REPORT

LJN2021-042

XRD FOR HYLOGGER VALIDATION

VARIOUS LOCATIONS

An unpublished Mineral Resources Report for:

David Green, MRT

By: 	R S Bottrill,

and L Unwin

Date:	24 June 2021

Mineral Resources Tasmania

Department of State Growth

# Summary

The XRD was used to confirm the HyLogger mineralogy for 21 samples of drill core from various locations The HyLogger seems to generate some false positives for biotite, chlorite and muscovite in particular, and also tends to miss chlorite and pyroxene, but generally, the results validate very well.

# Introduction

The HyLogger IR spectroscopic analyses of drill core routinely returns analyses indicating various minerals that often cannot be readily confirmed in the hand specimens, and require XRD (X-ray diffraction) or other methods for confirmation.

The objective of this study was to confirm the mineralogy of 21 samples of drill core from various locations, with details shown in Table 1.

Table 1: Sample Details

| Reg. Number | Field No. | Location | Sample Description |
| --- | --- | --- | --- |
| G408243 | 24998 WSP-14 #102276-102285 | White Spur, MRV | K-feldspar-albite-qtz |
| G408245 | 13529 MCH1 #73944-73949 | Mt Charter, MRV | Albite-qtz-calcite-biotite-muscovite-chlorite |
| G408246 | 6200 Forest-1 #109397-109414 | Black River | Biotite-calcite-albite-qtz(-K-feldspar) |
| G408248 | 8484 HAT7 #38045-38050 | Hatfield River, MRV | Muscovite-albite(-qtz) |
| G408249 | 27812 MCD37 #1468-1475 | Mackintosh, MRV | Muscovite(-albite-qtz) |
| G408250 | 6149 Thorp-1 #70841-70851 | Tasmania Basin | Muscovite-qtz-K-feldspar-kaolinite-albite |
| G408251 | 6149 Thorp-1 #70936-70954 | Tasmania Basin | Muscovite-qtz-K-feldspar-kaolinite-albite |
| G408253 | 19586 L4A #6226-6264 | Lefroy | Muscovite-qtz-K-feldspar-biotite(-albite) |
| G408254 | 19586 L4A #7331-7349 | Lefroy | Qtz-muscovite-albite |
| G408255 | 36739 WSP-16 #33386-33397 | White Spur, MRV | K-feldspar-biotite-albite(-muscovite-qtz) |
| G408260 | 15171 DD80OC3 #7014-7033 | Oonah prospect | Muscovite-qtz-K-feldspar-albite) |
| G408261 | 15171 DD80OC3 #41453-41494 | Oonah | Muscovite-qtz-albite-K-feldspar(-chlorite) |
| G408262 | 15171 DD80OC3 #11918-11929 | Oonah | Muscovite-qtz-K-feldspar-albite |
| G408264 | 29536 CETD4 #67704-67724 | Cethana | Biotite-qtz-(-chlorite) |
| G408265 | 29536 CETD4 #68737-68748 | Cethana | Biotite-qtz-garnet |
| G408266 | 18532 C0631 #77942-77964 | Cleveland | Amphibole-chlorite-qtz-muscovite-(-albite) |
| G408268 | 18532 C0631 #51238-51246 | Cleveland | Biotite-qtz(-chlorite) |
| G408275 | Quarry #434-456 | Gramalote Project, Colombia | Albite-qtz(-biotite-K-feldspar) |
| G408276 | 71763 550 #83505-83525 | Ernest Henry, Qld | K-feldspar-muscovite(-oxide) |
| G408277 | 8440749 D007 #21679-21701 | Pine Creek, NT | Albite-K-felsdpar-amphibole-muscovite |
| G408279 | M0001606 RAVD0120 #66913-66918 | Yilgarn-Ravensthorp WA | Biotite-chlorite |

# Sample Preparation

The samples were hand-milled (due to small sample sizes) and the analyses were done by XRD (X-Ray diffraction), in the Mineral Resources Tasmania (MRT) laboratories, Rosny, Tasmania.

# XRD analyses

The samples were prepared, examined and analysed in the MRT laboratories, Rosny Park, Tasmania. They were run on a Rigaku Miniflex 600 X-Ray Diffractometer system: a 600W generator 150mm goniometer with a Cu tube; 40kV/15mA, sample spinner and a Scintillation counter (SC) with Be window, -3o to 145o 2Ø scanning range and 3o - 145o 2Ø measuring range, with a scanning speed of 0.01 to 100o/min, a graphite counter monochromator and a Kß Ni- filter.  The analysis software used is the PDXL2 using the ICCD database.

Quantification is largely manual, using a series of prepared standards of the more common minerals to enable some semi-quantitative analysis. Quartz, if present, is used as an internal standard; and if not present, it is often added to the sample for a supplementary scan.  Our semi-quantitative results are calculated using single-peak calibration factors derived from scans of known mixtures of minerals.

The results are shown in Appendix 1, with tabulated Results in Table 2.

Table 2: Tabulated Results

| Registration Number | Quartz | Albite | Orthoclase | Anorthite | Microcline | Calcite | Clinopyroxene | Muscovite | Chlorite | Biotite | Kaolinite | Illite | Pyrite | Spessartine | Halloysite | Smectite | Phlogopite | Magnesio-ferri-hornblende | Magnetite | Serpentine | Amphibole | Vermiculite | Titanite |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| G408243 | 25 | 38 | 16 |  |  | 5 | 14 | <1 | <1 |  |  |  |  |  |  |  |  |  |  |  |  |  | <1 |
| G408245 | 29 | 36 |  |  |  | 14 |  | <1 | 15 | 5 |  |  |  |  |  |  |  |  |  |  |  |  |  |
| G408246 | 46 | 5 | 4 |  |  | 23 |  | 6 | 16 |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| G408248 | 19 | 29 |  |  | 28 | 1 |  | 11 | 9 |  |  |  | 2 |  |  | <1 |  |  |  |  |  |  |  |
| G408249 | 11 | 14 |  |  |  |  |  | 41 |  |  |  |  |  |  | 35 |  |  |  |  |  |  |  |  |
| G408250 | 35 |  |  |  |  |  |  |  |  |  | 45 |  |  |  |  |  |  |  |  |  |  |  |  |
| G408251 | 31 |  | 2 |  |  |  |  |  |  |  | 44 | 16 |  |  |  |  |  |  |  |  |  |  |  |
| G408253 | 30 | 1 | 3 |  |  |  |  | 36 | 30 |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| G408254 | 70 | 8 |  |  |  |  | 11 | 2 | 10 |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| G408255 | 25 | 24 | 24 |  |  |  | 7 | 5 | 15 |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| G408260 | 49 | 2 | 4 |  |  |  |  | 34 | 8 |  |  |  | 2 |  |  |  |  |  |  |  |  |  |  |
| G408261 | 44 | 2 | 3 |  |  |  |  | 13 |  |  | 33 |  | 4 |  |  |  |  |  |  |  |  |  |  |
| G408262 | 53 | 3 | 4 |  |  |  |  | 36 | 4 |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| G408264 | 31 |  | 5 |  |  |  |  |  | 30 | 34 |  |  |  |  |  |  |  |  |  |  |  |  |  |
| G408265 | 21 |  |  |  |  |  |  |  | 8 |  |  |  |  | 17 |  |  | 54 |  |  |  |  |  |  |
| G408266 | 9 |  | 6 |  |  |  |  |  | 37 | 1 |  |  |  |  |  |  |  | 46 |  |  |  |  |  |
| G408268 | 30 |  |  |  |  |  |  |  | 17 | 43 |  |  |  |  |  |  |  |  |  |  |  |  |  |
| G408275 | 32 | 39 | 7 |  |  | 1 | 8 |  | 10 | 3 |  |  |  |  |  |  |  |  |  |  |  |  |  |
| G408276 |  | 1 |  |  | 79 | <1 |  | 6 | 3 |  |  |  | 1 |  |  |  |  |  | 10 |  |  |  |  |
| G408277 | 5 |  |  | 27 |  |  | 22 |  |  | 3 |  |  |  |  | 9 | 10 |  |  |  |  |  |  |  |
| G408279 |  |  |  |  |  |  |  |  | 10 |  |  | 48 |  |  |  |  | 24 |  |  | 2 | 16 |  |  |

# Summary and Discussion

The summarised XRD analyses are compared with the HyLogger results in Table 3, highlighting some variations. The Hylogger generates some false positives for biotite, chlorite, albite and muscovite in particular, and also tends to miss chlorite, clay minerals (halloysite, kaolinite and smectite) and pyroxene (although it would be good to get some validation on the pyroxene). Generally, the results validate very well.

Table 3: Comparison with Hylogger Results (discrepancies Highlighted)

| Reg. Number | HYlogger results | XRD Summary (>10%) |
| --- | --- | --- |
| G408243 | K-feldspar-albite-qtz | Quartz, Albite, Orthoclase, Clinopyroxene |
| G408245 | Albite-qtz-calcite-biotite-muscovite-chlorite | Quartz, Albite, Calcite, Chlorite |
| G408246 | Biotite-calcite-albite-qtz(-K-feldspar) | Quartz, Calcite, Chlorite |
| G408248 | Muscovite-albite (-qtz) | Quartz, Albite, Microcline, Muscovite |
| G408249 | Muscovite(-albite-qtz) | Quartz, Albite, Muscovite, Halloysite |
| G408250 | Muscovite-qtz-K-feldspar-kaolinite-albite | Quartz, Kaolinite |
| G408251 | Muscovite-qtz-K-feldspar-kaolinite-albite | Quartz, Kaolinite, Illite |
| G408253 | Muscovite-qtz-K-feldspar-biotite(-albite) | Quartz, Muscovite, Chlorite |
| G408254 | Qtz-muscovite-albite | Quartz, Clinopyroxene, Chlorite |
| G408255 | K-feldspar-biotite-albite(-muscovite-qtz) | Quartz, Albite, Orthoclase, Chlorite |
| G408260 | Muscovite-qtz-K-feldspar-albite) | Quartz, Muscovite |
| G408261 | Muscovite-qtz-albite-K-feldspar(-chlorite) | Quartz, Muscovite, Kaolinite |
| G408262 | Muscovite-qtz-K-feldspar-albite | Quartz, Muscovite |
| G408264 | Biotite-qtz-(-chlorite) | Quartz, Chlorite, Biotite |
| G408265 | Biotite-qtz-garnet | Quartz, Spessartine, Phlogopite |
| G408266 | Amphibole-chlorite-qtz-muscovite-(-albite) | Chamosite, Magnesio-hornblende |
| G408268 | Biotite-qtz(-chlorite) | Quartz, Chlorite, Biotite |
| G408275 | Albite-qtz(-biotite-K-feldspar) | Quartz, Albite, Chlorite |
| G408276 | K-feldspar-muscovite(-oxide) | Microcline, Magnetite |
| G408277 | Albite-K-feldspar-amphibole-muscovite | Anorthite, Clinopyroxene, Smectite |
| G408279 | Biotite-chlorite | Illite, phlogopite, amphibole, chlorite |

# R.S. Bottrill 					L Unwin

# Mineralogist/Petrologist 	TECHNICAL OFFICER

# Disclaimers:

While every care has been taken in the preparation of this report, no warranty is given as to the correctness of the information and no liability is accepted for any statement or opinion or for any error or omission. No reader should act or fail to act on the basis of any material contained herein. Readers should consult professional advisers. As a result the Crown in Right of the State of Tasmania and its employees, contractors and agents expressly disclaim all and any liability (including all liability from or attributable to any negligent or wrongful act or omission) to any persons whatsoever in respect of anything done or omitted to be done by any such person in reliance whether in whole or in part upon any of the material in this report. The MRT laboratories are not NATA registered but work to similar standards. This and other data collected in MRT laboratories may enter the MRT databases but every attempt will be made to ensure it remains closed file and not be available externally, unless at your request.

Appendix 1: Laboratory Report: XRD Analyses

Client:  		David Green, MRT

MRT Job Number:  	LJN2021-042

Analysis:  		Mineralogy

Method: 		X-Ray Diffraction

Analyst:  		L Unwin

Lab Manager:  	R Bottrill

Date:  			7/6/2021

# XRD Results-G408243-LJN2021-042-DG-4/6/2021

## General Information

| ### Measurement date: | 22/04/2021 | ### Interpretative date: | 4/6/2021 |
| --- | --- | --- | --- |
| ### Job Number/Client: | LJN2021-042 DG | ### XRD | Rigaku Miniflex 600 |
| ### Registration Number: | G408243 | ### Analyst: | LUnwin |
| ### Quantitative Method: | PDXL Relative Heights | ### Process Medium: | Selective by Client |
| ### Sample Holder: | Low Reflectance | ### Speed (deg/min): | 0.5 |
| ### Comment: | Shifted -0.05 |  |  |

## Analysis Results

| ### Phase name | ### Content% | ### Formula |
| --- | --- | --- |
| Albite | 25(5) | NaAlSi3O8 |
| Quartz | 38(10) | SiO2 |
| Orthoclase | 16(5) | (K,Na)AlSi3O8 |
| Calcite | 5(3) | CaCO3 |
| Titanite | <1 | Ca(TiO)(SiO4) |
| Clinopyroxene | 14(4) | (Ca,Na)(Mg,Fe,Al)Si2O6 |
| Muscovite | <1 | KAl2(AlSi3O10)(OH)2 |
| Chamosite | <1 | (Fe,Mg,Al)6(Si,Al)4O10(OH)8 |

### Notes

Peak overlap may interfere with identifications and quantitative calculations.

Amorphous minerals and minerals present in trace amounts may not be detected.

## Peak List

| No. | 2-theta(deg) | d(ang.) | Phase name | Rel. int. I(a.u.) |
| --- | --- | --- | --- | --- |
| 1 | 8.85813 | 9.97473 | Muscovite(0,0,2) | 1.45 |
| 2 | 12.52(2) | 7.062(12) | Chamosite(0,0,2) | 1.76 |
| 3 | 13.846(14) | 6.391(6) | Albite(0,2,0),Orthoclase(0,0,1),Clinopyroxene(1,1,0) | 9.99 |
| 4 | 14.991(11) | 5.905(4) | Albite(1,1,-1),Orthoclase(1,1,-1) | 4.81 |
| 5 | 15.832(2) | 5.5931(8) | Albite(1,-1,-1) | 1.75 |
| 6 | 17.8646 | 4.96109 | Titanite(0,1,1),Muscovite(0,0,4) | 1.15 |
| 7 | 19.8177 | 4.47635 | Clinopyroxene(0,2,0),Muscovite(0,2,0),Chamosite | 2.35 |
| 8 | 20.8453 | 4.25795 | Quartz(1,0,0) | 22.92 |
| 9 | 22.030(5) | 4.0315(9) | Albite(2,0,-1) | 21.70 |
| 10 | 22.499(12) | 3.949(2) | Orthoclase(1,1,1),Muscovite(1,1,2),Chamosite(1,1,2) | 6.54 |
| 11 | 23.0415(19) | 3.8568(3) | Albite(1,-1,1),Orthoclase(2,0,0),Calcite(0,1,2),Muscovite(1,1,-3),Chamosite(0,2,2) | 7.33 |
| 12 | 23.539(6) | 3.7765(10) | Albite(1,1,1),Orthoclase(1,3,0) | 27.69 |
| 13 | 24.240(7) | 3.6688(10) | Albite(1,3,0),Clinopyroxene(1,1,1) | 22.32 |
| 14 | 24.577(10) | 3.6193(14) | Orthoclase(1,3,-1) | 1.46 |
| 15 | 25.384(12) | 3.5060(17) | Albite(1,1,-2) | 3.42 |
| 16 | 25.63(2) | 3.473(3) | Albite(2,2,-1),Orthoclase(1,-1,-2),Muscovite(1,1,-4) | 11.03 |
| 17 | 26.626(5) | 3.3452(6) | Albite(2,-2,-1),Quartz(1,0,1),Clinopyroxene(0,2,1),Muscovite(0,2,4) | 100.00 |
| 18 | 27.0121 | 3.29824 | Orthoclase(2,2,0),Chamosite(1,1,3) | 32.55 |
| 19 | 27.496(10) | 3.2413(12) | Orthoclase(0,4,0),Titanite(2,1,-1) | 19.44 |
| 20 | 27.704(8) | 3.2175(9) | Albite(2,0,-2),Clinopyroxene(2,2,0),Muscovite(1,1,4) | 19.33 |
| 21 | 27.910(5) | 3.1942(6) | Albite(0,0,2) | 63.39 |
| 22 | 28.166(10) | 3.1657(11) | Albite(2,2,0) | 26.55 |
| 23 | 29.414(9) | 3.0341(9) | Calcite(1,0,4) | 29.18 |
| 24 | 29.8457 | 2.99123 | Orthoclase(1,3,1),Titanite(0,0,2),Clinopyroxene(2,2,-1),Muscovite(0,2,5) | 4.05 |
| 25 | 30.032 | 2.9731 | Albite(1,-3,1) | 23.52 |
| 26 | 30.489(9) | 2.9296(9) | Albite(0,4,-1),Orthoclase(2,2,-2),Clinopyroxene(3,1,0) | 8.93 |
| 27 | 30.8036 | 2.90036 | Orthoclase(0,2,2),Clinopyroxene(3,1,-1) | 3.77 |
| 28 | 31.230(14) | 2.8618(12) | Albite(1,3,1),Calcite(0,0,6),Titanite(2,0,-2),Muscovite(1,1,5) | 9.34 |
| 29 | 32.3069 | 2.76875 | Albite(0,2,2),Orthoclase(1,-3,-2),Muscovite(1,1,-6) | 5.07 |
| 30 | 33.89(5) | 2.643(4) | Albite(1,-3,-2),Chamosite(1,3,1) | 2.15 |
| 31 | 34.3024 | 2.61211 | Orthoclase(3,1,-2),Titanite(1,2,-2) | 1.56 |
| 32 | 34.7281 | 2.58106 | Orthoclase(2,4,-1),Titanite(2,2,0),Muscovite(1,3,-1) | 0.91 |
| 33 | 35.01(3) | 2.561(2) | Albite(2,4,-1),Orthoclase(2,-4,-1),Clinopyroxene(1,3,-1),Muscovite(2,0,-2),Chamosite(2,0,2) | 23.25 |
| 34 | 36.0068 | 2.49228 | Albite(2,-2,1),Orthoclase(2,4,0),Calcite(1,1,0),Clinopyroxene(2,2,1),Muscovite(0,0,8) | 5.40 |
| 35 | 36.515(7) | 2.4587(4) | Albite(1,1,2),Quartz(1,1,0),Orthoclase(2,-4,0),Titanite(0,2,2),Muscovite(1,3,-3) | 18.28 |
| 36 | 37.4028 | 2.4024 | Albite(2,4,0) | 2.23 |
| 37 | 37.6416 | 2.38771 | Albite(2,-4,0),Orthoclase(3,3,-1),Muscovite(2,0,-4) | 2.43 |
| 38 | 38.79(8) | 2.319(5) | Albite(1,-5,-1),Orthoclase(1,1,-3),Clinopyroxene(4,0,0),Muscovite(1,1,7),Chamosite | 3.56 |
| 39 | 39.434 | 2.28321 | Albite(1,-1,-3),Quartz(1,0,2),Calcite(1,1,3),Titanite(1,3,1),Clinopyroxene(3,1,1),Chamosite(0,4,1) | 12.47 |
| 40 | 40.2934 | 2.23647 | Albite(1,-3,2),Quartz(1,1,1),Orthoclase(2,2,-3),Titanite(2,3,-1),Clinopyroxene(3,1,-2),Muscovite(2,2,0) | 3.96 |
| 41 | 41.180(15) | 2.1903(8) | Albite(2,-4,-2),Orthoclase(1,-5,1),Muscovite(0,4,2) | 2.44 |
| 42 | 41.689(15) | 2.1648(7) | Orthoclase(0,0,3),Titanite(0,4,0) | 3.70 |
| 43 | 42.426(12) | 2.1288(6) | Albite(0,6,0),Quartz(2,0,0),Orthoclase(2,4,1),Clinopyroxene(3,3,-1),Muscovite(1,3,5),Chamosite(1,3,4) | 13.28 |
| 44 | 43.145(11) | 2.0950(5) | Albite(3,-3,0),Calcite(2,0,2),Muscovite(1,3,-6),Chamosite(2,2,3) | 6.33 |
| 45 | 43.5304 | 2.07737 | Albite(2,-4,1),Orthoclase(1,-3,-3),Titanite(1,2,2),Muscovite(2,2,3),Chamosite(0,4,3) | 1.66 |
| 46 | 44.9808 | 2.0137 | Albite(4,0,-2),Orthoclase(4,2,-2),Chamosite(0,0,7) | 1.14 |
| 47 | 45.796(19) | 1.9797(8) | Albite(0,6,1),Quartz(2,0,1),Orthoclase(2,2,2),Titanite(3,2,-2),Muscovite(2,2,4) | 9.17 |
| 48 | 47.06(2) | 1.9296(9) | Albite(2,-2,2),Orthoclase(4,0,0),Calcite(0,2,4),Titanite(3,2,0),Muscovite(1,1,9),Chamosite(0,4,4) | 4.94 |
| 49 | 47.5249 | 1.91167 | Orthoclase(4,0,-3),Calcite(0,1,8) | 10.13 |
| 50 | 48.1193 | 1.88943 | Albite(4,-2,-2),Orthoclase(2,6,0),Clinopyroxene(5,1,-1),Muscovite(2,2,5) | 4.81 |
| 51 | 48.5642 | 1.87315 | Calcite(1,1,6),Titanite(2,3,1),Muscovite(1,3,7) | 4.07 |
| 52 | 49.1892 | 1.85081 | Albite(4,0,-3),Orthoclase(3,-5,-2),Titanite(2,0,2),Clinopyroxene(3,3,1),Chamosite | 3.05 |
| 53 | 50.067(8) | 1.8204(3) | Albite(3,-5,-1),Quartz(1,1,2),Orthoclase(3,-5,0),Titanite(3,3,-1),Clinopyroxene(5,1,0) | 13.26 |
| 54 | 50.597(14) | 1.8026(5) | Albite(4,2,-3),Quartz(0,0,3),Orthoclase(2,0,-4),Titanite(1,4,-2),Clinopyroxene(1,3,2),Muscovite(2,2,6),Chamosite | 7.18 |
| 55 | 51.103(10) | 1.7859(3) | Albite(1,7,-1),Clinopyroxene(2,4,1),Chamosite(0,4,5) | 5.00 |
| 56 | 52.2691 | 1.74876 | Albite(4,2,0),Orthoclase(2,4,2),Titanite(4,0,-2),Chamosite(1,5,0) | 1.29 |
| 57 | 53.22(3) | 1.7198(8) | Albite(2,-4,2),Orthoclase(2,6,1),Titanite(2,4,-2),Clinopyroxene(5,1,-2),Muscovite(2,0,8) | 2.22 |
| 58 | 54.846(16) | 1.6725(4) | Albite(1,7,-2),Quartz(2,0,2),Orthoclase(3,-1,2),Titanite(0,5,1),Clinopyroxene(1,5,-1),Muscovite(3,1,-3) | 6.55 |
| 59 | 56.5298 | 1.62665 | Orthoclase(3,-3,-4),Calcite(2,1,1),Clinopyroxene(2,2,-3),Muscovite(1,5,-4) | 1.38 |
| 60 | 57.38(6) | 1.6045(15) | Albite(3,-1,2),Quartz(2,1,0),Orthoclase(4,2,1),Calcite(1,2,2),Titanite(1,4,2),Clinopyroxene(4,4,0),Muscovite(3,1,-5) | 3.94 |
| 61 | 58.67(4) | 1.5722(10) | Albite(0,2,-4),Orthoclase(0,2,4),Titanite(1,5,1),Chamosite(1,5,4) | 1.54 |
| 62 | 59.920(11) | 1.5425(3) | Albite(5,3,-2),Quartz(2,1,1),Clinopyroxene(3,5,0),Chamosite | 5.47 |
| 63 | 60.64(3) | 1.5258(7) | Albite(0,2,4),Orthoclase(3,7,-2),Calcite(2,1,4),Titanite(3,4,0),Muscovite(1,1,12),Chamosite(3,3,2) | 0.78 |
| 64 | 61.4909 | 1.50677 | Albite(2,8,-1),Orthoclase(4,-6,-1),Calcite(1,1,9),Titanite(1,2,-4),Clinopyroxene(1,3,-3),Chamosite(0,6,2) | 1.47 |

## Phase Data Pattern

# XRD Results-G410245-LJN2021-042-DG-4/6/2021

## General Information

| ### Measurement date: | 11/5/2021 | ### Interpretative date: | 4/6/2021 |
| --- | --- | --- | --- |
| ### Job Number/Client: | LJN2021-42 DG | ### XRD | Rigaku Miniflex 600 |
| ### Registration Number: | G410245 | ### Analyst: | LUnwin |
| ### Quantitative Method: | PDXL Relative Heights | ### Process Medium: | Selective by Client |
| ### Sample Holder: | Low Reflectance | ### Speed (deg/min): | 0.5 |
| ### Comment: | Shifted -0.05 |  |  |

## Analysis Results

| ### Phase name | ### Content% | ### Formula |
| --- | --- | --- |
| Quartz | 29(8) | SiO2 |
| Calcite | 14(4) | CaCO3 |
| Chamosite | 15(4) | (Fe,Mg,Al)6(Si,Al)4O10(OH)8 |
| Albite | 36(10) | NaAlSi3O8 |
| Muscovite* | <1 | KAl2(AlSi3O10)(OH)2 |
| Biotite* | 5(2) | K(Mg,Fe)3[AlSi3O10](OH)2 |

### Notes

Peak overlap may interfere with identifications and quantitative calculations.

Amorphous minerals and minerals present in trace amounts may not be detected.

Muscovite and Biotite* definite double peak observed at approx. 10 d angle

## Peak List

| No. | 2-theta(deg) | d(ang.) | Phase name | Rel. int. I(a.u.) |
| --- | --- | --- | --- | --- |
| 1 | 6.23324 | 14.1681 | Chamosite(0,0,1) | 6.15 |
| 2 | 8.76636 | 10.0789 | Biotite(0,0,2) | 0.75 |
| 3 | 8.86674 | 9.96506 | Muscovite(0,0,1) | 3.23 |
| 4 | 12.484(5) | 7.085(3) | Chamosite(0,0,2) | 31.96 |
| 5 | 13.846(19) | 6.390(9) | Albite(0,0,1) | 2.95 |
| 6 | 14.9733 | 5.91192 | Albite(1,1,-1) | 0.75 |
| 7 | 15.9072 | 5.56689 | Albite(1,-1,-1) | 0.41 |
| 8 | 17.8333 | 4.96974 | Muscovite(0,0,2) | 1.63 |
| 9 | 18.756(14) | 4.727(4) | Chamosite(0,0,3) | 8.69 |
| 10 | 19.234 | 4.61085 | Chamosite(1,-1,0),Biotite(1,1,0) | 2.00 |
| 11 | 19.74(3) | 4.493(6) | Chamosite(1,1,-1),Muscovite(1,1,0),Biotite(0,2,1) | 9.93 |
| 12 | 20.819(7) | 4.2632(13) | Quartz(1,0,0),Chamosite(1,-1,1) | 16.55 |
| 13 | 22.032(7) | 4.0312(12) | Albite(2,0,-1) | 11.98 |
| 14 | 22.90(3) | 3.881(6) | Chamosite(0,2,-2) | 2.83 |
| 15 | 23.034(8) | 3.8580(13) | Calcite(0,1,2),Albite(1,-1,1),Muscovite(1,1,1) | 5.85 |
| 16 | 23.529(10) | 3.7780(16) | Albite(1,1,1) | 8.41 |
| 17 | 24.226(11) | 3.6709(17) | Chamosite(1,-1,2),Albite(1,3,0),Muscovite(1,1,-2),Biotite(1,1,3) | 16.09 |
| 18 | 25.113(8) | 3.5432(11) | Chamosite(0,0,4),Biotite(1,1,-4) | 31.21 |
| 19 | 26.619(4) | 3.3461(5) | Quartz(0,1,1),Albite(2,-2,-1),Muscovite(0,2,2) | 100.00 |
| 20 | 27.881(10) | 3.1974(11) | Albite(0,4,0) | 60.77 |
| 21 | 29.18(6) | 3.058(6) | Muscovite(1,1,2),Biotite(0,2,5) | 8.25 |
| 22 | 29.416(11) | 3.0339(11) | Calcite(1,0,4) | 58.31 |
| 23 | 30.0901 | 2.96749 | Chamosite(1,1,-4),Albite(1,-3,1) | 1.53 |
| 24 | 30.490(11) | 2.9295(10) | Albite(0,4,-1),Biotite(1,1,5) | 13.07 |
| 25 | 31.199 | 2.8645 | Albite(1,3,1) | 3.16 |
| 26 | 31.666 | 2.82332 | Chamosite(0,0,5),Biotite(1,1,-6) | 3.18 |
| 27 | 33.4753 | 2.67474 | Chamosite(1,-3,0),Albite(3,1,-1),Muscovite(0,2,3),Biotite(1,3,0) | 1.20 |
| 28 | 33.8839 | 2.64341 | Albite(1,-3,-2),Biotite(1,3,1) | 1.21 |
| 29 | 34.423(10) | 2.6032(8) | Chamosite(1,-3,1),Muscovite(1,3,-1) | 2.65 |
| 30 | 35.01(3) | 2.561(2) | Chamosite(1,3,-2),Albite(2,4,-1),Biotite(1,3,2) | 17.28 |
| 31 | 35.980(6) | 2.4941(4) | Calcite(1,1,0),Albite(2,-2,1) | 8.85 |
| 32 | 36.503(5) | 2.4595(3) | Quartz(1,1,0),Chamosite(1,-3,2),Albite(2,2,1),Biotite(1,3,3) | 14.57 |
| 33 | 37.480(16) | 2.3976(10) | Chamosite(0,2,5),Albite(2,4,0),Muscovite(1,3,-2),Biotite(1,3,-4) | 8.79 |
| 34 | 38.8449 | 2.31647 | Chamosite(2,-2,-1),Albite(3,3,-1),Biotite(2,2,0) | 1.19 |
| 35 | 39.434(10) | 2.2832(6) | Quartz(1,0,2),Calcite(1,1,3),Albite(1,-1,-3),Muscovite(0,4,0),Biotite(2,2,1) | 16.87 |
| 36 | 39.686(18) | 2.2693(10) | Chamosite(1,-3,3),Albite(2,2,-3),Biotite(0,4,2) | 2.03 |
| 37 | 40.217(16) | 2.2406(9) | Quartz(1,1,1),Chamosite(2,-2,1),Biotite(2,2,-3) | 2.95 |
| 38 | 41.1212 | 2.19334 | Chamosite(1,-3,-4),Albite(1,-5,1),Muscovite(2,2,-2),Biotite(0,4,3) | 1.10 |
| 39 | 42.434(9) | 2.1285(4) | Quartz(2,0,0),Chamosite(2,-2,2),Albite(0,6,0),Muscovite(2,0,2) | 7.36 |
| 40 | 42.705(17) | 2.1156(8) | Albite(1,5,1),Muscovite(2,2,1),Biotite(0,4,4) | 0.97 |
| 41 | 43.170(5) | 2.0939(2) | Calcite(2,0,2),Chamosite(0,2,6),Albite(3,-1,-3) | 9.78 |
| 42 | 45.21(7) | 2.004(3) | Chamosite(0,0,7),Albite(4,0,-2),Muscovite(1,1,4),Biotite(0,2,9) | 6.63 |
| 43 | 45.759(11) | 1.9812(5) | Quartz(2,0,1),Albite(0,2,3),Muscovite(0,0,5),Biotite(2,2,-6) | 2.81 |
| 44 | 47.114(12) | 1.9274(4) | Calcite(0,2,4),Chamosite(1,-1,-7),Albite(2,-2,2),Biotite(1,3,7) | 2.39 |
| 45 | 47.54(2) | 1.9112(9) | Calcite(0,1,8),Biotite(0,4,6) | 16.05 |
| 46 | 48.520(12) | 1.8747(5) | Calcite(1,1,6),Muscovite(0,4,3),Biotite(2,2,-7) | 8.26 |
| 47 | 50.104(12) | 1.8191(4) | Quartz(1,1,2),Albite(4,0,0),Muscovite(0,2,5) | 13.40 |
| 48 | 50.6932 | 1.79937 | Quartz(0,0,3),Chamosite(0,4,-5),Albite(1,1,3),Biotite(1,3,8) | 1.44 |
| 49 | 51.12(4) | 1.7853(12) | Chamosite(1,-1,7),Albite(1,7,-1) | 1.32 |
| 50 | 52.3274 | 1.74695 | Chamosite(1,-5,-1),Albite(4,-2,-3),Muscovite(2,0,-5),Biotite(3,1,-2) | 0.88 |
| 51 | 53.2029 | 1.72025 | Chamosite(1,5,-2),Albite(1,-3,3),Muscovite(1,5,0),Biotite(1,5,2) | 1.65 |
| 52 | 54.82(3) | 1.6733(9) | Quartz(0,2,2),Chamosite(1,5,-3),Albite(4,-4,-1),Muscovite(0,4,4),Biotite(2,2,-9) | 9.24 |
| 53 | 56.413 | 1.62974 | Calcite(2,1,1),Chamosite(1,-5,3),Muscovite(2,2,-5),Biotite(1,5,-5) | 1.03 |
| 54 | 57.41(4) | 1.6037(9) | Calcite(1,2,2),Chamosite(1,5,-4),Muscovite(2,4,-3) | 1.67 |
| 55 | 58.9228 | 1.56616 | Chamosite(2,-2,6),Albite(5,-1,-1),Muscovite(1,5,-3) | 1.50 |
| 56 | 59.605(15) | 1.5498(3) | Chamosite(1,-5,4),Albite(5,-1,-3),Muscovite(0,2,6),Biotite(0,6,0) | 3.06 |
| 57 | 59.904(6) | 1.54282(14) | Quartz(1,2,1),Chamosite(2,-4,-5),Albite(5,3,-2),Muscovite(3,1,-4),Biotite(1,5,6) | 6.15 |
| 58 | 60.671(19) | 1.5252(4) | Calcite(2,1,4),Chamosite(1,3,-8),Albite(3,-3,2),Muscovite(3,3,-1),Biotite(0,4,10) | 1.31 |
| 59 | 61.09(3) | 1.5157(7) | Calcite(2,0,8),Chamosite(2,0,7),Albite(1,-7,2),Muscovite(3,1,2),Biotite(0,6,3) | 3.67 |
| 60 | 61.506(15) | 1.5064(3) | Calcite(1,1,9),Albite(2,8,-1),Muscovite(0,6,1),Biotite(3,1,-8) | 3.19 |

## Phase Data Pattern

# XRD Results-G408246-LJN2021-042-DG-18/5/2021

## General Information

| ### Measurement date: | 11/5/2021 | ### Interpretative date: | 18/5/2021 |
| --- | --- | --- | --- |
| ### Job Number/Client: | LJN2021-042 DG | ### XRD | Rigaku Miniflex 600 |
| ### Registration Number: | G408246 | ### Analyst: | LUnwin |
| ### Quantitative Method: | PDXL Relative heights | ### Process Medium: | Selective by Client |
| ### Sample Holder: | Low Reflectance | ### Speed (deg/min): | 0.5 |
| ### Comment: | Shifted -0.05 |  |  |

## Analysis Results

| ### Phase name | ### Content wt% (± error) | ### Formula |
| --- | --- | --- |
| Quartz | 46(10) | SiO2 |
| Calcite | 23(5) | CaCO3 |
| Orthoclase | 4(2) | (K,Na)AlSi3O8 |
| Albite | 5(3) | NaAlSi3O8 |
| Mg-Chamosite | 16(5) | (Fe,Mg,Al)6(Si,Al)4O10(OH)8 |
| Muscovite | 6(3) | KAl2(AlSi3O10)(OH)2 |

### Notes

Peak overlap may interfere with identifications and quantitative calculations.

Amorphous minerals and minerals present in trace amounts may not be detected.

## Peak List

| No. | 2-theta(deg) | d(ang.) | Phase name | Rel. int. I(a.u.) |
| --- | --- | --- | --- | --- |
| 1 | 6.237(13) | 14.16(3) | Mg-Chamosite(0,0,1) | 4.12 |
| 2 | 8.843(17) | 9.992(19) | Muscovite(0,0,2) | 9.21 |
| 3 | 12.508(8) | 7.071(4) | Mg-Chamosite(0,0,2) | 20.84 |
| 4 | 17.796 | 4.98007 | Muscovite(0,0,4) | 1.85 |
| 5 | 18.9338 | 4.68328 | Mg-Chamosite(0,0,3) | 3.22 |
| 6 | 19.1506 | 4.63076 | Mg-Chamosite(0,2,0),Orthoclase(0,2,1) | 1.34 |
| 7 | 19.76(4) | 4.489(9) | Mg-Chamosite(1,1,-1),Muscovite(1,1,0) | 15.78 |
| 8 | 20.840(6) | 4.2591(13) | Quartz(1,0,0),Mg-Chamosite(1,-1,1),Muscovite(1,1,-2),Orthoclase(2,0,-1) | 15.51 |
| 9 | 22.0692 | 4.02449 | Albite(2,0,-1) | 1.70 |
| 10 | 23.107(10) | 3.8460(17) | Calcite(0,1,2),Mg-Chamosite(0,2,-2),Muscovite(1,1,-3),Orthoclase(2,0,0),Albite(1,-1,1) | 7.20 |
| 11 | 25.163(19) | 3.536(3) | Mg-Chamosite(0,0,4),Muscovite(1,1,-4),Orthoclase(2,2,-1) | 17.46 |
| 12 | 26.623(4) | 3.3455(5) | Quartz(1,0,1),Muscovite(0,0,6),Orthoclase(2,2,0),Albite(2,-2,-1) | 100.00 |
| 13 | 27.4187 | 3.25025 | Orthoclase(0,4,0) | 1.95 |
| 14 | 27.8772 | 3.19782 | Muscovite(1,1,4),Albite(2,0,-2) | 2.23 |
| 15 | 29.400(6) | 3.0355(6) | Calcite(1,0,4) | 53.46 |
| 16 | 30.7998 | 2.90071 | Orthoclase(0,2,2) | 1.82 |
| 17 | 31.5584 | 2.83269 | Calcite(0,0,6),Mg-Chamosite(0,0,5),Orthoclase(2,0,1),Albite(1,3,-2) | 3.14 |
| 18 | 33.5089 | 2.67213 | Mg-Chamosite(1,-3,0),Albite(3,1,-1) | 1.21 |
| 19 | 34.44(2) | 2.6020(16) | Mg-Chamosite(1,-3,1),Muscovite(0,2,0),Orthoclase | 13.08 |
| 20 | 34.91(3) | 2.568(2) | Mg-Chamosite(1,3,-2),Muscovite(0,2,1),Orthoclase(1,1,2),Albite(2,4,-1) | 15.77 |
| 21 | 35.989(16) | 2.4934(10) | Calcite(1,1,0),Muscovite(3,1,1),Albite(2,-2,1) | 6.43 |
| 22 | 36.503(12) | 2.4595(8) | Quartz(1,1,0),Mg-Chamosite(1,-3,2),Muscovite(2,0,6),Albite(1,1,2) | 14.99 |
| 23 | 37.471(10) | 2.3982(6) | Mg-Chamosite(0,2,-5),Muscovite(0,2,3),Orthoclase(3,-3,-1),Albite(1,5,-1) | 9.27 |
| 24 | 39.420(10) | 2.2840(6) | Calcite(1,1,3),Quartz(1,0,2),Muscovite(1,1,-8),Orthoclase(3,3,-2) | 20.68 |
| 25 | 40.24(2) | 2.2395(12) | Quartz(1,1,1),Mg-Chamosite(2,2,1),Muscovite(2,2,0),Orthoclase(2,-2,-3) | 3.50 |
| 26 | 42.432(9) | 2.1286(4) | Quartz(2,0,0),Mg-Chamosite(2,-2,2),Orthoclase(4,0,-2) | 7.93 |
| 27 | 43.177(17) | 2.0936(8) | Calcite(2,0,2),Mg-Chamosite(0,2,6),Muscovite(3,1,-7),Albite(3,-3,0) | 5.50 |
| 28 | 45.0498 | 2.01077 | Mg-Chamosite(1,-1,6),Muscovite(0,0,10),Albite(4,0,-2) | 2.26 |
| 29 | 45.769(18) | 1.9808(7) | Quartz(2,0,1),Mg-Chamosite(2,-2,3),Muscovite(2,2,4),Orthoclase(2,2,2),Albite(4,0,-1) | 12.29 |
| 30 | 47.103(15) | 1.9278(6) | Calcite(0,2,4),Mg-Chamosite(1,-1,-7),Muscovite(0,2,7),Orthoclase(4,0,-3),Albite(2,-2,2) | 1.65 |
| 31 | 47.525(12) | 1.9117(5) | Calcite(0,1,8) | 9.32 |
| 32 | 48.550(15) | 1.8737(5) | Calcite(1,1,6),Orthoclase(3,5,-2) | 11.13 |
| 33 | 50.096(9) | 1.8194(3) | Quartz(1,1,2),Orthoclase(1,7,0),Albite(3,-5,-1) | 12.82 |
| 34 | 54.862(13) | 1.6721(4) | Quartz(2,0,2),Mg-Chamosite(1,5,-3),Muscovite(0,0,12),Orthoclase(5,-1,-1),Albite(4,-4,-1) | 5.03 |
| 35 | 55.251(12) | 1.6612(3) | Quartz(1,0,3),Mg-Chamosite(1,-3,-7),Muscovite(1,3,-3),Orthoclase(1,7,-2),Albite(2,4,2) | 1.87 |
| 36 | 57.43(5) | 1.6032(13) | Calcite(1,2,2),Mg-Chamosite(1,5,-4),Muscovite(5,1,2),Orthoclase(4,-2,-4),Albite(3,-1,2) | 3.11 |
| 37 | 58.89(8) | 1.5670(19) | Mg-Chamosite(2,-2,6),Orthoclase(2,2,3),Albite(5,1,-1) | 0.51 |

## Phase Data Pattern

# XRD Results-G408248-LJN2021-042-DG-17/6/2021

## General Information

| ### Measurement date: | 13/5/2021 | ### Interpretative date: | 17/6/2021 |
| --- | --- | --- | --- |
| ### Job Number/Client: | LJN2021-042 DG | ### XRD | Rigaku Miniflex 600 |
| ### Registration Number: | G408248 | ### Analyst: | LUnwin |
| ### Quantitative Method: | PDXL Relative Heights | ### Process Medium: | Selective by Client |
| ### Sample Holder: | Low Reflectance | ### Speed (deg/min): | 0.5 |
| ### Comment: | Shifted -0.07 |  |  |

## Analysis Results

| ### Phase name | ### Content wt% (± error) | ### Formula |
| --- | --- | --- |
| Quartz | 19(5) | SiO2 |
| Microcline | 29(8) | (K,Na)AlSi3O8 |
| Mg-Chamosite | 9(3) | (Fe,Mg,Al)6(Si,Al)4O10(OH)8 |
| Albite | 28(8) | NaAlSi3O8 |
| Muscovite | 11(4) | KAl2(AlSi3O10)(OH)2 |
| Pyrite | 2(2) | FeS2 |
| Calcite | 1(1) | CaCO3 |
| Smectite | <1 |  |

### Notes

Peak overlap may interfere with identifications and quantitative calculations.

Amorphous minerals and minerals present in trace amounts may not be detected.

## Peak List

| No. | 2-theta(deg) | d(ang.) | Phase name | Rel. int. I(a.u.) |
| --- | --- | --- | --- | --- |
| 1 | 5.74749 | 15.3644 | Smectite(0,0,1) | 0.52 |
| 2 | 6.24(2) | 14.15(5) | Mg-Chamosite(0,0,1) | 6.20 |
| 3 | 8.828(10) | 10.009(11) | Muscovite(0,0,2) | 28.80 |
| 4 | 12.506(5) | 7.072(3) | Mg-Chamosite(0,0,2) | 24.94 |
| 5 | 13.885(11) | 6.373(5) | Microcline(0,2,0),Albite(0,2,0) | 10.32 |
| 6 | 15.002(10) | 5.901(4) | Microcline(1,1,-1),Albite(1,1,-1) | 3.71 |
| 7 | 15.8254 | 5.59547 | Albite(1,-1,-1) | 1.11 |
| 8 | 17.7702 | 4.98725 | Muscovite(0,0,4) | 10.80 |
| 9 | 18.7513 | 4.72845 | Mg-Chamosite(0,0,3) | 4.40 |
| 10 | 19.0911 | 4.64504 | Mg-Chamosite(0,2,0) | 3.13 |
| 11 | 19.692(7) | 4.5047(15) | Microcline(0,2,-1),Mg-Chamosite(1,1,-1),Muscovite(0,2,0),Smectite(0,2,0) | 31.87 |
| 12 | 20.3421 | 4.36212 | Muscovite(0,2,1),Smectite(1,1,-1) | 9.81 |
| 13 | 20.8831 | 4.25033 | Microcline(2,0,-1),Mg-Chamosite(1,-1,1),Muscovite(1,1,-2),Quartz(1,0,0) | 30.92 |
| 14 | 21.5688 | 4.11673 | Mg-Chamosite(1,1,-2),Muscovite(0,2,2) | 3.29 |
| 15 | 22.00(2) | 4.038(4) | Albite(2,0,-1) | 14.50 |
| 16 | 22.5441 | 3.94079 | Microcline(1,1,1),Mg-Chamosite(0,2,-2) | 8.35 |
| 17 | 22.981(17) | 3.867(3) | Microcline(2,0,0),Albite(1,-1,1),Muscovite(1,1,-3),Smectite(1,1,-2),Calcite(0,1,2) | 7.30 |
| 18 | 23.550(17) | 3.775(3) | Microcline(1,3,0),Albite(1,1,1) | 35.97 |
| 19 | 24.27(2) | 3.664(4) | Microcline(1,3,-1),Mg-Chamosite(1,1,2),Albite(1,3,0) | 27.76 |
| 20 | 25.16(2) | 3.536(3) | Microcline(2,2,-1),Mg-Chamosite(0,0,4),Albite(1,1,-2) | 25.38 |
| 21 | 25.590(14) | 3.4782(18) | Microcline(1,-1,-2),Albite(2,2,-1),Muscovite(1,1,-4) | 19.54 |
| 22 | 26.39(4) | 3.374(5) | Albite(1,-1,-2),Smectite(1,1,3) | 29.08 |
| 23 | 26.6206 | 3.34585 | Microcline(2,2,0),Mg-Chamosite(0,2,-3),Albite(2,-2,-1),Muscovite(0,2,4),Quartz(1,0,1) | 100.00 |
| 24 | 27.014(5) | 3.2980(5) | Microcline(2,0,-2),Mg-Chamosite(0,2,3) | 47.36 |
| 25 | 27.487(12) | 3.2423(14) | Microcline(0,4,0),Albite(2,0,-2),Muscovite(1,1,4) | 58.23 |
| 26 | 27.9113 | 3.19398 | Albite(0,0,2) | 47.33 |
| 27 | 28.15(2) | 3.168(2) | Mg-Chamosite(1,-1,3),Albite(2,2,0) | 19.87 |
| 28 | 29.0545 | 3.07087 | Smectite(0,0,5) | 9.76 |
| 29 | 29.4489 | 3.03063 | Calcite(1,0,4) | 11.20 |
| 30 | 29.8718 | 2.98867 | Microcline(1,3,1),Mg-Chamosite(1,1,-4),Albite(1,-3,1),Muscovite(0,2,5) | 25.48 |
| 31 | 30.4286 | 2.93525 | Microcline(2,2,-2),Albite(0,4,-1) | 15.33 |
| 32 | 30.78(3) | 2.903(2) | Microcline(0,4,-1),Smectite(1,-1,4) | 17.82 |
| 33 | 31.2133 | 2.86322 | Albite(1,3,1),Calcite(0,0,6) | 6.44 |
| 34 | 32.28(6) | 2.771(5) | Microcline(1,3,-2) | 8.35 |
| 35 | 33.004(7) | 2.7118(5) | Pyrite(2,0,0) | 11.47 |
| 36 | 33.4019 | 2.68044 | Mg-Chamosite(1,-3,0),Albite(3,1,-1),Muscovite(0,2,6) | 3.90 |
| 37 | 34.3378 | 2.6095 | Microcline(3,-1,-2),Mg-Chamosite(1,-3,1),Muscovite(1,3,0),Smectite(2,0,0) | 16.04 |
| 38 | 34.924(10) | 2.5670(7) | Microcline(2,-2,1),Mg-Chamosite(1,3,-2),Albite(2,4,-1),Muscovite(1,1,6),Smectite(1,3,-1) | 53.46 |
| 39 | 35.6468 | 2.51662 | Albite(1,-1,2),Muscovite(0,0,8) | 6.93 |
| 40 | 36.460(10) | 2.4623(7) | Microcline(1,-5,0),Mg-Chamosite(1,-3,2),Albite(2,2,1),Muscovite(1,3,-3),Quartz(1,1,0),Smectite(2,0,2) | 6.96 |
| 41 | 37.0209 | 2.4263 | Microcline(1,5,-1),Mg-Chamosite(0,2,-5),Albite(1,5,-1),Muscovite(0,2,7),Pyrite(2,1,0) | 4.88 |
| 42 | 37.57(5) | 2.392(3) | Microcline(3,3,-1),Mg-Chamosite(1,3,-3),Albite(2,4,0),Muscovite(2,0,-4) | 31.22 |
| 43 | 38.7446 | 2.32223 | Microcline(1,1,-3),Mg-Chamosite(2,-2,-1),Albite(1,-5,-1),Smectite(1,3,-3) | 1.75 |
| 44 | 39.449 | 2.28237 | Microcline(3,3,-2),Mg-Chamosite(1,-3,3),Albite(1,-1,-3),Quartz(1,0,2),Calcite(1,1,3) | 5.13 |
| 45 | 39.9908 | 2.25269 | Mg-Chamosite(2,-2,1),Albite(3,-3,-1),Muscovite(0,4,0) | 4.31 |
| 46 | 40.6952 | 2.21531 | Microcline(3,-3,0),Mg-Chamosite(0,4,-2),Muscovite(2,0,4),Smectite(1,1,6),Pyrite(2,1,1) | 5.72 |
| 47 | 41.690(13) | 2.1647(7) | Microcline(0,6,0),Mg-Chamosite(2,-2,-3),Albite(1,5,-2),Muscovite(2,2,2),Smectite(1,-3,4) | 12.39 |
| 48 | 42.3812 | 2.131 | Microcline(4,0,-1),Mg-Chamosite(2,2,2),Albite(0,6,0),Muscovite(1,3,5),Quartz(2,0,0) | 11.93 |
| 49 | 43.1876 | 2.09306 | Mg-Chamosite(0,4,-3),Albite(3,-1,-3),Muscovite(1,3,-6),Calcite(2,0,2) | 2.95 |
| 50 | 43.6191 | 2.07335 | Microcline(3,1,1),Mg-Chamosite(2,0,-5),Albite(0,2,-3),Muscovite(2,2,3) | 1.88 |
| 51 | 44.0219 | 2.05531 | Microcline(0,6,-1),Mg-Chamosite(2,2,-4),Muscovite(1,1,-9),Smectite(2,2,3) | 1.73 |
| 52 | 44.8156 | 2.02074 | Microcline(4,-2,-2),Mg-Chamosite(0,0,7),Albite(4,0,-2) | 4.02 |
| 53 | 45.3486 | 1.99821 | Mg-Chamosite(2,-2,3),Albite(4,0,-1),Muscovite(0,0,10) | 8.47 |
| 54 | 45.7884 | 1.98004 | Microcline(2,2,2),Albite(0,6,1),Quartz(2,0,1),Smectite | 6.88 |
| 55 | 46.9804 | 1.93254 | Microcline(3,5,-1),Mg-Chamosite(1,-1,-7),Albite(2,-2,2),Muscovite(1,1,9),Calcite(0,2,4) | 2.79 |
| 56 | 47.3055 | 1.92002 | Microcline(2,-6,-1),Calcite(0,1,8),Pyrite(2,2,0) | 5.58 |
| 57 | 48.1182 | 1.88947 | Microcline(3,3,1),Mg-Chamosite(2,0,-6),Albite(3,5,-1),Muscovite(2,0,-8) | 0.81 |
| 58 | 49.2019 | 1.85036 | Microcline(1,-1,3),Mg-Chamosite(0,2,7),Albite(4,0,-3),Muscovite(1,3,-8) | 2.09 |
| 59 | 50.046(9) | 1.8211(3) | Albite(4,0,0),Quartz(1,1,2),Smectite(1,3,-6) | 8.48 |
| 60 | 50.601(12) | 1.8024(4) | Microcline(2,0,-4),Mg-Chamosite(0,4,-5),Albite(1,1,3),Muscovite(2,2,6),Quartz(0,0,3),Pyrite | 14.55 |
| 61 | 51.19(3) | 1.7832(9) | Microcline(4,4,-2),Mg-Chamosite(1,1,7),Muscovite(1,1,10) | 3.64 |
| 62 | 52.4528 | 1.74307 | Microcline(2,-4,2),Mg-Chamosite(1,-5,1),Albite(4,4,-2),Muscovite(2,2,-8) | 1.67 |
| 63 | 53.2114 | 1.72 | Microcline(2,6,1),Mg-Chamosite(2,0,-7),Albite(2,-6,-2) | 1.62 |
| 64 | 53.7532 | 1.70393 | Mg-Chamosite(2,2,5),Albite(1,-1,-4),Muscovite(2,2,7),Smectite(1,-5,-1) | 1.29 |
| 65 | 54.9452 | 1.66975 | Microcline(3,-5,-3),Mg-Chamosite(1,-5,-3),Albite(4,-4,-2),Muscovite(2,4,-3),Quartz(2,0,2) | 2.92 |
| 66 | 56.298(19) | 1.6328(5) | Microcline(1,7,-2),Mg-Chamosite(3,1,2),Albite(4,4,-3),Muscovite(3,1,2),Smectite(2,4,-3),Calcite(2,1,1),Pyrite(3,1,1) | 39.84 |
| 67 | 59.358(15) | 1.5557(4) | Mg-Chamosite(1,-5,4),Albite(5,-1,-3),Muscovite(1,3,10) | 4.26 |

## Phase Data Pattern

# XRD Results-G408249-LJN2021-042-DG-03/06/2021

## General Information

| ### Measurement date: | 13/5/2021 | ### Interpretative date: | 3/6/2021 |
| --- | --- | --- | --- |
| ### Job Number/Client: | LJN2021-042 DG | ### XRD | Rigaku Miniflex 600 |
| ### Registration Number: | G408249 | ### Analyst: | LUnwin |
| ### Quantitative Method: | PDXL Relative Heights | ### Process Medium: | Selective by Client |
| ### Sample Holder: | Low Reflectance | ### Speed (deg/min): | 0.5 |
| ### Comment: | Shifted -0.09 |  |  |

## Analysis Results

| ### Phase name | ### Content wt% (± error) | ### Formula |
| --- | --- | --- |
| Quartz | 11(4) | SiO2 |
| Albite | 14(5) | NaAlSi3O8 |
| Muscovite | 41(10) | KAl2(AlSi3O10)(OH)2 |
| Halloysite-7 | 35(8) | Al2Si2O5(OH)4 |

### Notes

Peak overlap may interfere with identifications and quantitative calculations.

Amorphous minerals and minerals present in trace amounts may not be detected.

## Peak List

| No. | 2-theta(deg) | d(ang.) | Phase name | Rel. int. I(a.u.) |
| --- | --- | --- | --- | --- |
| 1 | 8.797(5) | 10.044(6) | Muscovite(0,0,3) | 71.42 |
| 2 | 12.0127 | 7.36151 | Halloysite-7 (0,0,1) | 63.36 |
| 3 | 17.709(13) | 5.004(4) | Muscovite(0,0,6),Halloysite-7 (1,0,0) | 32.59 |
| 4 | 19.733(7) | 4.4954(16) | Muscovite(1,0,0),Halloysite-7 (0,2,0) | 98.72 |
| 5 | 20.7883 | 4.2695 | Muscovite(1,0,2),Quartz(1,0,0),Halloysite-7 (1,1,-1) | 13.61 |
| 6 | 21.5278 | 4.12447 | Muscovite(1,0,3),Halloysite-7 (1,-1,-1) | 14.51 |
| 7 | 22.0074 | 4.03566 | Albite(2,0,-1) | 15.52 |
| 8 | 22.880(17) | 3.884(3) | Muscovite(1,0,4),Albite(1,-1,1),Halloysite-7 (0,2,-1) | 53.87 |
| 9 | 23.741 | 3.74475 | Albite(1,3,0),Halloysite-7 (1,0,1) | 28.13 |
| 10 | 24.307(18) | 3.659(3) | Muscovite(1,0,5),Albite(1,3,-1),Halloysite-7 (0,2,1) | 57.96 |
| 11 | 25.3238 | 3.51416 | Albite(1,1,-2),Halloysite-7 (1,-1,1) | 44.81 |
| 12 | 26.592(2) | 3.3493(3) | Muscovite(1,0,6),Albite(2,-2,-1),Quartz(1,0,1),Halloysite-7 (1,-2,0) | 100.00 |
| 13 | 27.81(3) | 3.205(3) | Albite(2,0,-2),Halloysite-7 (1,1,-2) | 49.14 |
| 14 | 29.057(18) | 3.0706(19) | Muscovite(1,0,7),Halloysite-7 (1,-1,-2) | 47.79 |
| 15 | 29.80(3) | 2.996(3) | Albite(1,-3,1),Halloysite-7 (0,3,0) | 42.55 |
| 16 | 30.4509 | 2.93315 | Albite(0,4,-1),Halloysite-7 (0,2,-2) | 11.97 |
| 17 | 31.1933 | 2.86501 | Muscovite(1,0,8),Albite(1,3,1) | 19.92 |
| 18 | 32.006 | 2.79409 | Albite(2,-2,-2),Halloysite-7 (0,3,-1) | 15.26 |
| 19 | 33.3413 | 2.68518 | Muscovite(1,0,9),Albite(2,0,1),Halloysite-7 (0,3,1) | 13.03 |
| 20 | 34.956(17) | 2.5647(12) | Muscovite(1,1,0),Albite(2,4,-1),Halloysite-7 (2,0,-1) | 86.19 |
| 21 | 35.94(4) | 2.497(3) | Muscovite(1,1,3),Albite(2,-2,1),Halloysite-7 (2,0,0) | 17.58 |
| 22 | 36.4726 | 2.46151 | Muscovite(1,1,4),Albite(1,1,2),Halloysite-7 (1,-3,-1) | 23.37 |
| 23 | 37.5909 | 2.39081 | Muscovite(1,1,5),Albite(2,4,0),Halloysite-7 (2,1,0) | 52.80 |
| 24 | 39.4318 | 2.28333 | Muscovite(1,1,-6),Albite(1,-1,-3),Quartz(1,0,2),Halloysite-7 (1,3,-2) | 7.76 |
| 25 | 39.9708 | 2.25377 | Muscovite(2,0,0),Albite(3,-3,-1),Halloysite-7 (2,2,-1) | 11.34 |
| 26 | 40.6752 | 2.21635 | Muscovite(2,0,1),Albite(2,-4,-2),Quartz(1,1,1),Halloysite-7 (2,-2,-1) | 11.90 |
| 27 | 41.9214 | 2.1533 | Muscovite(2,0,4),Albite(1,5,-2),Halloysite-7 (1,-3,-2) | 19.55 |
| 28 | 42.3567 | 2.13218 | Muscovite(1,1,-8),Albite(0,6,0),Halloysite-7 (2,1,1) | 13.48 |
| 29 | 45.33(3) | 1.9988(13) | Muscovite(0,0,15),Albite(1,-3,-3),Halloysite-7 (2,-2,1) | 46.77 |
| 30 | 46.49(3) | 1.9517(12) | Muscovite(1,1,-10),Albite(4,2,-2),Halloysite-7 (2,2,1) | 12.59 |
| 31 | 50.1237 | 1.81847 | Muscovite(1,0,15),Albite(3,-3,1),Quartz(1,1,2),Halloysite-7 (1,-3,-3) | 10.14 |
| 32 | 53.8957 | 1.69976 | Muscovite(2,1,0),Albite(1,-1,-4),Halloysite-7 (2,3,-3) | 10.68 |
| 33 | 55.1474 | 1.66411 | Muscovite(2,1,3),Albite(1,3,3),Quartz(2,0,2),Halloysite-7 (3,1,-2) | 32.31 |
| 34 | 55.7921 | 1.64639 | Muscovite(2,1,4),Albite(2,6,-3),Halloysite-7 (0,2,4) | 21.41 |
| 35 | 56.3208 | 1.63219 | Muscovite(1,0,17),Halloysite-7 (1,3,-4) | 10.78 |
| 36 | 57.6885 | 1.5967 | Muscovite(2,1,6),Albite(0,8,0),Quartz(2,1,0),Halloysite-7 (2,-4,-2) | 6.83 |

## Phase Data Pattern

# XRD Results-G408250-LJN2021-042-DG-03/06/2021

## General Information

| ### Measurement date: | 13/5/2021 | ### Interpretative date: | 3/6/2021 |
| --- | --- | --- | --- |
| ### Job Number/Client: | LJN2021-042 DG | ### XRD | Rigaku Miniflex 600 |
| ### Registration Number: | G408250 | ### Analyst: | LUnwin |
| ### Quantitative Method: | PDXL Relative Heights | ### Process Medium: | Selective by Client |
| ### Sample Holder: | Low Reflectance | ### Speed (deg/min): | 0.5 |
| ### Comment: | Shifted -0.03 |  |  |

## Analysis Results

| ### Phase name | ### Content wt% (± error) | ### Formula |
| --- | --- | --- |
| Quartz | 35(10) | SiO2 |
| Kaolinite | 45(10) | Al2(Si2O5)(OH)4 |
| Calcite | 1(1) | CaCO3 |
| Illite | 15(4) | K0.7Al2[Al0.7Si3.3O10](OH)2 |
| Orthoclase | 2(2) | K(AlSi3O8) |
| Albite | 2(2) | NaAlSi3O8 |

### Notes

Peak overlap may interfere with identifications and quantitative calculations.

Amorphous minerals and minerals present in trace amounts may not be detected.

## Peak List

| No. | 2-theta(deg) | d(ang.) | Phase name | Rel. int. I(a.u.) |
| --- | --- | --- | --- | --- |
| 1 | 8.827(6) | 10.010(7) | Illite(0,0,1) | 28.55 |
| 2 | 12.356(5) | 7.158(3) | Kaolinite(0,0,1) | 24.68 |
| 3 | 17.786(14) | 4.983(4) | Illite(0,0,2) | 10.40 |
| 4 | 19.784(16) | 4.484(4) | Kaolinite(0,2,0),Illite(0,2,0) | 14.11 |
| 5 | 20.844(6) | 4.2582(12) | Quartz(1,0,0) | 22.30 |
| 6 | 21.5993 | 4.11098 | Kaolinite(1,-1,-1),Illite(0,2,1) | 2.97 |
| 7 | 22.0593 | 4.02628 | Albite(2,0,-1) | 2.01 |
| 8 | 23.1063 | 3.84615 | Kaolinite(0,2,-1),Illite(1,1,1),Orthoclase(2,0,0),Albite(1,-1,1),Calcite(0,1,2) | 3.78 |
| 9 | 24.864(4) | 3.5781(6) | Kaolinite(0,0,2),Illite(1,1,-2) | 20.35 |
| 10 | 25.300(14) | 3.5174(19) | Orthoclase(2,2,-1),Albite(1,1,-2) | 6.29 |
| 11 | 26.617(4) | 3.3463(5) | Quartz(1,0,1),Kaolinite(1,0,-2),Illite(0,2,2),Albite | 100.00 |
| 12 | 27.4608 | 3.24535 | Kaolinite(1,2,-1),Orthoclase(0,4,0),Albite(2,0,-2) | 2.86 |
| 13 | 29.431(14) | 3.0324(14) | Calcite(1,0,4) | 7.68 |
| 14 | 32.01(4) | 2.793(3) | Kaolinite(1,2,1),Orthoclase(2,0,1),Albite(2,-2,-2) | 8.46 |
| 15 | 34.94(3) | 2.5656(19) | Kaolinite(1,-3,0),Illite(1,3,0),Orthoclase(3,1,-2),Albite(2,4,-1) | 10.71 |
| 16 | 36.01(3) | 2.4918(19) | Kaolinite(1,-3,-1),Illite(0,0,4),Orthoclase(3,1,0),Albite(2,-2,1),Calcite(1,1,0) | 2.21 |
| 17 | 36.515(7) | 2.4587(4) | Quartz(1,1,0),Illite(1,3,1),Orthoclase(1,5,0),Albite | 6.84 |
| 18 | 37.636(16) | 2.3881(10) | Kaolinite(2,1,0),Illite(2,0,1),Orthoclase(2,0,-3),Albite(2,-4,0) | 3.75 |
| 19 | 38.367(18) | 2.3442(10) | Kaolinite(2,0,-2),Albite(2,4,-2) | 1.69 |
| 20 | 39.446(9) | 2.2825(5) | Quartz(1,0,2),Albite(1,-1,-3),Calcite(1,1,3) | 4.53 |
| 21 | 40.233(7) | 2.2397(4) | Quartz(1,1,1),Kaolinite(0,4,0),Illite(2,2,-1),Orthoclase(2,2,-3),Albite(1,-3,2) | 2.62 |
| 22 | 42.421(11) | 2.1291(5) | Quartz(2,0,0),Kaolinite(2,-1,1),Illite(1,3,-3),Orthoclase(2,4,1),Albite(0,6,0) | 7.50 |
| 23 | 45.42(3) | 1.9951(12) | Kaolinite(2,0,-3),Illite(0,0,5),Orthoclase(4,2,-1),Albite(4,0,-2) | 8.26 |
| 24 | 45.743(6) | 1.9819(3) | Quartz(2,0,1),Kaolinite(2,-2,1),Albite(3,-1,1) | 1.45 |
| 25 | 50.098(5) | 1.81933(16) | Quartz(1,1,2),Orthoclase(3,5,0),Albite(3,-3,1) | 9.02 |
| 26 | 51.02(3) | 1.7885(10) | Kaolinite(0,0,4),Illite(2,2,-4),Albite(1,7,-1) | 1.03 |
| 27 | 52.8179 | 1.73188 | Kaolinite(0,5,-1),Illite(2,2,3),Orthoclase(1,5,-3),Albite(4,4,-2) | 3.91 |
| 28 | 54.880(8) | 1.6716(2) | Quartz(2,0,2),Kaolinite(2,-4,0),Illite(0,4,4),Orthoclase(3,5,-3),Albite(1,-5,-3) | 2.03 |
| 29 | 55.36(4) | 1.6583(11) | Quartz(1,0,3),Kaolinite(1,-5,-1),Illite(0,0,6),Orthoclase(3,1,2),Albite(4,-4,-1) | 5.51 |

## Phase Data Pattern

# XRD Results-G408251-LJN2021-042-DG-03/06/2021

## General Information

| ### Measurement date: | 14/5/2021 | ### Interpretative date: | 03/06/2021 |
| --- | --- | --- | --- |
| ### Job Number/Client: | LJN2021-042 DG | ### XRD | Rigaku Miniflex 600 |
| ### Registration Number: | G408251 | ### Analyst: | LUnwin |
| ### Quantitative Method: | PDXL Relative Heights | ### Process Medium: | Selective by Client |
| ### Sample Holder: | Low Reflectance | ### Speed (deg/min): | 0.5 |
| ### Comment: | Shifted -0.09 |  |  |

## Analysis Results

| ### Phase name | ### Content wt% (± error) | ### Formula |
| --- | --- | --- |
| Quartz | 31(8) | SiO2 |
| Kaolinite | 44(10) | Al2(Si2O5)(OH)4 |
| Illite | 16(5) | K0.7Al2[Al0.7Si3.3O10](OH)2 |
| Orthoclase | 2(2) | K(AlSi3O8) |
| Albite | 4(2) | NaAlSi3O8 |
| Mg-Calcite | 3(2) | (Ca,Mg)CO3 |

### Notes

Peak overlap may interfere with identifications and quantitative calculations.

Amorphous minerals and minerals present in trace amounts may not be detected.

## Peak List

| No. | 2-theta(deg) | d(ang.) | Phase name | Rel. int. I(a.u.) |
| --- | --- | --- | --- | --- |
| 1 | 8.820(6) | 10.018(7) | Illite(0,0,1) | 19.95 |
| 2 | 12.350(5) | 7.161(3) | Kaolinite(0,0,2) | 21.96 |
| 3 | 17.704(13) | 5.006(4) | Illite(0,0,2) | 6.37 |
| 4 | 19.777(6) | 4.4854(13) | Kaolinite(1,1,-1),Illite(0,2,0),Orthoclase(0,2,1) | 16.53 |
| 5 | 20.8403 | 4.25895 | Quartz(1,0,0),Kaolinite(0,2,1),Illite(1,1,-1) | 18.77 |
| 6 | 23.1201 | 3.8439 | Illite(1,1,1),Orthoclase(2,0,0),Mg-Calcite(0,1,2),Albite(1,-1,1) | 2.47 |
| 7 | 24.841(9) | 3.5814(13) | Kaolinite(0,0,4),Illite(1,1,-2),Orthoclase(1,3,-1) | 21.53 |
| 8 | 25.26(3) | 3.523(4) | Kaolinite(1,1,-3),Orthoclase(2,2,-1),Albite(1,1,-2) | 3.70 |
| 9 | 26.611(4) | 3.3470(4) | Quartz(0,1,1),Illite(0,2,2),Albite(2,-2,-1) | 100.00 |
| 10 | 27.492(19) | 3.242(2) | Kaolinite(0,2,3),Orthoclase(2,0,-2),Albite(2,0,-2) | 2.84 |
| 11 | 29.414(10) | 3.0342(10) | Mg-Calcite(1,0,4) | 4.58 |
| 12 | 32.030(12) | 2.7921(10) | Kaolinite(0,2,4),Orthoclase(2,0,1),Albite(2,-2,-2) | 20.62 |
| 13 | 34.94(4) | 2.566(3) | Kaolinite(1,1,4),Illite(1,3,0),Orthoclase(3,1,-2),Albite(2,4,-1) | 12.29 |
| 14 | 36.0155 | 2.49169 | Kaolinite(1,3,-2),Illite(1,1,3),Orthoclase(3,1,0),Mg-Calcite(1,1,0),Albite(3,-1,-2) | 2.34 |
| 15 | 36.490(15) | 2.4604(10) | Quartz(1,1,0),Illite(1,3,1),Orthoclase(2,4,0),Albite(2,2,1) | 8.02 |
| 16 | 37.70(3) | 2.3842(16) | Kaolinite(0,0,6),Illite(2,0,1),Orthoclase(1,5,-1),Albite(3,1,0) | 3.99 |
| 17 | 38.359(11) | 2.3447(7) | Kaolinite(1,3,2),Orthoclase(2,0,-3),Albite(2,4,-2) | 3.42 |
| 18 | 39.416(4) | 2.2842(2) | Quartz(1,0,2),Orthoclase(2,4,-2),Mg-Calcite(1,1,3),Albite(1,-1,-3) | 4.88 |
| 19 | 40.240(4) | 2.23930(19) | Quartz(1,1,1),Illite(0,4,0),Orthoclase(3,3,-2),Albite(1,-3,2) | 3.10 |
| 20 | 42.429(13) | 2.1287(6) | Quartz(2,0,0),Kaolinite(2,2,1),Illite(1,3,-3),Orthoclase(0,0,3),Albite(0,6,0) | 10.74 |
| 21 | 45.737(11) | 1.9822(4) | Quartz(2,0,1),Kaolinite(1,1,6),Illite(2,2,-3),Orthoclase(4,2,-1),Albite(0,2,3) | 15.13 |
| 22 | 47.9898 | 1.89422 | Kaolinite(2,2,3),Illite(2,0,3),Orthoclase(2,4,-3),Albite(3,5,-1) | 1.03 |
| 23 | 50.113(8) | 1.8188(3) | Quartz(1,1,2),Orthoclase(1,5,2),Albite(3,-3,1) | 9.30 |
| 24 | 51.0241 | 1.78847 | Kaolinite(0,0,8),Illite(2,2,-4),Orthoclase(2,6,-2),Albite(1,7,-1) | 1.81 |
| 25 | 52.90(6) | 1.7295(18) | Illite(2,2,3),Orthoclase(1,5,-3),Albite(1,1,-4) | 5.10 |
| 26 | 54.831(11) | 1.6730(3) | Quartz(0,2,2),Kaolinite(3,1,-1),Illite(3,1,0),Orthoclase(5,1,-2),Albite(1,-5,-3) | 7.38 |

## Phase Data Pattern

# XRD Results-G408253-LJN2021-042-DG-03/06/2021

## General Information

| ### Measurement date: | 14/5/2021 | ### Interpretative date: | 03/06/2021 |
| --- | --- | --- | --- |
| ### Job Number/Client: | LJN2021-042 DG | ### XRD | Rigaku Miniflex 600 |
| ### Registration Number: | G408253 | ### Analyst: | LUnwin |
| ### Quantitative Method: | PDXL Relative Heights | ### Process Medium: | Selective by Client |
| ### Sample Holder: | Low Reflectance | ### Speed (deg/min): | 0.5 |
| ### Comment: | Shifted -0.09 |  |  |

## Analysis Results

| ### Phase name | ### Content wt% (± error) | ### Formula |
| --- | --- | --- |
| Quartz | 30(8) | SiO2 |
| Muscovite | 36(10) | KAl2(AlSi3O10)(OH)2 |
| Mg-Chamosite | 30(8) | (Fe,Mg,Al)6(Si,Al)4O10(OH)8 |
| Albite | 1(1) | NaAlSi3O8 |
| Orthoclase | 3(2) | K(AlSi3O8) |

### Notes

Peak overlap may interfere with identifications and quantitative calculations.

Amorphous minerals and minerals present in trace amounts may not be detected.

## Peak List

| No. | 2-theta(deg) | d(ang.) | Phase name | Rel. int. I(a.u.) |
| --- | --- | --- | --- | --- |
| 1 | 6.224(4) | 14.190(10) | Chamosite(0,0,1) | 11.64 |
| 2 | 8.840(2) | 9.995(3) | Muscovite(0,0,2) | 39.12 |
| 3 | 12.487(2) | 7.0832(14) | Chamosite(0,0,2) | 38.51 |
| 4 | 17.754(4) | 4.9917(12) | Muscovite(0,0,4) | 15.10 |
| 5 | 18.799(6) | 4.7165(14) | Chamosite(0,0,3) | 9.29 |
| 6 | 19.17(2) | 4.626(5) | Chamosite(0,2,0),Orthoclase(0,2,1) | 0.23 |
| 7 | 19.807(9) | 4.479(2) | Muscovite(0,2,0),Chamosite(0,2,-1) | 4.48 |
| 8 | 20.816(5) | 4.2639(10) | Quartz(1,0,0),Chamosite(1,-1,1),Orthoclase(2,0,-1) | 18.64 |
| 9 | 21.5134 | 4.1272 | Muscovite(0,2,2) | 0.91 |
| 10 | 22.0871 | 4.02129 | Albite(2,0,-1) | 0.40 |
| 11 | 22.86(3) | 3.887(5) | Muscovite(1,1,-3),Chamosite(0,2,-2),Orthoclase(2,0,0) | 2.56 |
| 12 | 23.762(5) | 3.7416(8) | Muscovite(0,2,3) | 2.56 |
| 13 | 25.138(5) | 3.5397(7) | Chamosite(0,0,4) | 25.32 |
| 14 | 25.462(8) | 3.4953(11) | Muscovite(1,1,-4),Chamosite(1,1,-3),Orthoclase(1,1,-2),Albite(1,1,-2) | 4.80 |
| 15 | 26.631(6) | 3.3446(8) | Quartz(0,1,1),Muscovite(0,2,4),Orthoclase(2,2,0) | 100.00 |
| 16 | 27.4496 | 3.24666 | Orthoclase(0,0,2) | 1.72 |
| 17 | 27.82(3) | 3.204(4) | Albite(2,0,-2) | 4.95 |
| 18 | 28.6316 | 3.11525 | Muscovite(1,1,-5) | 1.00 |
| 19 | 29.803(3) | 2.9954(3) | Muscovite(0,2,5),Chamosite(1,1,-4),Orthoclase(1,3,1) | 8.90 |
| 20 | 31.222(13) | 2.8624(12) | Albite(1,3,1) | 6.07 |
| 21 | 31.592(8) | 2.8298(7) | Chamosite(0,0,5),Orthoclase(2,0,1),Albite(1,3,-2) | 4.31 |
| 22 | 32.047(13) | 2.7906(11) | Muscovite(1,1,-6),Orthoclase(3,1,-1),Albite(2,-2,-2) | 6.05 |
| 23 | 33.0198 | 2.71058 | Muscovite(0,2,6),Chamosite(1,-3,0) | 1.71 |
| 24 | 34.465(15) | 2.6001(11) | Muscovite(1,3,0),Chamosite(1,-3,1),Orthoclase(2,2,1) | 3.83 |
| 25 | 34.92(2) | 2.5673(15) | Muscovite(2,0,-2),Chamosite(1,3,-2),Orthoclase(1,1,2),Albite(2,4,-1) | 8.07 |
| 26 | 35.969(19) | 2.4948(13) | Muscovite(1,3,2),Orthoclase(2,4,0),Albite(2,-2,1) | 4.84 |
| 27 | 36.496(7) | 2.4600(5) | Quartz(1,1,0),Muscovite(1,3,-3),Chamosite(1,-3,2),Albite(1,1,2) | 8.97 |
| 28 | 37.56(4) | 2.393(2) | Muscovite(0,2,7),Chamosite(0,2,5),Orthoclase(3,3,-1),Albite(2,4,0) | 4.56 |
| 29 | 39.402(6) | 2.2850(3) | Quartz(1,0,2),Chamosite(1,-3,3),Orthoclase(3,3,-2) | 5.18 |
| 30 | 39.704(13) | 2.2683(7) | Muscovite(1,3,4),Chamosite(2,0,-4),Albite(1,-1,-3) | 0.98 |
| 31 | 39.965(7) | 2.2541(4) | Muscovite(0,4,0),Albite(2,2,-3) | 0.54 |
| 32 | 40.222(6) | 2.2403(3) | Quartz(1,1,1),Muscovite(0,4,1),Chamosite(2,2,1),Orthoclase(2,2,-3),Albite(3,-3,-1) | 2.97 |
| 33 | 40.73(2) | 2.2135(11) | Muscovite(2,0,4),Chamosite(0,4,-2),Orthoclase(3,3,0),Albite(1,-3,2) | 0.82 |
| 34 | 42.407(8) | 2.1298(4) | Quartz(2,0,0),Chamosite(2,2,2),Orthoclase(4,0,-1),Albite(3,-3,-2) | 7.51 |
| 35 | 44.0635 | 2.05347 | Muscovite(0,4,4),Orthoclase(0,2,3),Albite(0,2,-3) | 0.61 |
| 36 | 45.02(4) | 2.0122(17) | Muscovite(2,2,-5),Chamosite(0,0,7),Orthoclase(4,2,-1),Albite(2,4,1) | 6.96 |
| 37 | 45.390(8) | 1.9965(3) | Muscovite(0,2,9),Chamosite(2,-2,3),Albite(4,0,-1) | 21.82 |
| 38 | 47.3237 | 1.91932 | Orthoclase(4,0,-3),Albite(2,-2,2) | 0.56 |
| 39 | 48.17(4) | 1.8875(15) | Muscovite(2,0,-8),Chamosite(2,-2,-5),Orthoclase(3,3,1),Albite(4,-2,-2) | 1.48 |
| 40 | 50.098(7) | 1.8194(2) | Quartz(1,1,2),Orthoclase(2,6,-2),Albite(3,-5,-1) | 12.01 |
| 41 | 52.76(5) | 1.7337(14) | Muscovite(1,1,-11),Chamosite(1,-5,1),Orthoclase(1,1,-4),Albite(4,4,-2) | 1.99 |
| 42 | 54.828(8) | 1.6731(2) | Quartz(0,2,2),Muscovite(2,4,-3),Chamosite(1,5,-3) | 3.08 |
| 43 | 55.25(2) | 1.6612(6) | Quartz(0,1,3),Muscovite(1,5,-3),Chamosite(2,0,6),Orthoclase(4,0,1),Albite(4,-4,-2) | 4.20 |
| 44 | 55.732(14) | 1.6480(4) | Muscovite(3,1,2),Chamosite(3,1,-4),Albite(1,3,3) | 2.75 |
| 45 | 56.2894 | 1.63302 | Muscovite(1,5,-4),Chamosite(1,-5,3),Orthoclase(5,1,-3),Albite(2,6,-3) | 1.40 |
| 46 | 57.2131 | 1.60883 | Quartz(2,1,0),Muscovite(2,2,8),Chamosite(2,-2,-7),Orthoclase(2,6,-3),Albite(3,-1,2) | 0.92 |
| 47 | 58.93(4) | 1.5660(11) | Muscovite(3,1,-6),Chamosite(1,-3,7),Orthoclase(5,3,-1),Albite(0,2,-4) | 1.65 |

## Phase Data Pattern

# XRD Results-G408254-LJN2021-042-DG-17/06/2021

## General Information

| ### Measurement date: | 14/5/2021 | ### Interpretative date: | 17/06/2021 |
| --- | --- | --- | --- |
| ### Job Number/Client: | LJN2021-042 DG | ### XRD | Rigaku Miniflex 600 |
| ### Registration Number: | G408254 | ### Analyst: | LUnwin |
| ### Quantitative Method: | PDXL Relative Heights | ### Process Medium: | Selective by Client |
| ### Sample Holder: | Low Reflectance | ### Speed (deg/min): | 0.5 |
| ### Comment: | Shifted -0.05 |  |  |

## Analysis Results

| ### Phase name | ### Content wt% (± error) | ### Formula |
| --- | --- | --- |
| Quartz | 70(10) | SiO2 |
| Mg-Chamosite | 10(4) | (Fe,Mg,Al)6(Si,Al)4O10(OH)8 |
| Muscovite | 2(2) | KAl2(AlSi3O10)(OH)2 |
| Albite | 8(3) | NaAlSi3O8 |
| Clinopyroxene | 11(4) | (Ca,Na)(Mg,Fe,Al)Si2O6 |

### Notes

Peak overlap may interfere with identifications and quantitative calculations.

Amorphous minerals and minerals present in trace amounts may not be detected.

## Peak List

| No. | 2-theta(deg) | d(ang.) | Phase name | Rel. int. I(a.u.) |
| --- | --- | --- | --- | --- |
| 1 | 6.239(9) | 14.15(2) | Mg-Chamosite(0,0,1) | 1.61 |
| 2 | 8.856(5) | 9.977(6) | Muscovite(0,0,2) | 4.05 |
| 3 | 12.494(5) | 7.079(3) | Mg-Chamosite(0,0,2) | 5.73 |
| 4 | 13.841(4) | 6.3931(19) | Albite(0,2,0),Clinopyroxene(1,1,0) | 0.81 |
| 5 | 17.767(9) | 4.988(3) | Muscovite(0,0,4) | 1.48 |
| 6 | 18.8071(13) | 4.7146(3) | Mg-Chamosite(0,0,3) | 1.30 |
| 7 | 19.83(3) | 4.474(6) | Muscovite(1,1,0) | 0.94 |
| 8 | 20.827(3) | 4.2615(6) | Quartz(1,0,0),Mg-Chamosite(1,-1,1),Muscovite(1,1,1) | 17.39 |
| 9 | 22.024(4) | 4.0327(7) | Albite(2,0,-1) | 1.08 |
| 10 | 23.0549 | 3.85462 | Mg-Chamosite(0,2,2),Albite(1,-1,1) | 0.45 |
| 11 | 23.525(10) | 3.7787(16) | Muscovite(2,0,2),Albite(1,1,1) | 1.43 |
| 12 | 24.310(10) | 3.6584(15) | Mg-Chamosite(1,1,2),Muscovite(2,0,-4),Albite(1,3,0) | 2.44 |
| 13 | 25.145(13) | 3.5388(17) | Mg-Chamosite(0,0,4) | 3.80 |
| 14 | 25.41(4) | 3.502(5) | Mg-Chamosite(1,1,-3),Muscovite(1,1,-4),Albite(1,1,-2) | 1.85 |
| 15 | 26.618(3) | 3.3462(4) | Quartz(0,1,1),Albite(2,-2,-1) | 100.00 |
| 16 | 27.903(4) | 3.1950(5) | Muscovite(1,1,4),Albite(0,0,2),Clinopyroxene(2,2,0) | 10.36 |
| 17 | 28.296(17) | 3.1515(19) | Mg-Chamosite(1,-1,3),Albite(2,2,0) | 1.07 |
| 18 | 29.8671 | 2.98914 | Clinopyroxene(2,2,-1) | 1.12 |
| 19 | 30.1167 | 2.96493 | Mg-Chamosite(1,1,-4),Albite(1,-3,1) | 0.76 |
| 20 | 30.4731 | 2.93106 | Muscovite(2,0,-6),Albite(0,4,-1) | 0.66 |
| 21 | 30.7982 | 2.90086 | Clinopyroxene(3,1,0) | 0.95 |
| 22 | 31.175(6) | 2.8666(6) | Albite(1,3,1) | 0.76 |
| 23 | 31.6146 | 2.82779 | Mg-Chamosite(0,0,5),Albite(1,3,-2) | 0.53 |
| 24 | 31.971(12) | 2.7971(10) | Mg-Chamosite(0,2,4),Muscovite(1,1,-6),Albite(2,-2,-2),Clinopyroxene(1,3,0) | 0.91 |
| 25 | 34.469(15) | 2.5999(11) | Mg-Chamosite(1,-3,1) | 0.77 |
| 26 | 34.99(2) | 2.5620(15) | Mg-Chamosite(1,3,-2),Muscovite(3,1,-2),Albite(2,4,-1),Clinopyroxene(1,3,-1) | 2.43 |
| 27 | 35.9328 | 2.49724 | Muscovite(0,2,2),Albite(2,-2,1) | 0.41 |
| 28 | 36.509(7) | 2.4591(5) | Quartz(1,1,0),Mg-Chamosite(1,-3,2),Albite(1,1,2) | 7.39 |
| 29 | 37.57(2) | 2.3922(13) | Mg-Chamosite(0,2,5),Muscovite(3,1,2),Albite(2,4,0) | 1.20 |
| 30 | 39.421(4) | 2.2839(2) | Quartz(1,0,2) | 5.82 |
| 31 | 40.253(7) | 2.2386(4) | Quartz(1,1,1),Mg-Chamosite(2,-2,1),Muscovite(2,2,-1),Albite(3,-3,-1) | 3.36 |
| 32 | 41.185(19) | 2.1901(10) | Mg-Chamosite(1,-3,-4),Muscovite(2,2,1),Albite(2,-4,-2),Clinopyroxene(1,1,2) | 0.47 |
| 33 | 42.413(6) | 2.1295(3) | Quartz(2,0,0),Mg-Chamosite(2,-2,2),Albite(0,6,0),Clinopyroxene(3,3,0) | 4.83 |
| 34 | 42.662(17) | 2.1176(8) | Muscovite(2,2,-4),Albite(3,3,0),Clinopyroxene(3,3,-1) | 0.37 |
| 35 | 43.537(11) | 2.0770(5) | Mg-Chamosite(0,4,3),Muscovite(3,1,-7),Albite(2,-4,1) | 0.26 |
| 36 | 45.47(2) | 1.9933(10) | Mg-Chamosite(1,3,-5),Muscovite(3,1,5),Albite(4,0,-2),Clinopyroxene(2,4,0) | 3.90 |
| 37 | 45.775(3) | 1.98058(13) | Quartz(2,0,1),Albite(0,6,1),Clinopyroxene(2,0,2) | 3.00 |
| 38 | 48.15(8) | 1.888(3) | Mg-Chamosite(2,2,-5),Muscovite(4,0,4),Albite(4,-2,-2),Clinopyroxene(5,1,-1) | 0.49 |
| 39 | 50.096(6) | 1.8194(2) | Quartz(1,1,2),Albite(3,-5,-1) | 12.32 |
| 40 | 50.6583 | 1.80052 | Quartz(0,0,3),Mg-Chamosite(0,4,-5),Albite(1,1,3) | 0.46 |
| 41 | 50.9843 | 1.78977 | Mg-Chamosite(0,4,5),Albite(3,3,1) | 0.33 |
| 42 | 54.848(11) | 1.6725(3) | Quartz(0,2,2),Mg-Chamosite(1,5,-3),Muscovite(5,1,-4),Albite(1,7,-2) | 3.33 |
| 43 | 55.295(16) | 1.6600(4) | Quartz(0,1,3),Mg-Chamosite(2,0,6),Muscovite(0,0,12),Clinopyroxene | 1.49 |
| 44 | 56.50(7) | 1.6274(19) | Mg-Chamosite(1,-5,3),Muscovite(1,1,11),Clinopyroxene(2,2,-3) | 0.06 |
| 45 | 57.170(18) | 1.6099(5) | Quartz(2,1,0),Mg-Chamosite(2,2,-7),Muscovite(1,1,-12),Albite(3,-1,2),Clinopyroxene(1,5,1) | 0.11 |
| 46 | 59.567(17) | 1.5508(4) | Mg-Chamosite(1,-5,4),Albite(5,-1,-3) | 0.37 |
| 47 | 59.915(5) | 1.54258(12) | Quartz(1,2,1),Mg-Chamosite(2,-4,-5),Muscovite | 11.31 |

## Phase Data Pattern

# XRD Results-G408255-LJN2021-042-DG-17/06/2021

## General Information

| ### Measurement date: | 17/5/2021 | ### Interpretative date: | 17/06/2021 |
| --- | --- | --- | --- |
| ### Job Number/Client: | LJN2021-042 DG | ### XRD | Rigaku Miniflex 600 |
| ### Registration Number: | G408255 | ### Analyst: | LUnwin |
| ### Quantitative Method: | PDXL Relative Heights | ### Process Medium: | Selective by Client |
| ### Sample Holder: | Low Reflectance | ### Speed (deg/min): | 0.5 |
| ### Comment: | Shifted -0.08 |  |  |

## Analysis Results

| ### Phase name | ### Content wt% (± error) | ### Formula |
| --- | --- | --- |
| Quartz | 25(5) | SiO2 |
| Mg-Chamosite | 15(4) | (Fe,Mg,Al)6(Si,Al)4O10(OH)8 |
| Albite | 24(5) | NaAlSi3O8 |
| Muscovite | 5(2) | KAl2(AlSi3O10)(OH)2 |
| Orthoclase | 24(5) | K(AlSi3O8) |
| Clinopyroxene | 7()3 | (Ca,Na)(Mg,Fe,Al)Si2O6 |

### Notes

Peak overlap may interfere with identifications and quantitative calculations.

Amorphous minerals and minerals present in trace amounts may not be detected.

## Peak List

| No. | 2-theta(deg) | d(ang.) | Phase name | Rel. int. I(a.u.) |
| --- | --- | --- | --- | --- |
| 1 | 6.254(14) | 14.12(3) | Mg-Chamosite(0,0,1) | 8.94 |
| 2 | 8.885(5) | 9.945(5) | Muscovite(0,0,2) | 10.62 |
| 3 | 12.486(5) | 7.084(3) | Mg-Chamosite(0,0,2) | 39.39 |
| 4 | 13.89(2) | 6.370(9) | Albite(0,0,1) | 8.69 |
| 5 | 15.076(15) | 5.872(6) | Albite(1,1,-1),Orthoclase(1,1,-1) | 2.69 |
| 6 | 17.74(5) | 4.996(14) | Muscovite(0,0,4) | 2.31 |
| 7 | 18.760(7) | 4.7263(17) | Mg-Chamosite(0,0,3),Clinopyroxene(2,0,0) | 9.59 |
| 8 | 19.1583 | 4.62892 | Mg-Chamosite(0,2,0),Albite(0,2,-1),Orthoclase(0,2,1) | 5.68 |
| 9 | 19.7689 | 4.48729 | Mg-Chamosite(1,1,-1),Albite(0,2,1),Muscovite(1,1,0) | 13.58 |
| 10 | 20.8493 | 4.25715 | Quartz(1,0,0),Mg-Chamosite(1,-1,1),Muscovite(1,1,1) | 24.73 |
| 11 | 22.079 | 4.02273 | Albite(2,0,-1) | 14.86 |
| 12 | 22.4002 | 3.96578 | Muscovite(1,1,2),Orthoclase(1,1,1) | 3.77 |
| 13 | 22.910(16) | 3.879(3) | Mg-Chamosite(0,2,-2),Albite(1,-1,1),Muscovite(1,1,-3),Orthoclase(2,0,0) | 6.36 |
| 14 | 23.490(4) | 3.7842(6) | Albite(1,1,1),Muscovite(2,0,2),Orthoclase(1,3,0) | 24.63 |
| 15 | 24.290(6) | 3.6614(8) | Mg-Chamosite(1,1,2),Albite(1,3,0),Muscovite(2,0,-4) | 15.90 |
| 16 | 25.146(4) | 3.5386(6) | Mg-Chamosite(0,0,4),Muscovite(1,1,3),Orthoclase(2,2,-1) | 21.60 |
| 17 | 25.610(10) | 3.4756(14) | Mg-Chamosite(1,1,-3),Albite(1,1,-2),Muscovite(1,1,-4),Orthoclase(1,1,-2) | 24.12 |
| 18 | 26.6217 | 3.34572 | Quartz(1,0,1) | 100.00 |
| 19 | 26.86(4) | 3.317(5) | Mg-Chamosite(0,2,-3),Muscovite(0,0,6),Orthoclase(2,2,0) | 40.32 |
| 20 | 27.4975 | 3.2411 | Albite(0,4,0),Orthoclase(0,0,2) | 21.88 |
| 21 | 27.9 | 3.19526 | Albite(2,-2,0),Muscovite(1,1,4) | 47.28 |
| 22 | 29.7899 | 2.99671 | Albite(1,-3,1),Orthoclase(1,3,1) | 13.32 |
| 23 | 30.0969 | 2.96684 | Mg-Chamosite(1,1,-4),Clinopyroxene(3,1,0) | 8.89 |
| 24 | 30.4895 | 2.92952 | Albite(0,2,-2),Muscovite(2,0,-6),Orthoclase(2,2,-2) | 8.56 |
| 25 | 30.7679 | 2.90364 | Albite(2,2,-2),Orthoclase(0,4,1),Clinopyroxene(3,1,-1) | 10.61 |
| 26 | 31.2575 | 2.85928 | Albite(2,-2,-2),Muscovite(1,1,5) | 2.58 |
| 27 | 31.5284 | 2.83532 | Mg-Chamosite(0,0,5),Albite(0,2,2),Orthoclase(2,0,1) | 3.42 |
| 28 | 31.9315 | 2.80044 | Mg-Chamosite(0,2,4),Albite(1,3,-2),Muscovite(1,1,-6),Orthoclase(3,1,-1) | 4.98 |
| 29 | 32.3953 | 2.7614 | Orthoclase(1,3,-2) | 4.28 |
| 30 | 34.496(14) | 2.5979(11) | Mg-Chamosite(1,-3,1),Orthoclase(3,1,-2) | 11.93 |
| 31 | 35.048(14) | 2.5582(10) | Mg-Chamosite(1,3,-2),Albite(2,4,-1),Muscovite(0,2,0),Orthoclase(2,2,1),Clinopyroxene(1,3,-1) | 43.51 |
| 32 | 36.558(5) | 2.4560(4) | Quartz(1,1,0),Mg-Chamosite(1,-3,2),Albite(1,-5,0),Muscovite(2,0,6),Orthoclase(1,5,0) | 25.93 |
| 33 | 37.571(12) | 2.3921(7) | Mg-Chamosite(1,3,-3),Albite(3,-1,0),Muscovite(3,1,2),Orthoclase(2,0,-3) | 19.61 |
| 34 | 38.72(13) | 2.324(7) | Mg-Chamosite(0,4,0),Albite(1,1,-3),Muscovite(3,1,-5),Orthoclase(2,4,-2) | 1.60 |
| 35 | 39.41(3) | 2.2843(16) | Quartz(1,0,2),Mg-Chamosite(0,4,1),Albite(3,3,-1),Muscovite(1,1,-8) | 17.17 |
| 36 | 40.3059 | 2.2358 | Quartz(1,1,1),Mg-Chamosite(2,-2,1),Albite(2,2,-3),Muscovite(2,2,-1),Orthoclase(2,2,-3) | 3.77 |
| 37 | 41.67(3) | 2.1659(14) | Mg-Chamosite(2,2,-3),Albite(0,6,0),Muscovite(0,2,5),Orthoclase(0,6,0),Clinopyroxene(3,3,0) | 7.98 |
| 38 | 42.385(7) | 2.1308(3) | Quartz(2,0,0),Mg-Chamosite(2,-2,2),Albite(3,-3,0),Muscovite(3,1,4),Orthoclase(2,4,1),Clinopyroxene(4,2,-1) | 13.16 |
| 39 | 43.478(11) | 2.0797(5) | Mg-Chamosite(0,4,3),Albite(0,6,-1),Muscovite(3,1,-7),Orthoclase(1,3,-3) | 3.42 |
| 40 | 45.10(4) | 2.0089(17) | Mg-Chamosite(0,0,7),Albite(0,6,1),Muscovite(2,0,8),Orthoclase(4,2,-1),Clinopyroxene(2,0,2) | 23.69 |
| 41 | 45.744(16) | 1.9819(6) | Quartz(2,0,1),Mg-Chamosite(2,2,3),Albite(3,-1,1),Orthoclase(2,2,2) | 7.24 |
| 42 | 46.9704 | 1.93293 | Mg-Chamosite(0,4,4),Albite(2,-2,2),Muscovite(2,2,-6),Orthoclase(2,6,-1) | 1.54 |
| 43 | 48.06(9) | 1.892(3) | Mg-Chamosite(2,2,-5),Albite(2,2,2),Muscovite(4,0,4),Orthoclase(2,6,0) | 6.41 |
| 44 | 49.0835 | 1.85454 | Mg-Chamosite(0,2,-7),Albite(1,-5,2),Orthoclase(3,5,-2),Clinopyroxene(5,1,0) | 3.18 |
| 45 | 50.086(10) | 1.8197(3) | Quartz(1,1,2),Albite(0,4,-3) | 19.12 |
| 46 | 50.62(2) | 1.8019(8) | Quartz(0,0,3),Mg-Chamosite(0,4,-5),Albite(1,-7,0),Muscovite(0,2,8),Orthoclase(2,0,-4) | 13.32 |
| 47 | 51.11(2) | 1.7858(6) | Mg-Chamosite(1,-1,7),Orthoclase(1,7,-1) | 3.70 |
| 48 | 52.3886 | 1.74505 | Mg-Chamosite(2,-2,-6),Albite(0,4,3),Muscovite(2,2,-8),Orthoclase(3,1,-4) | 1.39 |
| 49 | 53.3097 | 1.71705 | Mg-Chamosite(1,-3,6),Albite(4,4,-2),Muscovite(3,1,-10),Orthoclase(2,6,1) | 1.63 |
| 50 | 54.874(16) | 1.6717(5) | Quartz(2,0,2),Mg-Chamosite(1,5,-3),Albite(3,5,-3),Muscovite(4,2,-3),Orthoclase(3,5,-3) | 17.22 |
| 51 | 58.73(3) | 1.5709(8) | Mg-Chamosite(3,1,-5),Albite(4,2,-4),Muscovite(4,2,3),Orthoclase(0,8,1),Clinopyroxene(3,5,0) | 9.40 |

## Phase Data Pattern

# XRD Results-G408260-LJN2021-042-DG-03/06/2021

## General Information

| ### Measurement date: | 17/5/2021 | ### Interpretative date: | 03/06/2021 |
| --- | --- | --- | --- |
| ### Job Number/Client: | LJN2021-042 DG | ### XRD | Rigaku Miniflex 600 |
| ### Registration Number: | G408260 | ### Analyst: | LUnwin |
| ### Quantitative Method: | PDXL Relative Heights | ### Process Medium: | Selective by Client |
| ### Sample Holder: | Low Reflectance | ### Speed (deg/min): | 0.5 |
| ### Comment: | Shifted -0.05 |  |  |

## Analysis Results

| ### Phase name | ### Content wt% (± error) | ### Formula |
| --- | --- | --- |
| Quartz | 49(10) | SiO2 |
| Muscovite | 34(8) | KAl2(AlSi3O10)(OH)2 |
| Mg-Chamosite | 8(3) | (Fe,Mg,Al)6(Si,Al)4O10(OH)8 |
| Pyrite | 2(2) | FeS2 |
| Albite | 2(2) | NaAlSi3O8 |
| Orthoclase | 4(2) | K(AlSi3O8) |

### Notes

Peak overlap may interfere with identifications and quantitative calculations.

Amorphous minerals and minerals present in trace amounts may not be detected.

## Peak List

| No. | 2-theta(deg) | d(ang.) | Phase name | Rel. int. I(a.u.) |
| --- | --- | --- | --- | --- |
| 1 | 6.22(2) | 14.19(6) | Mg-Chamosite(0,0,1) | 1.83 |
| 2 | 8.822(6) | 10.015(7) | Muscovite(0,0,2) | 22.02 |
| 3 | 12.473(8) | 7.091(4) | Mg-Chamosite(0,0,2) | 7.10 |
| 4 | 17.691(8) | 5.009(2) | Muscovite(0,0,4) | 9.86 |
| 5 | 18.828(2) | 4.7095(5) | Mg-Chamosite(0,0,3) | 1.25 |
| 6 | 19.819(13) | 4.476(3) | Muscovite(0,2,0),Mg-Chamosite(0,2,-1) | 11.01 |
| 7 | 20.8427 | 4.25848 | Quartz(1,0,0),Mg-Chamosite(1,1,1) | 11.94 |
| 8 | 21.6067 | 4.10959 | Muscovite(0,2,2),Mg-Chamosite(1,1,-2) | 1.17 |
| 9 | 22.0466 | 4.02857 | Albite(2,0,-1) | 0.63 |
| 10 | 22.856(7) | 3.8877(12) | Muscovite(1,1,-3),Mg-Chamosite(0,2,-2),Albite(1,-1,1) | 2.61 |
| 11 | 23.81(3) | 3.734(5) | Muscovite(0,2,3),Mg-Chamosite(1,-1,2),Orthoclase(1,3,0) | 2.17 |
| 12 | 25.125(5) | 3.5416(7) | Mg-Chamosite(0,0,4),Albite(1,1,-2),Orthoclase(2,2,-1) | 4.00 |
| 13 | 25.418(5) | 3.5014(7) | Muscovite(1,1,-4),Mg-Chamosite(1,1,-3),Albite(2,2,-1) | 3.80 |
| 14 | 26.606(4) | 3.3476(5) | Quartz(0,1,1),Muscovite(0,2,4),Albite(2,-2,-1) | 100.00 |
| 15 | 27.4253 | 3.24947 | Orthoclase(0,4,0) | 1.65 |
| 16 | 27.9181 | 3.19322 | Albite(2,2,0) | 2.33 |
| 17 | 28.4594 | 3.1337 | Mg-Chamosite(1,-1,3),Pyrite(1,-1,-1) | 1.99 |
| 18 | 29.8107 | 2.99467 | Muscovite(0,2,5),Orthoclase(1,3,1) | 3.75 |
| 19 | 31.15(2) | 2.8685(19) | Muscovite(1,1,5),Albite(1,3,1) | 5.38 |
| 20 | 31.94(2) | 2.7997(17) | Muscovite(1,1,-6),Mg-Chamosite(0,2,4),Albite(2,-2,-2),Orthoclase(2,0,1) | 4.81 |
| 21 | 32.961(17) | 2.7153(14) | Pyrite(0,0,2) | 1.41 |
| 22 | 34.891(10) | 2.5694(7) | Muscovite(1,1,6),Mg-Chamosite(1,3,-2),Albite(2,4,-1),Orthoclase(2,2,1) | 14.25 |
| 23 | 36.0555 | 2.48902 | Muscovite(1,3,2),Albite(3,-1,-2) | 1.73 |
| 24 | 36.494(11) | 2.4601(7) | Quartz(1,1,0),Muscovite(1,3,-3),Mg-Chamosite(1,-3,2),Albite(2,-4,-1) | 6.96 |
| 25 | 36.991(8) | 2.4282(5) | Mg-Chamosite(0,2,-5),Pyrite(1,0,-2) | 0.86 |
| 26 | 37.61(5) | 2.390(3) | Muscovite(2,0,-4),Mg-Chamosite(0,2,5),Albite(1,-5,0),Orthoclase(1,5,-1) | 3.67 |
| 27 | 39.414(10) | 2.2843(6) | Quartz(1,0,2),Mg-Chamosite(1,-3,3),Albite(1,-1,-3),Orthoclase(0,4,2) | 4.93 |
| 28 | 40.253(7) | 2.2386(4) | Quartz(1,1,1),Muscovite(0,4,1),Albite(1,-3,2) | 3.13 |
| 29 | 40.74(4) | 2.213(2) | Muscovite(2,2,-2),Mg-Chamosite(0,4,-2),Pyrite(1,1,-2),Albite(2,-4,-2),Orthoclase(2,2,-3) | 4.78 |
| 30 | 41.902(8) | 2.1542(4) | Muscovite(2,2,2),Orthoclase(0,6,0) | 1.55 |
| 31 | 42.382(8) | 2.1310(4) | Quartz(2,0,0),Muscovite(0,4,3),Mg-Chamosite(2,2,2),Albite(0,6,0) | 6.96 |
| 32 | 44.0203 | 2.05538 | Muscovite(0,4,4),Orthoclase(3,1,1) | 0.79 |
| 33 | 45.222(7) | 2.0035(3) | Muscovite(1,3,6),Mg-Chamosite(1,1,6),Albite(1,-5,-2),Orthoclase(4,2,-1) | 10.48 |
| 34 | 45.739(10) | 1.9820(4) | Quartz(2,0,1),Albite(3,-1,1) | 2.67 |
| 35 | 47.3797 | 1.91718 | Pyrite(0,2,-2),Orthoclase(2,6,-1) | 0.94 |
| 36 | 50.085(7) | 1.8198(2) | Quartz(1,1,2),Albite(3,-3,1),Orthoclase(3,5,0) | 8.74 |
| 37 | 52.9063 | 1.72919 | Muscovite(1,3,-9),Mg-Chamosite(1,5,-2),Albite(2,-4,2),Orthoclase(2,2,-4) | 0.65 |
| 38 | 54.812(9) | 1.6735(3) | Quartz(0,2,2),Muscovite(2,4,-3),Mg-Chamosite(1,5,-3),Albite(4,-4,-2) | 1.88 |
| 39 | 55.36(8) | 1.658(2) | Quartz(0,1,3),Muscovite(3,1,-3),Mg-Chamosite(2,0,6),Albite(1,7,-2),Orthoclase(3,1,2) | 5.81 |
| 40 | 56.172(12) | 1.6362(3) | Pyrite(1,1,3) | 1.63 |
| 41 | 59.895(11) | 1.5430(3) | Quartz(1,2,1),Mg-Chamosite(1,1,-9),Albite(3,7,-1) | 4.45 |

## Phase Data Pattern

# XRD Results-G408261-LJN2021-042-DG-03/06/2021

## General Information

| ### Measurement date: | 17/5/2021 | ### Interpretative date: | 03/06/2021 |
| --- | --- | --- | --- |
| ### Job Number/Client: | LJN2021-042 DG | ### XRD | Rigaku Miniflex 600 |
| ### Registration Number: | G408261 | ### Analyst: | LUnwin |
| ### Quantitative Method: | PDXL Relative Heights | ### Process Medium: | Selective by Client |
| ### Sample Holder: | Low Reflectance | ### Speed (deg/min): | 0.5 |
| ### Comment: | Shifted -0.07 |  |  |

## Analysis Results

| ### Phase name | ### Content wt% (± error) | ### Formula |
| --- | --- | --- |
| Quartz | 44(10) | SiO2 |
| Albite | 2(2) | NaAlSi3O8 |
| Pyrite | 4(2) | FeS2 |
| Kaolinite | 33(8) | Al2(Si2O5)(OH)4 |
| Muscovite | 13(4) | KAl2(AlSi3O10)(OH)2 |
| Orthoclase | 3(2) | K(AlSi3O8) |

### Notes

Peak overlap may interfere with identifications and quantitative calculations.

Amorphous minerals and minerals present in trace amounts may not be detected.

## Peak List

| No. | 2-theta(deg) | d(ang.) | Phase name | Rel. int. I(a.u.) |
| --- | --- | --- | --- | --- |
| 1 | 8.810(8) | 10.029(9) | Muscovite(0,0,3) | 14.60 |
| 2 | 12.4726 | 7.09109 | Kaolinite(0,0,1) | 13.04 |
| 3 | 17.75(2) | 4.993(6) | Muscovite(0,0,6) | 5.96 |
| 4 | 19.0764 | 4.6486 | Orthoclase(0,2,1) | 0.82 |
| 5 | 19.828(11) | 4.474(2) | Kaolinite(0,2,0),Muscovite(1,0,0) | 9.44 |
| 6 | 20.834(5) | 4.2602(11) | Quartz(1,0,0),Orthoclase(2,0,-1) | 17.68 |
| 7 | 21.6468 | 4.10206 | Kaolinite(1,-1,-1),Muscovite(1,0,3) | 0.99 |
| 8 | 22.0616 | 4.02588 | Albite(2,0,-1) | 0.61 |
| 9 | 22.891 | 3.88185 | Kaolinite(0,2,-1),Muscovite(1,0,4),Albite(1,-1,1),Orthoclase(2,0,0) | 2.85 |
| 10 | 23.788(18) | 3.737(3) | Kaolinite(0,2,1),Albite(1,3,0),Orthoclase(1,3,0) | 4.99 |
| 11 | 24.789(10) | 3.5887(15) | Muscovite(1,0,5) | 0.60 |
| 12 | 25.080(8) | 3.5477(11) | Kaolinite(0,0,2),Albite(1,1,-2),Orthoclase(2,2,-1) | 6.98 |
| 13 | 25.428(12) | 3.5000(16) | Albite(1,-3,-1),Orthoclase(1,1,-2) | 4.28 |
| 14 | 26.612(4) | 3.3469(4) | Quartz(0,1,1),Muscovite(1,0,6) | 100.00 |
| 15 | 27.4236 | 3.24967 | Albite(2,0,-2),Orthoclase(0,4,0) | 1.49 |
| 16 | 27.79(3) | 3.207(3) | Albite(2,2,0) | 2.83 |
| 17 | 28.51(2) | 3.128(2) | Pyrite(1,-1,-1),Kaolinite(1,1,-2) | 1.19 |
| 18 | 29.772(10) | 2.9984(10) | Albite(1,-3,1),Orthoclase(1,3,1) | 4.56 |
| 19 | 31.19(4) | 2.865(4) | Muscovite(1,0,8),Albite(1,3,-2) | 3.49 |
| 20 | 32.03(3) | 2.792(2) | Orthoclase(3,1,-1) | 3.55 |
| 21 | 33.01(2) | 2.712(2) | Pyrite(0,0,2),Albite(3,1,-1) | 2.83 |
| 22 | 34.91(3) | 2.5682(19) | Kaolinite(1,-3,0),Muscovite(1,1,0),Albite(2,4,-1),Orthoclase(2,2,1) | 12.82 |
| 23 | 35.9813 | 2.49398 | Kaolinite(1,-3,-1),Muscovite(0,0,12),Albite(2,2,1),Orthoclase(2,4,0) | 1.47 |
| 24 | 36.522(16) | 2.4583(10) | Quartz(1,1,0),Muscovite(1,1,4) | 9.84 |
| 25 | 37.034(6) | 2.4255(4) | Pyrite(1,0,-2),Albite(2,-4,0),Orthoclase(1,5,-1) | 2.55 |
| 26 | 37.652(18) | 2.3871(11) | Kaolinite(0,0,3),Muscovite(1,1,5),Albite(2,4,-2),Orthoclase(2,0,-3) | 2.65 |
| 27 | 39.434(10) | 2.2832(5) | Quartz(1,0,2),Kaolinite(1,3,1),Albite(3,-3,-1),Orthoclase(3,3,-2) | 4.96 |
| 28 | 40.268(7) | 2.2378(4) | Quartz(1,1,1),Kaolinite(1,3,-2),Muscovite(2,0,1),Orthoclase(1,3,2) | 3.50 |
| 29 | 40.730(6) | 2.2135(3) | Pyrite(1,1,-2),Kaolinite(2,-2,-1),Muscovite(1,1,-7),Orthoclase(3,3,0) | 2.31 |
| 30 | 42.433(15) | 2.1285(7) | Quartz(2,0,0),Kaolinite(0,2,-3),Muscovite(1,1,-8),Albite(3,-3,0),Orthoclase(4,0,-1) | 8.50 |
| 31 | 43.5669 | 2.07571 | Kaolinite(2,2,-2),Orthoclase(3,1,1) | 0.52 |
| 32 | 44.1087 | 2.05147 | Kaolinite(2,-2,-2),Muscovite(2,0,6),Albite(4,0,-2) | 0.83 |
| 33 | 45.27(3) | 2.0016(14) | Kaolinite(1,-3,2),Muscovite(0,0,15),Albite(0,6,1) | 6.82 |
| 34 | 45.761(12) | 1.9812(5) | Quartz(2,0,1),Kaolinite(2,0,-3),Albite(4,2,-2),Orthoclase(2,2,2) | 3.05 |
| 35 | 47.37(2) | 1.9177(9) | Pyrite(0,2,-2),Kaolinite(0,4,-2),Albite(3,5,-1) | 1.23 |
| 36 | 50.089(6) | 1.8196(2) | Quartz(1,1,2),Muscovite(1,0,15),Albite(3,3,1),Orthoclase(2,6,-2) | 10.80 |
| 37 | 54.830(15) | 1.6730(4) | Quartz(0,2,2),Kaolinite(1,5,0),Muscovite(2,1,3),Albite(4,4,-3) | 3.25 |
| 38 | 55.28(2) | 1.6604(6) | Quartz(0,1,3),Kaolinite(1,-3,3),Muscovite(0,0,18),Albite(1,7,1),Orthoclase(4,4,0) | 1.51 |
| 39 | 56.217(7) | 1.63496(19) | Pyrite(1,1,3),Kaolinite(3,-1,0),Muscovite(2,1,-5),Albite(3,-1,2),Orthoclase(5,1,-3) | 3.33 |

## Phase Data Pattern

# XRD Results-G408262-LJN2021-042-DG-03/06/2021

## General Information

| ### Measurement date: | 03/06/2021 | ### Interpretative date: | 03/06/2021 |
| --- | --- | --- | --- |
| ### Job Number/Client: | LJN2021-042 DG | ### XRD | Rigaku Miniflex 600 |
| ### Registration Number: | G408262 | ### Analyst: | LUnwin |
| ### Quantitative Method: | PDXL Relative Heights | ### Process Medium: | Selective by Client |
| ### Sample Holder: | Low Reflectance | ### Speed (deg/min): | 0.5 |
| ### Comment: | Shifted -0.09 |  |  |

## Analysis Results

| ### Phase name | ### Content wt% (± error) | ### Formula |
| --- | --- | --- |
| Quartz | 53(10) | SiO2 |
| Muscovite | 36(10) | KAl2(AlSi3O10)(OH)2 |
| Mg-Chamosite | 4(2) | (Fe,Mg,Al)6(Si,Al)4O10(OH)8 |
| Albite | 3(2) | NaAlSi3O8 |
| Orthoclase | 4(2) | K(AlSi3O8) |

### Notes

Peak overlap may interfere with identifications and quantitative calculations.

Amorphous minerals and minerals present in trace amounts may not be detected.

## Peak List

| No. | 2-theta(deg) | d(ang.) | Phase name | Rel. int. I(a.u.) |
| --- | --- | --- | --- | --- |
| 1 | 6.209(11) | 14.22(3) | Mg-Chamosite(0,0,1) | 1.23 |
| 2 | 8.822(4) | 10.016(4) | Muscovite(0,0,2) | 20.80 |
| 3 | 12.482(10) | 7.086(5) | Mg-Chamosite(0,0,2) | 3.90 |
| 4 | 17.719(11) | 5.002(3) | Muscovite(0,0,4) | 9.09 |
| 5 | 18.7222 | 4.73574 | Mg-Chamosite(0,0,3) | 0.62 |
| 6 | 19.789(15) | 4.483(3) | Muscovite(0,2,0),Mg-Chamosite(0,2,-1),Albite(0,2,1) | 11.62 |
| 7 | 20.832(5) | 4.2606(11) | Quartz(1,0,0),Mg-Chamosite(1,-1,1) | 16.50 |
| 8 | 21.5478 | 4.1207 | Muscovite(0,2,2),Mg-Chamosite(1,1,-2) | 0.91 |
| 9 | 22.0486 | 4.02822 | Albite(2,0,-1) | 0.56 |
| 10 | 22.857(5) | 3.8876(8) | Muscovite(1,1,-3),Mg-Chamosite(0,2,-2) | 2.50 |
| 11 | 23.77(2) | 3.740(3) | Muscovite(0,2,3),Albite(1,1,1),Orthoclase(1,3,0) | 2.34 |
| 12 | 24.319 | 3.65705 | Albite(1,3,0) | 1.33 |
| 13 | 25.427(8) | 3.5001(11) | Muscovite(1,1,-4),Mg-Chamosite(1,1,-3),Orthoclase(2,2,-1) | 6.74 |
| 14 | 26.605(5) | 3.3477(6) | Quartz(0,1,1),Muscovite(0,2,4) | 100.00 |
| 15 | 27.43 | 3.24893 | Muscovite(1,1,4),Albite(0,4,0),Orthoclase(0,0,2) | 1.66 |
| 16 | 27.8794 | 3.19757 | Albite(2,0,-2) | 4.22 |
| 17 | 28.5303 | 3.12608 | Muscovite(1,1,-5),Mg-Chamosite(1,-1,3),Albite(2,2,0) | 1.31 |
| 18 | 29.869(10) | 2.9889(10) | Muscovite(0,2,5),Mg-Chamosite(1,1,-4),Albite(1,-3,1),Orthoclase(1,3,1) | 6.27 |
| 19 | 31.176(18) | 2.8665(16) | Muscovite(1,1,5),Albite(1,3,1) | 6.60 |
| 20 | 31.972(11) | 2.7970(9) | Muscovite(1,1,-6),Mg-Chamosite(0,2,4),Albite(0,2,2),Orthoclase(2,0,1) | 3.83 |
| 21 | 33.339 | 2.68536 | Muscovite(0,2,6),Mg-Chamosite(1,-3,0),Albite(1,-3,-2) | 0.67 |
| 22 | 34.556(14) | 2.5935(10) | Muscovite(1,3,0),Mg-Chamosite(1,-3,1),Orthoclase(3,1,-2) | 6.32 |
| 23 | 34.926(17) | 2.5669(12) | Muscovite(2,0,-2),Mg-Chamosite(1,3,-2),Orthoclase(2,4,-1) | 9.76 |
| 24 | 35.84(3) | 2.5035(19) | Muscovite(0,0,8),Albite(2,4,-1),Orthoclase(3,1,0) | 2.10 |
| 25 | 36.482(8) | 2.4609(6) | Quartz(1,1,0),Muscovite(1,3,-3),Mg-Chamosite(1,-3,2),Albite(1,1,2) | 8.80 |
| 26 | 37.65(4) | 2.387(2) | Muscovite(2,0,-4),Mg-Chamosite(0,2,5),Albite(1,5,0),Orthoclase(1,5,-1) | 5.11 |
| 27 | 39.21(2) | 2.2959(12) | Mg-Chamosite(0,4,1),Albite(3,-3,-1) | 0.12 |
| 28 | 39.421(8) | 2.2839(4) | Quartz(1,0,2),Mg-Chamosite(1,-3,3),Albite(1,-1,-3),Orthoclase(0,4,2) | 4.57 |
| 29 | 39.94(3) | 2.2555(14) | Muscovite(0,4,0),Mg-Chamosite(2,-2,1),Albite(2,-4,-2),Orthoclase(3,3,-2) | 0.83 |
| 30 | 40.248(19) | 2.2389(10) | Quartz(1,1,1),Muscovite(0,4,1),Mg-Chamosite(2,2,1),Albite(2,2,-3) | 2.87 |
| 31 | 41.0006 | 2.19951 | Muscovite(0,4,2),Mg-Chamosite(2,0,3),Albite(3,3,-2),Orthoclase(1,5,1) | 0.87 |
| 32 | 41.97(3) | 2.1512(14) | Muscovite(2,2,2),Albite(0,6,0),Orthoclase(0,6,0) | 1.30 |
| 33 | 42.381(16) | 2.1310(8) | Quartz(2,0,0),Muscovite(0,4,3),Mg-Chamosite(2,-2,2),Albite(3,-3,0) | 7.27 |
| 34 | 45.302(17) | 2.0002(7) | Muscovite(1,3,6),Mg-Chamosite(2,0,4),Albite(4,0,-2),Orthoclase(4,2,-2) | 9.41 |
| 35 | 45.743(6) | 1.9819(2) | Quartz(2,0,1) | 3.02 |
| 36 | 45.98(2) | 1.9722(8) | Muscovite(1,3,-7),Albite(3,-1,1),Orthoclase(2,2,2) | 1.54 |
| 37 | 46.48(3) | 1.9520(10) | Muscovite(1,1,9),Mg-Chamosite(0,4,-4),Albite(3,1,1),Orthoclase(3,3,-3) | 1.20 |
| 38 | 50.090(6) | 1.81962(19) | Quartz(1,1,2),Albite(0,6,-2),Orthoclase(3,5,0) | 9.14 |
| 39 | 52.7375 | 1.73433 | Muscovite(1,1,-11),Mg-Chamosite(1,-5,1),Albite(4,2,0) | 0.72 |
| 40 | 54.834(5) | 1.67288(15) | Quartz(0,2,2),Muscovite(2,4,-3),Mg-Chamosite(1,5,-3) | 2.83 |
| 41 | 55.46(7) | 1.655(2) | Quartz(0,1,3),Muscovite(1,5,-3),Mg-Chamosite(2,0,6),Albite(3,5,-3),Orthoclase(3,1,2) | 10.16 |

## Phase Data Pattern

# XRD Results-G408264-LJN2021-042-DG-4/6/2021

## General Information

| ### Measurement date: | 3/6/2021 | ### Interpretative date: | 4/6/2021 |
| --- | --- | --- | --- |
| ### Job Number/Client: | LJN2021-042 DG | ### XRD | Rigaku Miniflex 600 |
| ### Registration Number: | G408264 | ### Analyst: | LUnwin |
| ### Quantitative Method: | PDXL Relative Heights | ### Process Medium: | Selective by Client |
| ### Sample Holder: | Low Reflectance | ### Speed (deg/min): | 0.5 |
| ### Comment: | Shifted -0.05 |  |  |

## Analysis Results

| ### Phase name | ### Content wt% (± error) | ### Formula |
| --- | --- | --- |
| Quartz | 31(8) | SiO2 |
| Biotite | 34(8) | K(Mg,Fe)3[AlSi3O10](OH)2 |
| Mg-Chamosite | 30(8) | (Fe,Mg,Al)6(Si,Al)4O10(OH)8 |
| Orthoclase | 5(2) | K(AlSi3O8) |

### Notes

Peak overlap may interfere with identifications and quantitative calculations.

Amorphous minerals and minerals present in trace amounts may not be detected.

## Peak List

| No. | 2-theta(deg) | d(ang.) | Phase name | Rel. int. I(a.u.) |
| --- | --- | --- | --- | --- |
| 1 | 6.253(14) | 14.12(3) | Mg-Chamosite(0,0,1) | 5.55 |
| 2 | 8.763(2) | 10.082(3) | Biotite(0,0,1) | 100.00 |
| 3 | 12.501(5) | 7.075(3) | Mg-Chamosite(0,0,2) | 19.03 |
| 4 | 17.5972 | 5.03588 | Biotite(0,0,2) | 1.36 |
| 5 | 18.765(11) | 4.725(3) | Mg-Chamosite(0,0,3) | 7.03 |
| 6 | 19.1506 | 4.63076 | Biotite(0,2,0),Mg-Chamosite(0,2,0) | 1.55 |
| 7 | 20.18 | 4.39679 | Mg-Chamosite(0,2,-1) | 0.64 |
| 8 | 20.846(3) | 4.2578(6) | Quartz(1,0,0),Mg-Chamosite(1,-1,1) | 7.11 |
| 9 | 22.573(9) | 3.9357(16) | Biotite(1,1,1),Orthoclase(1,1,1) | 1.01 |
| 10 | 23.49(4) | 3.784(6) | Orthoclase(1,3,0) | 1.73 |
| 11 | 24.163(4) | 3.6803(7) | Biotite(1,1,-2),Mg-Chamosite(1,-1,2),Orthoclase | 4.14 |
| 12 | 25.159(7) | 3.5368(10) | Mg-Chamosite(0,0,4),Orthoclase(2,2,-1) | 12.60 |
| 13 | 26.109(9) | 3.4102(11) | Biotite(0,2,2) | 7.77 |
| 14 | 26.476(4) | 3.3638(5) | Biotite(0,0,3) | 47.46 |
| 15 | 26.632(3) | 3.3444(4) | Quartz(1,0,1) | 49.73 |
| 16 | 27.5845 | 3.23109 | Orthoclase(0,4,0) | 1.71 |
| 17 | 28.244(6) | 3.1571(6) | Biotite(1,1,2) | 6.43 |
| 18 | 30.402(9) | 2.9378(9) | Biotite(1,1,-3),Mg-Chamosite(1,-1,-4),Orthoclase | 6.93 |
| 19 | 31.55(4) | 2.834(4) | Mg-Chamosite(0,0,5) | 1.45 |
| 20 | 32.91(6) | 2.719(5) | Biotite(0,2,3),Orthoclase(3,-1,-1) | 3.41 |
| 21 | 34.042(16) | 2.6315(12) | Biotite(1,3,-1) | 16.81 |
| 22 | 34.40(2) | 2.6051(17) | Mg-Chamosite(1,-3,1) | 1.27 |
| 23 | 35.026 | 2.55978 | Mg-Chamosite(1,3,-2),Orthoclase(3,-1,-2) | 1.17 |
| 24 | 35.57(2) | 2.5219(17) | Biotite(1,1,3),Orthoclase(2,-2,1) | 9.53 |
| 25 | 36.681(18) | 2.4480(11) | Biotite(1,3,-2),Quartz(1,1,0),Mg-Chamosite(1,-3,2),Orthoclase(1,5,0) | 16.31 |
| 26 | 38.8188 | 2.31796 | Biotite(0,4,0),Mg-Chamosite(0,4,0),Orthoclase(2,4,-2) | 1.11 |
| 27 | 39.463(10) | 2.2816(6) | Biotite(2,2,0),Quartz, Mg-Chamosite, Orthoclase | 6.39 |
| 28 | 40.3359 | 2.23421 | Quartz(1,1,1),Mg-Chamosite(2,2,1),Orthoclase(1,3,2) | 1.29 |
| 29 | 41.31(2) | 2.1840(10) | Biotite(1,3,-3),Orthoclase(1,-3,2) | 13.99 |
| 30 | 42.418(13) | 2.1293(6) | Quartz(2,0,0),Mg-Chamosite(2,-2,2),Orthoclase | 2.66 |
| 31 | 44.852(9) | 2.0192(4) | Mg-Chamosite(0,0,7) | 3.76 |
| 32 | 45.16(2) | 2.0059(9) | Biotite(0,0,5),Mg-Chamosite(1,-1,6),Orthoclase | 13.06 |
| 33 | 45.767(7) | 1.9809(3) | Quartz(2,0,1) | 1.25 |
| 34 | 47.327(17) | 1.9192(7) | Biotite(1,3,-4),Mg-Chamosite(1,-1,-7),Orthoclase | 4.30 |
| 35 | 50.095(4) | 1.81943(15) | Quartz(1,1,2) | 5.02 |
| 36 | 54.601(16) | 1.6795(5) | Biotite(1,5,-2),Quartz(2,0,2),Mg-Chamosite(2,-4,-3),Orthoclase(5,1,-2) | 25.93 |
| 37 | 58.76(5) | 1.5701(11) | Mg-Chamosite(3,-1,3),Orthoclase(4,-2,-4) | 1.15 |

## Phase Data Pattern

# XRD Results-G408265-LJN2021-042-DG-4/6/2021

## General Information

| ### Measurement date: | 3/6/2021 | ### Interpretative date: | 4/6/2021 |
| --- | --- | --- | --- |
| ### Job Number/Client: | LJN2021-042 DG | ### XRD | Rigaku Miniflex 600 |
| ### Registration Number: | G408265 | ### Analyst: | LUnwin |
| ### Quantitative Method: | PDXL Relative Heights | ### Process Medium: | Selective by Client |
| ### Sample Holder: | Low reflectance | ### Speed (deg/min): | 0.5 |
| ### Comment: | Shifted -0.09 |  |  |

## Analysis Results

| ### Phase name | ### Content wt% (± error) | ### Formula |
| --- | --- | --- |
| Quartz | 21(5) | SiO2 |
| Spessartine | 17(5) | Mn2+3Al2(SiO4)3 |
| Phlogopite | 54(10) | KMg3AlSi3O10F(OH) |
| Mg-Chamosite | 8(3) | (Fe,Mg,Al)6(Si,Al)4O10(OH)8 |

### Notes

Peak overlap may interfere with identifications and quantitative calculations.

Amorphous minerals and minerals present in trace amounts may not be detected.

## Peak List

| No. | 2-theta(deg) | d(ang.) | Phase name | Rel. int. I(a.u.) |
| --- | --- | --- | --- | --- |
| 1 | 6.289(4) | 14.043(8) | Mg-Chamosite(0,0,1) | 3.93 |
| 2 | 8.745(3) | 10.103(3) | Phlogopite(0,0,1) | 94.89 |
| 3 | 12.503(6) | 7.074(4) | Mg-Chamosite(0,0,2) | 14.34 |
| 4 | 17.5393 | 5.05238 | Phlogopite(0,0,2) | 1.15 |
| 5 | 18.808(10) | 4.714(2) | Mg-Chamosite(0,0,3) | 5.71 |
| 6 | 19.3815 | 4.57611 | Phlogopite(1,1,0),Mg-Chamosite(1,1,-1) | 1.89 |
| 7 | 20.834(7) | 4.2602(13) | Quartz(1,0,0),Mg-Chamosite(1,-1,1) | 15.27 |
| 8 | 21.6571 | 4.10013 | Spessartine(2,2,0),Mg-Chamosite(1,1,-2) | 0.93 |
| 9 | 22.5783 | 3.9349 | Phlogopite(1,1,1) | 1.82 |
| 10 | 24.14(3) | 3.684(4) | Phlogopite(1,1,-2),Mg-Chamosite(1,-1,2) | 3.03 |
| 11 | 25.147(11) | 3.5385(15) | Mg-Chamosite(0,0,4) | 9.32 |
| 12 | 26.100(9) | 3.4114(12) | Phlogopite(0,2,2) | 6.53 |
| 13 | 26.459(4) | 3.3659(5) | Phlogopite(0,0,3) | 36.64 |
| 14 | 26.623(3) | 3.3455(4) | Quartz(0,1,1),Mg-Chamosite(0,2,-3) | 100.00 |
| 15 | 28.282(6) | 3.1530(7) | Phlogopite(1,1,2),Mg-Chamosite(1,-1,3) | 6.48 |
| 16 | 30.046(11) | 2.9718(11) | Mg-Chamosite(1,-1,-4) | 2.59 |
| 17 | 30.413(19) | 2.9367(17) | Phlogopite(1,1,-3) | 4.35 |
| 18 | 30.690(14) | 2.9108(13) | Spessartine(4,0,0) | 10.07 |
| 19 | 31.6267 | 2.82673 | Mg-Chamosite(0,0,5) | 2.26 |
| 20 | 32.8729 | 2.72236 | Phlogopite(0,2,3) | 2.52 |
| 21 | 34.000(7) | 2.6347(6) | Phlogopite(1,3,-1) | 18.36 |
| 22 | 34.431(5) | 2.6026(4) | Spessartine(4,2,0),Mg-Chamosite(2,0,-2) | 20.93 |
| 23 | 35.460(5) | 2.5294(3) | Phlogopite(1,1,3),Mg-Chamosite(1,-1,-5) | 18.87 |
| 24 | 36.59(2) | 2.4538(13) | Quartz(1,1,0),Phlogopite(1,3,-2),Mg-Chamosite(1,-3,2) | 19.63 |
| 25 | 37.841(6) | 2.3756(4) | Spessartine(4,2,2),Phlogopite(1,1,-4) | 3.26 |
| 26 | 39.0497 | 2.30479 | Mg-Chamosite(1,1,5) | 1.18 |
| 27 | 39.438(11) | 2.2830(6) | Quartz(1,0,2),Spessartine(4,3,1),Phlogopite, Mg-Chamosite(1,-3,3) | 12.93 |
| 28 | 40.241(13) | 2.2392(7) | Quartz(1,1,1) | 2.86 |
| 29 | 41.274(6) | 2.1856(3) | Phlogopite(1,3,-3),Mg-Chamosite(2,2,-3) | 13.51 |
| 30 | 42.443(8) | 2.1280(4) | Quartz(2,0,0),Spessartine(5,2,1),Mg-Chamosite(2,2,2) | 8.01 |
| 31 | 42.993(12) | 2.1021(6) | Mg-Chamosite(0,2,6) | 1.44 |
| 32 | 44.0887 | 2.05235 | Phlogopite(2,2,-3),Mg-Chamosite(2,2,-4) | 1.26 |
| 33 | 44.903(9) | 2.0170(4) | Phlogopite(0,0,5),Mg-Chamosite(0,0,7) | 14.93 |
| 34 | 45.733(7) | 1.9823(3) | Quartz(2,0,1),Phlogopite(2,2,2) | 2.99 |
| 35 | 47.31(6) | 1.920(2) | Phlogopite(1,3,-4) | 3.30 |
| 36 | 48.162(6) | 1.8879(2) | Spessartine(6,1,1),Mg-Chamosite(1,3,5) | 5.09 |
| 37 | 50.087(9) | 1.8197(3) | Quartz(1,1,2) | 10.48 |
| 38 | 53.28(2) | 1.7179(6) | Spessartine(6,3,1),Mg-Chamosite(2,0,-7) | 1.28 |
| 39 | 54.59(3) | 1.6798(8) | Quartz(0,2,2),Spessartine(4,4,4),Phlogopite(0,0,6), Mg-Chamosite(1,5,2) | 29.65 |
| 40 | 57.049(17) | 1.6131(4) | Quartz(2,1,0),Spessartine(6,4,0),Mg-Chamosite(2,2,-7) | 15.52 |
| 41 | 59.44(3) | 1.5539(7) | Spessartine(6,4,2),Phlogopite(3,1,-4),Mg-Chamosite(1,-5,4) | 21.83 |

## Phase Data Pattern

# XRD Results-G408266-LJN2021-042-DG-4/6/2021

## General Information

| ### Measurement date: | 3/6/2021 | ### Interpretative date: | 4/6/2021 |
| --- | --- | --- | --- |
| ### Job Number/Client: | LJN2021-042 DG | ### XRD | Rigaku Miniflex 600 |
| ### Registration Number: | G408266 | ### Analyst: | LUnwin |
| ### Quantitative Method: | PDXL Relative Heights | ### Process Medium: | Selective by Client |
| ### Sample Holder: | Low Reflectance | ### Speed (deg/min): | 0.5 |
| ### Comment: | Shifted -0.03 |  |  |

## Analysis Results

| ### Phase name | ### Content wt% (± error) | ### Formula |
| --- | --- | --- |
| Quartz | 9(3) | SiO2 |
| Magnesio-ferri-hornblende | 46(10) |  |
| Mg-Chamosite | 37(10) | (Fe,Mg,Al)6(Si,Al)4O10(OH)8 |
| Orthoclase | 6(3) | K(AlSi3O8) |
| Biotite | 1(1) | K(Mg,Fe)3[AlSi3O10](OH)2 |

### Notes

Peak overlap may interfere with identifications and quantitative calculations.

Amorphous minerals and minerals present in trace amounts may not be detected.

## Peak List

| No. | 2-theta(deg) | d(ang.) | Phase name | Rel. int. I(a.u.) |
| --- | --- | --- | --- | --- |
| 1 | 6.243(9) | 14.15(2) | Mg-Chamosite(0,0,1) | 28.15 |
| 2 | 8.753(13) | 10.094(15) | Biotite(0,0,1) | 3.31 |
| 3 | 9.794(5) | 9.023(5) | Magnesio-ferri-hornblende(0,2,0) | 6.97 |
| 4 | 10.481(3) | 8.434(2) | Magnesio-ferri-hornblende(1,1,0) | 99.78 |
| 5 | 12.501(5) | 7.075(3) | Mg-Chamosite(0,0,2) | 97.68 |
| 6 | 17.3825 | 5.09758 | Magnesio-ferri-hornblende(0,0,1) | 4.11 |
| 7 | 18.084(6) | 4.9014(16) | Magnesio-ferri-hornblende(1,1,-1) | 5.75 |
| 8 | 18.79(2) | 4.719(5) | Mg-Chamosite(0,0,3) | 36.58 |
| 9 | 19.55(3) | 4.536(6) | Magnesio-ferri-hornblende(0,4,0),Mg-Chamosite(1,1,-1),Orthoclase(0,2,1),Biotite(1,1,0) | 25.05 |
| 10 | 20.828(7) | 4.2614(14) | Mg-Chamosite(1,-1,1),Quartz(1,0,0) | 8.08 |
| 11 | 20.99(3) | 4.228(6) | Magnesio-ferri-hornblende(2,2,0),Orthoclase(2,0,-1) | 6.05 |
| 12 | 21.9339 | 4.04902 | Magnesio-ferri-hornblende(2,0,-1),Mg-Chamosite | 4.17 |
| 13 | 22.855 | 3.88788 | Magnesio-ferri-hornblende(1,3,-1),Mg-Chamosite | 6.09 |
| 14 | 23.6135 | 3.76468 | Orthoclase(1,3,0) | 6.99 |
| 15 | 24.5888 | 3.61752 | Orthoclase(1,3,-1) | 5.84 |
| 16 | 25.150(10) | 3.5380(14) | Mg-Chamosite(0,0,4),Orthoclase(2,2,-1) | 58.87 |
| 17 | 26.205(18) | 3.398(2) | Magnesio-ferri-hornblende(0,4,1) | 10.44 |
| 18 | 26.626(9) | 3.3451(11) | Quartz(1,0,1),Biotite(0,0,3) | 37.59 |
| 19 | 27.095(7) | 3.2883(9) | Magnesio-ferri-hornblende(2,4,0),Orthoclase(2,0,-2) | 13.97 |
| 20 | 27.538(16) | 3.2364(18) | Orthoclase(0,4,0) | 9.62 |
| 21 | 28.484(10) | 3.1311(11) | Magnesio-ferri-hornblende(3,1,0),Mg-Chamosite(1,-1,3),Biotite(1,1,2) | 100.00 |
| 22 | 29.418(6) | 3.0338(6) | Magnesio-ferri-hornblende(3,1,-1) | 24.30 |
| 23 | 30.26(4) | 2.951(4) | Magnesio-ferri-hornblende(1,5,-1),Mg-Chamosite | 14.03 |
| 24 | 30.7656 | 2.90385 | Orthoclase(0,4,1),Biotite(1,1,-3) | 3.83 |
| 25 | 31.77(3) | 2.814(2) | Magnesio-ferri-hornblende(3,3,0),Mg-Chamosite(0,0,5),Orthoclase(2,0,1) | 18.58 |
| 26 | 32.605(19) | 2.7441(16) | Magnesio-ferri-hornblende(3,3,-1),Orthoclase(1,3,-2) | 11.75 |
| 27 | 32.932(10) | 2.7176(8) | Magnesio-ferri-hornblende(1,5,1) | 31.54 |
| 28 | 34.420(9) | 2.6035(7) | Mg-Chamosite(1,-3,1),Biotite(2,0,0) | 23.78 |
| 29 | 34.59(3) | 2.591(3) | Magnesio-ferri-hornblende(0,6,1),Mg-Chamosite(1,3,1),Orthoclase(3,1,-2) | 12.62 |
| 30 | 35.16(2) | 2.5501(14) | Magnesio-ferri-hornblende(0,0,2),Mg-Chamosite(1,3,-2),Orthoclase(2,4,-1) | 31.27 |
| 31 | 36.52(4) | 2.458(2) | Magnesio-ferri-hornblende(2,2,-2),Mg-Chamosite(1,-3,2),Quartz(1,1,0),Orthoclase(1,5,0) | 10.62 |
| 32 | 37.555(11) | 2.3930(7) | Magnesio-ferri-hornblende(3,5,0),Mg-Chamosite(1,3,-3),Orthoclase(3,3,-1) | 19.69 |
| 33 | 38.267(8) | 2.3501(5) | Magnesio-ferri-hornblende(3,5,-1),Mg-Chamosite(0,0,6),Biotite(1,1,-4) | 25.63 |
| 34 | 39.41(3) | 2.2845(15) | Magnesio-ferri-hornblende(3,1,-2),Mg-Chamosite(0,4,1),Quartz(1,0,2),Orthoclase(0,4,2), Biotite | 29.66 |
| 35 | 41.551(14) | 2.1716(7) | Magnesio-ferri-hornblende(1,3,2),Mg-Chamosite(2,2,-3),Biotite(1,3,-3) | 17.02 |
| 36 | 42.409(15) | 2.1297(7) | Magnesio-ferri-hornblende(4,4,-1),Mg-Chamosite(2,-2,2),Quartz(2,0,0) | 2.95 |
| 37 | 43.2818 | 2.08872 | Mg-Chamosite(0,4,-3),Biotite(0,4,2) | 3.52 |
| 38 | 44.021(10) | 2.0553(4) | Magnesio-ferri-hornblende(2,0,2),Orthoclase(0,6,1),Biotite(1,1,4) | 6.71 |
| 39 | 44.817(11) | 2.0207(5) | Magnesio-ferri-hornblende(4,0,-2),Mg-Chamosite(2,2,-4),Orthoclase(4,2,-1),Biotite(2,2,-3) | 44.94 |
| 40 | 45.8825 | 1.9762 | Magnesio-ferri-hornblende(3,7,-1),Quartz(2,0,1),Orthoclase(2,2,2) | 4.78 |
| 41 | 47.0204 | 1.93099 | Magnesio-ferri-hornblende(4,2,1),Mg-Chamosite(0,4,4),Orthoclase(4,0,0) | 6.36 |
| 42 | 48.19(11) | 1.887(4) | Magnesio-ferri-hornblende(5,1,0),Mg-Chamosite(2,2,-5),Orthoclase(3,5,-1),Biotite(1,3,-4) | 21.32 |
| 43 | 48.58(2) | 1.8726(8) | Magnesio-ferri-hornblende(1,9,-1) | 7.10 |
| 44 | 50.139(14) | 1.8179(5) | Magnesio-ferri-hornblende(5,3,0),Quartz(1,1,2) | 13.26 |
| 45 | 52.0594 | 1.75531 | Magnesio-ferri-hornblende(1,1,-3),Mg-Chamosite(3,-1,-1),Biotite(2,2,3) | 3.95 |
| 46 | 52.9805 | 1.72695 | Magnesio-ferri-hornblende(2,2,-3),Mg-Chamosite(1,5,1),Orthoclase(2,2,-4),Biotite(1,5,-1) | 4.45 |
| 47 | 54.1183 | 1.69329 | Magnesio-ferri-hornblende(0,8,2),Mg-Chamosite(2,2,5),Orthoclase(5,1,-2),Biotite(2,4,-2) | 4.33 |
| 48 | 55.409(11) | 1.6569(3) | Magnesio-ferri-hornblende(4,6,1),Mg-Chamosite(1,-3,-7),Quartz(1,0,3),Orthoclase(5,1,-1) | 26.88 |
| 49 | 56.51(3) | 1.6273(9) | Mg-Chamosite(1,-5,3),Orthoclase(3,3,-4) | 2.67 |
| 50 | 58.00(5) | 1.5888(13) | Magnesio-ferri-hornblende(6,0,0),Mg-Chamosite(1,1,8),Orthoclase(4,2,-4) | 7.21 |
| 51 | 58.8863 | 1.56704 | Magnesio-ferri-hornblende(1,11,-1),Mg-Chamosite(0,0,9),Orthoclase(0,2,4),Biotite(0,2,6) | 8.27 |
| 52 | 59.56(6) | 1.5509(15) | Magnesio-ferri-hornblende(3,9,1),Mg-Chamosite(1,-5,4),Orthoclase(3,7,-1) | 4.29 |

## Phase Data Pattern

# XRD Results-G408268-LJN2021-042 DG-4/6/2021

## General Information

| ### Measurement date: | 4/6/2021 | ### Interpretative date: | 4/6/2021 |
| --- | --- | --- | --- |
| ### Job Number/Client: | LJN2021-042 DG | ### XRD | Rigaku Miniflex 600 |
| ### Registration Number: | G408268 | ### Analyst: | LUnwin |
| ### Quantitative Method: | PDXL Relative Heights | ### Process Medium: | Selective by Client |
| ### Sample Holder: | Low Reflectance | ### Speed (deg/min): | 0.5 |
| ### Comment: | Shifted -0.05 |  |  |

## Analysis Results

| ### Phase name | ### Content wt% (± error) | ### Formula |
| --- | --- | --- |
| Quartz | 30(8) | SiO2 |
| Biotite | 53(10) | K(Mg,Fe)3[AlSi3O10](OH)2 |
| Mg-Chamosite | 17(5) | (Fe,Mg,Al)6(Si,Al)4O10(OH)8 |

### Notes

Peak overlap may interfere with identifications and quantitative calculations.

Amorphous minerals and minerals present in trace amounts may not be detected.

## Peak List

| No. | 2-theta(deg) | d(ang.) | Phase name | Rel. int. I(a.u.) |
| --- | --- | --- | --- | --- |
| 1 | 6.250(13) | 14.13(3) | Mg-Chamosite(0,0,1) | 3.21 |
| 2 | 8.776(2) | 10.068(3) | Biotite(0,0,1) | 73.17 |
| 3 | 12.492(5) | 7.080(3) | Mg-Chamosite(0,0,2) | 15.54 |
| 4 | 18.833(3) | 4.7081(8) | Mg-Chamosite(0,0,3) | 3.56 |
| 5 | 19.437(11) | 4.563(3) | Biotite(0,2,0),Mg-Chamosite(0,2,0) | 5.04 |
| 6 | 20.814(5) | 4.2642(11) | Quartz(1,0,0),Mg-Chamosite(1,-1,1) | 11.45 |
| 7 | 22.5641 | 3.93734 | Biotite(1,1,1) | 1.20 |
| 8 | 24.211(11) | 3.6731(17) | Biotite(1,1,-2),Mg-Chamosite(1,-1,2) | 4.66 |
| 9 | 25.148(12) | 3.5384(16) | Mg-Chamosite(0,0,4) | 10.76 |
| 10 | 26.161(6) | 3.4035(8) | Biotite(0,2,2) | 6.64 |
| 11 | 26.607(2) | 3.3476(3) | Quartz(0,1,1),Biotite(0,0,3) | 100.00 |
| 12 | 28.32(2) | 3.149(3) | Biotite(1,1,2),Mg-Chamosite(1,-1,3) | 5.11 |
| 13 | 30.59(3) | 2.921(3) | Biotite(1,1,-3) | 6.19 |
| 14 | 31.6115 | 2.82805 | Mg-Chamosite(0,0,5) | 2.00 |
| 15 | 32.4743 | 2.75486 | Unknown | 1.18 |
| 16 | 33.005(12) | 2.7118(9) | Biotite(0,2,3) | 1.63 |
| 17 | 33.7644 | 2.65249 | Biotite(1,3,0),Mg-Chamosite(1,-3,0) | 3.96 |
| 18 | 34.073(12) | 2.6292(9) | Biotite(1,3,-1) | 13.22 |
| 19 | 35.10(2) | 2.5548(18) | Mg-Chamosite(1,3,-2) | 2.26 |
| 20 | 35.717(13) | 2.5119(9) | Biotite(1,1,3) | 5.54 |
| 21 | 36.73(2) | 2.4447(14) | Quartz(1,1,0),Biotite(1,3,-2),Mg-Chamosite(1,-3,2) | 14.75 |
| 22 | 37.53(3) | 2.3944(18) | Mg-Chamosite(0,2,5) | 2.35 |
| 23 | 38.99(4) | 2.308(2) | Biotite(0,4,0),Mg-Chamosite(0,4,0) | 1.99 |
| 24 | 39.429(15) | 2.2835(8) | Quartz(1,0,2),Biotite(2,2,0),Mg-Chamosite(0,4,-1) | 7.85 |
| 25 | 40.241(18) | 2.2392(10) | Mg-Chamosite(2,-2,1) | 1.30 |
| 26 | 41.41(3) | 2.1785(13) | Biotite(1,3,-3),Mg-Chamosite(1,-1,-6) | 11.03 |
| 27 | 42.41(2) | 2.1296(10) | Quartz(2,0,0),Mg-Chamosite(2,-2,2) | 2.54 |
| 28 | 45.084(5) | 2.0093(2) | Biotite(0,0,5),Mg-Chamosite(0,0,7) | 14.89 |
| 29 | 45.720(11) | 1.9828(4) | Quartz(2,0,1),Mg-Chamosite(2,-2,3) | 2.31 |
| 30 | 47.48(7) | 1.913(3) | Biotite(1,3,-4),Mg-Chamosite(1,1,-7) | 3.10 |
| 31 | 48.2466 | 1.88474 | Mg-Chamosite(2,2,-5) | 0.49 |
| 32 | 50.093(12) | 1.8195(4) | Quartz(1,1,2),Mg-Chamosite(2,0,5) | 8.73 |
| 33 | 52.6354 | 1.73745 | Biotite(3,1,-1),Mg-Chamosite(2,-2,-6) | 1.19 |
| 34 | 54.781(19) | 1.6744(5) | Quartz(0,2,2),Biotite(1,5,-2),Mg-Chamosite(2,-4,-3) | 17.85 |
| 35 | 56.9158 | 1.61653 | Biotite(2,4,-3),Mg-Chamosite(1,-5,3) | 1.12 |
| 36 | 59.0289 | 1.5636 | Mg-Chamosite(3,-1,-5) | 2.15 |

## Phase Data Pattern

# XRD Results-G408275-LJN2021-042-DG-17/06/2021

## General Information

| ### Measurement date: | 4/6/2021 | ### Interpretative date: | 17/6/2021 |
| --- | --- | --- | --- |
| ### Job Number/Client: | LJN2021-042 DG | ### XRD | Rigaku Miniflex 600 |
| ### Registration Number: | G408275 | ### Analyst: | LUnwin |
| ### Quantitative Method: | PDXL Relative Heights | ### Process Medium: | Selective by Client |
| ### Sample Holder: | Low Reflectance | ### Speed (deg/min): | 0.5 |
| ### Comment: | Shifted -0.07 |  |  |

## Analysis Results

| ### Phase name | ### Content wt% (± error) | ### Formula |
| --- | --- | --- |
| Quartz | 32(8) | SiO2 |
| Albite | 39(10) | NaAlSi3O8 |
| Mg-Chamosite | 10(4) | (Fe,Mg,Al)6(Si,Al)4O10(OH)8 |
| Orthoclase | 7(3) | K(AlSi3O8) |
| Calcite | 1(1) | CaCO3 |
| Clinopyroxene | 8(3) | (Ca,Na)(Mg,Fe,Al)Si2O6 |
| Biotite | 3(2) | K(Mg,Fe)3[AlSi3O10](OH)2 |

### Notes

Peak overlap may interfere with identifications and quantitative calculations.

Amorphous minerals and minerals present in trace amounts may not be detected.

## Peak List

| No. | 2-theta(deg) | d(ang.) | Phase name | Rel. int. I(a.u.) |
| --- | --- | --- | --- | --- |
| 1 | 6.247(17) | 14.14(4) | Mg-Chamosite(0,0,1) | 3.17 |
| 2 | 8.740(8) | 10.110(9) | Biotite(0,0,1) | 6.79 |
| 3 | 12.484(6) | 7.084(3) | Mg-Chamosite(0,0,2) | 12.01 |
| 4 | 13.846(11) | 6.391(5) | Albite(0,0,1),Clinopyroxene(1,1,0) | 6.12 |
| 5 | 15.06(2) | 5.877(8) | Albite(1,1,-1),Orthoclase(1,1,-1) | 0.76 |
| 6 | 18.75(2) | 4.728(6) | Mg-Chamosite(0,0,3) | 4.30 |
| 7 | 20.825(5) | 4.2621(10) | Quartz(1,0,0),Mg-Chamosite(1,-1,1) | 16.51 |
| 8 | 22.001(7) | 4.0367(12) | Albite(2,0,-1) | 11.08 |
| 9 | 22.924(11) | 3.8763(18) | Mg-Chamosite(0,2,2),Calcite(0,1,2) | 4.99 |
| 10 | 23.584(6) | 3.7693(9) | Albite(1,1,1),Orthoclase(1,3,0) | 13.31 |
| 11 | 23.949(8) | 3.7127(12) | Mg-Chamosite(1,-1,2) | 9.40 |
| 12 | 24.267(7) | 3.6648(10) | Albite(1,3,0),Biotite(1,1,-2),Clinopyroxene(1,1,1) | 11.12 |
| 13 | 25.081(4) | 3.5476(6) | Mg-Chamosite(0,0,4),Orthoclase(2,2,-1) | 7.16 |
| 14 | 25.492(10) | 3.4913(14) | Albite(1,1,-2),Mg-Chamosite(1,1,-3),Orthoclase | 4.65 |
| 15 | 26.621(4) | 3.3458(5) | Quartz(0,1,1),Albite(2,-2,-1),Mg-Chamosite(0,2,-3),Biotite(0,0,3),Clinopyroxene(0,2,1) | 100.00 |
| 16 | 27.508(13) | 3.2399(15) | Orthoclase(0,4,0) | 4.66 |
| 17 | 27.789(7) | 3.2078(8) | Albite(2,0,-2),Clinopyroxene(2,2,0) | 33.46 |
| 18 | 27.954(4) | 3.1892(4) | Albite(0,4,0) | 64.97 |
| 19 | 28.237(10) | 3.1579(11) | Albite(2,2,0),Mg-Chamosite(1,-1,3),Biotite(1,1,2) | 11.30 |
| 20 | 29.389(14) | 3.0366(14) | Calcite(1,0,4) | 2.65 |
| 21 | 29.803(14) | 2.9954(13) | Mg-Chamosite(1,1,-4),Orthoclase(1,3,1),Clinopyroxene(2,2,-1) | 8.68 |
| 22 | 30.397(10) | 2.9382(9) | Albite(0,4,-1),Orthoclase(2,2,-2),Clinopyroxene(3,1,0) | 14.72 |
| 23 | 31.330(7) | 2.8528(6) | Albite(1,3,1),Mg-Chamosite(0,0,5),Calcite(0,0,6) | 10.98 |
| 24 | 33.80(2) | 2.6495(15) | Albite(1,-3,-2),Biotite(2,0,-1) | 3.96 |
| 25 | 35.25(4) | 2.544(3) | Albite(2,4,-1),Mg-Chamosite(1,1,-5),Orthoclase(1,1,2),Biotite(1,1,3),Clinopyroxene | 10.30 |
| 26 | 36.515(6) | 2.4588(4) | Quartz(1,1,0),Albite(2,2,1),Mg-Chamosite(1,3,2),Orthoclase(1,5,0) | 8.46 |
| 27 | 36.98(16) | 2.429(10) | Albite(2,-4,-1),Mg-Chamosite(0,2,-5),Orthoclase(1,5,-1),Biotite(2,0,1) | 1.81 |
| 28 | 39.114(19) | 2.3012(10) | Mg-Chamosite(0,4,-1),Orthoclase(0,4,2),Biotite(0,4,0) | 1.74 |
| 29 | 39.456(10) | 2.2820(5) | Quartz(1,0,2),Albite(1,-1,-3),Mg-Chamosite(1,-3,3),Biotite(2,2,0),Calcite(1,1,3),Clinopyroxene(3,1,1) | 6.50 |
| 30 | 40.251(12) | 2.2387(6) | Quartz(1,1,1),Orthoclase(2,2,-3),Biotite(0,4,1),Clinopyroxene(3,1,-2) | 1.92 |
| 31 | 42.364(15) | 2.1318(7) | Quartz(2,0,0),Albite(0,6,0),Mg-Chamosite(2,2,2),Orthoclase(2,4,1),Clinopyroxene | 7.23 |
| 32 | 42.89(4) | 2.1069(17) | Albite(1,5,1),Mg-Chamosite(0,2,-6),Orthoclase(4,0,-1),Biotite(0,4,2),Calcite(2,0,2),Clinopyroxene(4,2,-1) | 6.44 |
| 33 | 44.90(2) | 2.0172(10) | Albite(2,4,1),Mg-Chamosite(0,0,7),Orthoclase(4,2,-1),Biotite(2,2,-3),Clinopyroxene(0,4,1) | 4.57 |
| 34 | 45.58(6) | 1.989(2) | Albite(0,2,3),Biotite(1,3,3) | 1.79 |
| 35 | 45.738(8) | 1.9821(3) | Quartz(2,0,1) | 2.35 |
| 36 | 46.82(6) | 1.939(2) | Mg-Chamosite(1,1,-7) | 0.66 |
| 37 | 48.25(3) | 1.8845(11) | Albite(3,5,-1),Orthoclase(2,6,0),Calcite(1,1,6) | 1.98 |
| 38 | 49.133(12) | 1.8528(4) | Albite(4,0,-3),Mg-Chamosite(2,-2,4),Orthoclase(4,2,0),Clinopyroxene(3,3,1) | 1.62 |
| 39 | 49.772(11) | 1.8305(4) | Albite(1,-1,3),Mg-Chamosite(2,0,5),Orthoclase(3,5,0),Biotite(2,2,-4),Clinopyroxene(5,1,0) | 6.19 |
| 40 | 50.089(5) | 1.81965(16) | Quartz(1,1,2),Albite(4,0,0) | 9.80 |
| 41 | 50.678(12) | 1.7999(4) | Quartz(0,0,3),Albite(3,3,1),Mg-Chamosite(0,4,5),Orthoclase(0,6,2) | 3.57 |
| 42 | 51.271(11) | 1.7804(4) | Mg-Chamosite(0,0,8) | 5.19 |
| 43 | 53.06(2) | 1.7246(7) | Albite(4,4,-2),Mg-Chamosite(2,4,-2),Orthoclase(2,2,-4),Biotite(3,1,-1),Clinopyroxene(5,1,-2) | 3.49 |
| 44 | 54.31(3) | 1.6879(9) | Albite(2,-6,1),Mg-Chamosite(1,5,2),Orthoclase(1,7,1),Biotite(2,4,-2) | 1.20 |
| 45 | 54.832(11) | 1.6729(3) | Quartz(0,2,2),Albite(1,-5,-3),Mg-Chamosite(1,-5,-3),Orthoclase(3,1,2),Biotite(2,0,4),Clinopyroxene | 2.98 |
| 46 | 55.285(12) | 1.6603(3) | Quartz(0,1,3),Mg-Chamosite(0,4,6),Orthoclase(5,1,-1),Biotite(1,1,-6) | 1.62 |
| 47 | 58.7(2) | 1.573(5) | Albite(5,1,-1),Mg-Chamosite(1,-3,7),Orthoclase(2,4,-4),Biotite(0,2,6) | 1.32 |

## Phase Data Pattern

# XRD Results-G408276-LJN2021-042-DG-10/6/2021

## General Information

| ### Measurement date: | 10/6/2021 | ### Interpretative date: | 10/6/2021 |
| --- | --- | --- | --- |
| ### Job Number/Client: | LJN2021-042 DG | ### XRD | Rigaku Miniflex 600 |
| ### Registration Number: | G408276 | ### Analyst: | LUnwin |
| ### Quantitative Method: | PDXL Relative Heights | ### Process Medium: | Selective by Client |
| ### Sample Holder: | Low Reflectance | ### Speed (deg/min): | 0.5 |
| ### Comment: | Shifted -0.08, Quartz added for calibration shift |  |  |

## Analysis Results

| ### Phase name | ### Content wt% (± error) | ### Formula |
| --- | --- | --- |
| Microcline | 79(10) | K(AlSi3O8) |
| Magnetite | 101(4) | Fe2+Fe3+2O4 |
| Mg-Chamosite | 3(2) | (Fe,Mg,Al)6(Si,Al)4O10(OH)8 |
| Muscovite | 6(2) | KAl2(AlSi3O10)(OH)2 |
| Calcite | <1 | CaCO3 |
| Pyrite | 1(1) | FeS2 |
| Albite | 1(1) | NaAlSi3O8 |

### Notes

Peak overlap may interfere with identifications and quantitative calculations.

Amorphous minerals and minerals present in trace amounts may not be detected.

## Peak List

| No. | 2-theta(deg) | d(ang.) | Phase name | Rel. int. I(a.u.) |
| --- | --- | --- | --- | --- |
| 1 | 6.21(4) | 14.22(8) | Mg-Chamosite(0,0,1) | 2.23 |
| 2 | 8.845(6) | 9.989(7) | Muscovite(0,0,2) | 17.21 |
| 3 | 12.470(8) | 7.092(5) | Mg-Chamosite(0,0,2) | 10.94 |
| 4 | 13.2247 | 6.68944 | Microcline(1,-1,0) | 0.93 |
| 5 | 13.644(16) | 6.485(8) | Microcline(0,2,0),Albite(0,2,0) | 3.44 |
| 6 | 15.0669 | 5.87542 | Microcline(1,-1,-1),Albite(1,1,-1) | 1.03 |
| 7 | 17.79(3) | 4.983(8) | Muscovite(0,0,4) | 3.43 |
| 8 | 18.252(6) | 4.8566(17) | Magnetite(1,1,1) | 3.29 |
| 9 | 18.74(4) | 4.731(11) | Mg-Chamosite(0,0,3) | 2.25 |
| 10 | 19.349(17) | 4.584(4) | Microcline(0,2,1),Mg-Chamosite(1,1,-1) | 1.62 |
| 11 | 20.8383 | 4.25937 | Microcline(2,0,-1),Quartz(1,0,0),Mg-Chamosite | 16.29 |
| 12 | 22.484(17) | 3.951(3) | Microcline(1,-1,1) | 7.52 |
| 13 | 22.9775 | 3.86742 | Microcline(2,0,0),Albite(1,-1,1),Muscovite(1,1,-3),Calcite(0,1,2) | 2.09 |
| 14 | 23.557(10) | 3.7737(16) | Microcline(1,3,0),Albite(1,1,1) | 31.15 |
| 15 | 24.538(6) | 3.6248(9) | Microcline(1,3,-1) | 6.50 |
| 16 | 25.055(4) | 3.5513(6) | Microcline(2,2,-1),Albite(1,-3,-1),Mg-Chamosite(0,0,4) | 8.01 |
| 17 | 25.622(5) | 3.4739(6) | Microcline(1,-1,-2),Muscovite(1,1,-4) | 26.78 |
| 18 | 26.616(5) | 3.3464(6) | Quartz(0,1,1),Muscovite(0,2,4),Mg-Chamosite(0,2,-3) | 63.35 |
| 19 | 26.825(6) | 3.3208(7) | Microcline(2,2,0),Muscovite(0,0,6),Mg-Chamosite | 50.06 |
| 20 | 27.062(6) | 3.2923(7) | Microcline(2,0,-2) | 18.99 |
| 21 | 27.482(4) | 3.2429(5) | Microcline(0,0,2),Albite(0,4,0) | 100.00 |
| 22 | 28.502(8) | 3.1291(8) | Pyrite(1,1,1) | 1.97 |
| 23 | 29.409(14) | 3.0347(14) | Calcite(1,0,4) | 3.04 |
| 24 | 29.796(12) | 2.9961(11) | Microcline(1,-3,1),Albite(1,-3,1),Muscovite(0,2,5),Mg-Chamosite(1,1,-4) | 32.70 |
| 25 | 30.060(6) | 2.9704(6) | Magnetite(2,2,0) | 7.18 |
| 26 | 30.5089 | 2.9277 | Albite(0,2,-2) | 1.33 |
| 27 | 30.772(10) | 2.9033(9) | Microcline(0,4,1) | 20.29 |
| 28 | 32.255(6) | 2.7731(5) | Microcline(1,-3,-2),Muscovite(1,1,-6) | 10.56 |
| 29 | 32.97(2) | 2.7143(16) | Albite(1,-3,-2),Pyrite(2,0,0) | 3.25 |
| 30 | 34.362(13) | 2.6077(10) | Microcline(3,-1,-2),Mg-Chamosite(1,-3,1) | 9.39 |
| 31 | 34.768(12) | 2.5782(8) | Microcline(2,-4,-1),Muscovite(1,3,0),Mg-Chamosite(1,3,-2) | 20.53 |
| 32 | 35.037(6) | 2.5590(4) | Microcline(1,1,2),Muscovite(2,0,-2),Mg-Chamosite(1,1,-5) | 8.40 |
| 33 | 35.391(5) | 2.5342(4) | Microcline(3,1,0),Magnetite(3,1,1),Albite(2,4,-1),Muscovite(1,3,-2) | 38.65 |
| 34 | 36.506(16) | 2.4594(10) | Quartz(1,1,0),Albite(2,2,1),Muscovite(1,3,-3),Mg-Chamosite(1,3,2) | 5.12 |
| 35 | 37.039(5) | 2.4251(3) | Microcline(1,-5,-1),Magnetite(2,2,2),Albite(1,5,0),Mg-Chamosite(0,2,5),Pyrite(2,1,0) | 8.55 |
| 36 | 37.544(18) | 2.3937(11) | Microcline(3,-3,-1),Albite(3,-1,0),Muscovite(0,2,7),Mg-Chamosite(2,0,2) | 4.61 |
| 37 | 38.614(15) | 2.3298(8) | Microcline(1,-1,-3),Muscovite(1,1,7),Mg-Chamosite(2,-2,0) | 2.98 |
| 38 | 39.42(2) | 2.2842(11) | Quartz(1,0,2),Mg-Chamosite(1,-3,3),Calcite(1,1,3) | 3.78 |
| 39 | 40.264(4) | 2.2380(2) | Microcline(2,-2,-3),Quartz(1,1,1),Albite(1,-3,2),Muscovite(2,2,0) | 1.79 |
| 40 | 40.9661 | 2.20128 | Microcline(1,5,1),Albite(2,-2,-3),Muscovite(2,2,1) | 2.08 |
| 41 | 41.664(14) | 2.1660(7) | Microcline(0,6,0),Albite(0,6,0) | 11.10 |
| 42 | 42.396(12) | 2.1303(6) | Microcline(2,-4,1),Quartz(2,0,0),Albite(3,1,-3),Muscovite(2,0,-6) | 8.98 |
| 43 | 43.016(4) | 2.10101(18) | Magnetite(4,0,0),Albite(1,3,-3),Muscovite(2,2,-4),Mg-Chamosite(0,4,-3),Calcite(2,0,2) | 6.33 |
| 44 | 43.565(16) | 2.0758(7) | Microcline(2,0,2),Albite(1,-5,-2),Muscovite(2,2,3),Mg-Chamosite(1,3,4) | 1.66 |
| 45 | 44.005(16) | 2.0560(7) | Microcline(0,6,1),Albite(0,2,-3),Muscovite(1,1,-9),Mg-Chamosite(2,2,-4) | 1.08 |
| 46 | 45.037(15) | 2.0113(6) | Albite(2,0,2) | 3.50 |
| 47 | 45.39(3) | 1.9965(11) | Muscovite(1,3,6),Mg-Chamosite(2,-2,3) | 6.40 |
| 48 | 45.85(2) | 1.9774(10) | Microcline(2,2,2),Quartz(2,0,1),Albite(3,-1,1) | 8.21 |
| 49 | 46.289(17) | 1.9598(7) | Microcline(3,-3,-3),Muscovite(0,4,5),Mg-Chamosite(0,4,-4) | 0.95 |
| 50 | 47.03(3) | 1.9306(11) | Microcline(2,-6,-1),Magnetite(3,3,1),Albite(4,-2,-2),Muscovite(1,1,9),Calcite(0,2,4) | 3.85 |
| 51 | 47.37(2) | 1.9175(8) | Microcline(4,0,-3),Albite(2,6,-1),Calcite(0,1,8),Pyrite(2,2,0) | 2.23 |
| 52 | 48.30(5) | 1.883(2) | Albite(2,-4,-3),Muscovite(2,0,-8),Calcite(1,1,6) | 2.21 |
| 53 | 48.962(10) | 1.8589(3) | Microcline(1,1,3),Albite(1,-5,2),Mg-Chamosite(0,2,7) | 3.97 |
| 54 | 49.6353 | 1.83521 | Microcline(3,5,0),Albite(0,6,-2),Muscovite(2,2,-7),Mg-Chamosite(2,0,5) | 1.23 |
| 55 | 50.092(10) | 1.8195(3) | Quartz(1,1,2),Albite(2,6,-2) | 7.27 |
| 56 | 50.603(10) | 1.8024(3) | Microcline(0,6,-2),Quartz(0,0,3),Mg-Chamosite(0,4,5),Pyrite(2,2,1) | 20.00 |
| 57 | 51.4233 | 1.77552 | Microcline(4,-4,-2),Albite(1,-7,-1),Muscovite(1,1,10),Mg-Chamosite(0,0,8) | 1.36 |
| 58 | 52.8863 | 1.7298 | Microcline(1,1,-4),Albite(1,1,-4),Muscovite(1,1,-11),Mg-Chamosite(1,5,-2) | 0.87 |
| 59 | 53.37(2) | 1.7152(7) | Magnetite(4,2,2),Albite(4,-4,-2),Mg-Chamosite(3,1,-3) | 2.26 |
| 60 | 53.9699 | 1.6976 | Microcline(1,7,1),Albite(4,4,-1),Muscovite(2,2,7),Mg-Chamosite(1,-5,2) | 0.84 |
| 61 | 54.587(19) | 1.6799(5) | Microcline(3,-5,-3),Albite(3,5,-3),Muscovite(2,4,1),Mg-Chamosite(1,5,-3) | 0.41 |
| 62 | 54.83(3) | 1.6730(8) | Microcline(3,1,2),Quartz(0,2,2),Albite(1,3,3),Muscovite(3,1,-3),Mg-Chamosite(1,-5,-3) | 2.73 |
| 63 | 55.617(15) | 1.6512(4) | Microcline(1,7,-2),Muscovite(2,0,-10),Mg-Chamosite(3,1,2) | 2.11 |
| 64 | 56.194(6) | 1.63557(17) | Microcline(3,5,1),Albite(1,3,-4),Muscovite(2,4,-4),Mg-Chamosite(1,-5,3),Pyrite(3,1,1) | 3.06 |
| 65 | 56.59(7) | 1.6251(19) | Microcline(0,8,0),Quartz(2,1,0),Albite(3,-5,-3),Muscovite(2,2,-9),Mg-Chamosite(2,-4,-4),Calcite(2,1,1) | 7.26 |
| 66 | 56.877(6) | 1.61755(15) | Microcline(1,3,-4),Magnetite(3,3,3),Muscovite(1,3,-10),Mg-Chamosite(2,-2,-7) | 6.50 |
| 67 | 57.8711 | 1.5921 | Albite(1,-3,-4),Muscovite(2,4,-5),Calcite(1,0,10) | 0.94 |
| 68 | 58.661(19) | 1.5725(5) | Microcline(0,2,-4),Albite(0,2,-4),Mg-Chamosite(2,2,6) | 3.67 |
| 69 | 59.06(4) | 1.5629(10) | Microcline(2,2,3),Albite(2,0,3),Muscovite(3,1,-6),Mg-Chamosite(1,-5,4),Pyrite(2,2,2) | 1.65 |

## Phase Data Pattern

# XRD Results-G408277-LJN2021-042-DG-17/6/2021

## General Information

| ### Measurement date: | 8/6/2021 | ### Interpretative date: | 17/6/2021 |
| --- | --- | --- | --- |
| ### Job Number/Client: | LJN2021-042 DG | ### XRD | Rigaku Miniflex 600 |
| ### Registration Number: | G408277 | ### Analyst: | LUnwin |
| ### Quantitative Method: | PDXL Relative Heights | ### Process Medium: | Selective by Client |
| ### Sample Holder: | Standard | ### Speed (deg/min): | 0.5 |
| ### Comment: | Shifted -0.11 |  |  |

## Analysis Results

| ### Phase name | ### Content wt% (± error) | ### Formula |
| --- | --- | --- |
| Quartz | 5(2) | SiO2 |
| Anorthite | 27(8) | CaAl2Si2O8 |
| Clinopyroxene | 22(5) | (Ca,Na)(Mg,Fe,Al)Si2O6 |
| Halloysite-7 | 9(3) | Al2Si2O5(OH)4 |
| Biotite | 3(2) | K(Mg,Fe)3[AlSi3O10](OH)2 |
| Orthoclase | 24(5) | K(AlSi3O8) |
| Smectite (w - 0.8°) | 10(3) |  |

### Notes

Peak overlap may interfere with identifications and quantitative calculations.

Amorphous minerals and minerals present in trace amounts may not be detected.

## Peak List

| No. | 2-theta(deg) | d(ang.) | Phase name | Rel. int. I(a.u.) |
| --- | --- | --- | --- | --- |
| 1 | 5.93665 | 14.8752 | Montmorillonite(0,0,1) | 57.26 |
| 2 | 8.828(3) | 10.009(4) | Biotite(0,0,1) | 13.02 |
| 3 | 12.1519 | 7.27749 | Halloysite-7(0,0,1),Montmorillonite(0,0,2) | 14.17 |
| 4 | 13.5474 | 6.53082 | Anorthite(1,-1,0),Orthoclase(0,2,0) | 5.60 |
| 5 | 13.8074 | 6.40839 | Orthoclase(0,0,1) | 26.56 |
| 6 | 15.00(3) | 5.900(11) | Anorthite(0,2,-1),Orthoclase(1,1,-1) | 3.57 |
| 7 | 17.6847 | 5.01116 | Halloysite-7(1,0,0),Montmorillonite(0,0,3),Biotite(0,0,2) | 10.56 |
| 8 | 18.928 | 4.6847 | Halloysite-7(1,0,-1),Anorthite(0,2,-2) | 6.58 |
| 9 | 19.7365 | 4.49458 | Montmorillonite(0,2,0),Biotite(1,1,0),Clinopyroxene | 19.03 |
| 10 | 20.3673 | 4.35678 | Halloysite-7(0,2,0),Montmorillonite(1,-1,-1),Biotite | 5.13 |
| 11 | 20.8212 | 4.26282 | Quartz(1,0,0),Orthoclase(2,0,-1) | 15.84 |
| 12 | 21.9717 | 4.04214 | Halloysite-7(1,-1,-1),Anorthite(2,0,-2) | 16.08 |
| 13 | 22.9363 | 3.87427 | Halloysite-7(0,2,-1),Montmorillonite(1,-1,-2),Biotite(1,1,1),Anorthite(1,-1,2),Orthoclase(2,0,0) | 8.92 |
| 14 | 23.558(11) | 3.7735(18) | Anorthite(1,-3,0),Orthoclase(1,3,0) | 32.47 |
| 15 | 24.20(3) | 3.675(4) | Halloysite-7(1,0,1) | 20.32 |
| 16 | 25.639 | 3.47167 | Halloysite-7(1,-1,1),Anorthite(1,1,-4),Orthoclase(1,1,-2) | 14.54 |
| 17 | 26.5906 | 3.34955 | Halloysite-7(1,1,1),Montmorillonite(1,-1,3),Biotite(0,2,2),Quartz(1,0,1),Anorthite(1,-1,-4),Orthoclase(2,2,0),Clinopyroxene(0,2,1) | 59.30 |
| 18 | 27.4376 | 3.24805 | Halloysite-7(1,2,-1),Orthoclase(0,4,0) | 29.94 |
| 19 | 27.6565 | 3.22284 | Anorthite(0,4,0) | 36.52 |
| 20 | 27.9011 | 3.19513 | Anorthite(2,0,-4) | 100.00 |
| 21 | 28.3067 | 3.15027 | Halloysite-7(1,-2,-1),Anorthite(2,2,0) | 13.31 |
| 22 | 29.0602 | 3.07028 | Halloysite-7(1,-1,-2),Anorthite(2,1,1) | 4.07 |
| 23 | 29.7029 | 3.00528 | Montmorillonite(0,0,5),Orthoclase(1,3,1),Clinopyroxene | 23.62 |
| 24 | 30.305(13) | 2.9470(12) | Anorthite(0,4,-2),Orthoclase(2,2,-2),Clinopyroxene(3,1,0) | 57.47 |
| 25 | 30.703(14) | 2.9096(13) | Halloysite-7(0,3,0),Biotite(1,1,-3),Anorthite(1,4,0),Orthoclase(0,4,1),Clinopyroxene | 27.25 |
| 26 | 31.4442 | 2.84272 | Anorthite(2,-2,-4) | 2.60 |
| 27 | 32.3111 | 2.7684 | Halloysite-7(0,3,-1),Orthoclase(1,3,-2) | 1.51 |
| 28 | 33.09(4) | 2.705(3) | Halloysite-7(0,2,2) | 10.62 |
| 29 | 33.774 | 2.65176 | Halloysite-7(0,3,1),Anorthite(1,-3,-4) | 4.09 |
| 30 | 34.86(3) | 2.5714(18) | Halloysite-7(1,-2,-2),Montmorillonite(2,0,0),Biotite(1,3,-1),Anorthite(2,-2,2),Orthoclase(3,1,-2),Clinopyroxene(2,0,-2) | 58.86 |
| 31 | 35.500(12) | 2.5267(8) | Halloysite-7(1,-3,0),Anorthite(2,-4,-2),Orthoclase(3,1,0) | 40.43 |
| 32 | 36.5373 | 2.4573 | Halloysite-7(1,1,2),Montmorillonite(1,-3,-2),Quartz(1,1,0),Anorthite(2,4,-3),Orthoclase(1,5,0) | 2.66 |
| 33 | 37.621 | 2.38897 | Halloysite-7(0,0,3),Anorthite(1,-5,1),Orthoclase(2,0,-3) | 4.81 |
| 34 | 38.6505 | 2.32767 | Halloysite-7(2,0,-2),Biotite(1,1,-4),Anorthite(3,-3,-2),Orthoclase(1,1,-3) | 2.63 |
| 35 | 38.9756 | 2.309 | Halloysite-7(1,-2,2),Orthoclase(0,4,2) | 4.05 |
| 36 | 39.3548 | 2.28762 | Halloysite-7(1,-1,-3),Montmorillonite(1,3,-3),Biotite(0,4,0),Quartz(1,0,2) | 5.02 |
| 37 | 40.80(3) | 2.2098(14) | Halloysite-7(2,2,-1),Orthoclase(3,3,0),Clinopyroxene(0,4,0) | 8.75 |
| 38 | 41.64(2) | 2.1670(11) | Halloysite-7(2,0,1),Montmorillonite(1,-1,-6),Biotite(0,2,4),Anorthite(3,-3,0),Orthoclase(3,1,-3),Clinopyroxene(3,3,0) | 16.33 |
| 39 | 42.31(3) | 2.1346(13) | Halloysite-7(2,2,0),Montmorillonite(2,0,-4),Biotite(2,2,1),Quartz(2,0,0),Anorthite(2,-4,2),Orthoclase(2,4,1),Clinopyroxene(3,3,-1) | 26.91 |
| 40 | 42.66 | 2.11772 | Anorthite(2,4,-5),Orthoclase(4,0,-1),Clinopyroxene(4,2,-1) | 3.67 |
| 41 | 44.2313 | 2.04607 | Halloysite-7(1,-2,-3),Biotite(1,1,4) | 2.87 |
| 42 | 44.7189 | 2.02488 | Halloysite-7(2,-2,-2),Anorthite(4,-1,-3),Orthoclase | 4.30 |
| 43 | 45.26(2) | 2.0020(10) | Halloysite-7(1,-3,2),Biotite(2,2,-3),Quartz(2,0,1),Anorthite(0,6,2),Orthoclase(4,2,-2) | 28.82 |
| 44 | 47.1029 | 1.9278 | Halloysite-7(2,2,1),Montmorillonite(2,-2,4),Biotite(1,1,-5),Anorthite(4,2,-4),Orthoclase(2,6,-1) | 1.78 |
| 45 | 48.4575 | 1.87703 | Halloysite-7(1,4,-2),Biotite(0,4,3),Anorthite(1,6,-4) | 2.57 |
| 46 | 49.3244 | 1.84605 | Halloysite-7(2,2,-3),Anorthite(4,0,-6),Orthoclase(4,2,0),Clinopyroxene(5,1,0) | 6.62 |
| 47 | 49.7579 | 1.83098 | Halloysite-7(1,1,-4),Biotite(0,2,5),Quartz(1,1,2),Orthoclase(3,5,0) | 8.66 |
| 48 | 50.647(19) | 1.8009(6) | Halloysite-7(1,-3,-3),Montmorillonite(1,3,-6),Anorthite(1,1,6),Orthoclase(0,6,2) | 8.40 |
| 49 | 52.08(3) | 1.7548(9) | Orthoclase(1,5,-3) | 4.21 |
| 50 | 52.7921 | 1.73266 | Halloysite-7(0,1,4),Montmorillonite(1,-1,8),Biotite(2,0,-5),Anorthite(2,2,-8),Orthoclase(1,3,3) | 3.36 |
| 51 | 53.98(6) | 1.6974(16) | Biotite(3,1,-2),Orthoclase(1,7,1) | 5.00 |
| 52 | 54.9052 | 1.67087 | Halloysite-7(0,4,-3),Quartz(2,0,2),Orthoclase(3,1,2) | 4.27 |
| 53 | 56.498(19) | 1.6275(5) | Halloysite-7(1,4,2),Biotite(3,1,-3),Orthoclase(5,1,-3),Clinopyroxene(5,3,-1) | 11.14 |
| 54 | 57.6685 | 1.59721 | Biotite(2,4,-3),Anorthite(5,-1,-2),Orthoclase(4,2,-4) | 3.07 |
| 55 | 59.222(9) | 1.5590(2) | Halloysite-7(3,0,-3),Biotite(2,2,4),Orthoclase(3,7,-1) | 3.10 |

## Phase Data Pattern

# XRD Results-G408279

## General Information

| ### Measurement date: | 22/04/2021 | ### Interpretative date: | 10/04/2024 |
| --- | --- | --- | --- |
| ### Job Number/Client: | LJN2021-042 DG | ### XRD | Rigaku Miniflex 600 |
| ### Registration Number: | G408279 | ### Analyst: | LUnwin/T Coyte |
| ### Quantitative Method: | Siroquant | ### Process Medium: | Selective by Client |
| ### Sample Holder: | Low Reflectance | ### Speed (deg/min): | 0.5 |
| ### Comment: | Shifted -0.02 |  |  |

## Analysis Results

| ### Phase name | ### Content% | ### Formula |
| --- | --- | --- |
| ### Illite | ### 48 (10) | K0.7Al2[Al0.7Si3.3O10](OH)2 |
| Phlogopite | 24 (5) | KMg3(Si3Al)O10(OH)2 |
| Amphibole* | 16 (5) | Variable silicate |
| Chlorite* (Clinochlore)* | 10 (4) | (Mg,Fe,Al)6(Si,Al)4O10(OH,O)8 |
| Serpentine Group* | 2 (2) | Mg3Si2O5(OH)4 |

### Notes

Peak overlap may interfere with identifications and quantitative calculations.

Amorphous minerals and minerals present in trace amounts may not be detected.

Chlorite* possibly Clinochlore, ideally would have done additional testing but no sample available.

Serpentine group* Without additional testing it is possible that serpentine is not even present.

There is an unusual broad 7.3Å peak

A percentage of Phlogopite is poorly crystallized, (altering to Chlorite? And Illite?)

Amphibole* possibly actinolite or ferro actinolite

## Peak List

| No. | 2-theta | d | Phase name | Rel. height |
| --- | --- | --- | --- | --- |
|  | (deg) | (ang.) |  | (a.u.) |
| 1 | 6.20(3) | 14.24(6) | Chlorite (Clinochlore Fe bearing)(0,0,1) | 0.45 |
| 2 | 8.690(3) | 10.167(3) | Phlogopite(0,0,1) | 88.13 |
| 3 | 9.59(4) | 9.22(4) | Amphibole(0,2,0) | 1.08 |
| 4 | 10.465(4) | 8.447(3) | Amphibole(1,1,0) | 6.13 |
| 5 | 12.103(14) | 7.307(8) | Serpentine Group(0,0,1),Chlorite (Clinochlore Fe bearing)(0,0,2) | 7.92 |
| 6 | 17.499(4) | 5.0639(12) | Amphibole(1,3,0),Phlogopite(0,0,2) | 12.03 |
| 7 | 18.49(3) | 4.794(7) | Amphibole(2,0,0),Chlorite (Clinochlore Fe bearing)(0,0,3) | 2.02 |
| 8 | 19.19(3) | 4.621(7) | Phlogopite(0,2,0),Serpentine Group(0,2,0) | 1.8 |
| 9 | 19.53(5) | 4.541(11) | Amphibole(0,4,0) | 1.34 |
| 10 | 21.05(4) | 4.218(8) | Amphibole(2,2,0) | 1.19 |
| 11 | 24.272(11) | 3.6640(17) | Phlogopite(1,1,-2),Serpentine Group(0,0,2),Chlorite (Clinochlore Fe bearing)(0,0,4) | 4.34 |
| 12 | 26.373(5) | 3.3767(6) | Amphibole(1,3,1),Phlogopite(0,0,3) | 100 |
| 13 | 27.137(14) | 3.2834(17) | Amphibole(2,4,0) | 4.11 |
| 14 | 28.120(12) | 3.1707(13) | Phlogopite | 1.83 |
| 15 | 28.461(4) | 3.1335(4) | Amphibole(3,1,0) | 8.72 |
| 16 | 29.735(17) | 3.0022(16) | Amphibole(2,4,-1) | 2.75 |
| 17 | 30.28(4) | 2.950(3) | Amphibole(1,5,-1) | 2.75 |
| 18 | 30.7(3) | 2.91(2) | Phlogopite(1,1,-3),Serpentine Group(1,1,-2),Chlorite (Clinochlore Fe bearing)(0,0,5) | 1.06 |
| 19 | 32.75(2) | 2.7321(19) | Amphibole(3,3,-1) | 1.14 |
| 20 | 33.065(8) | 2.7070(7) | Amphibole(1,5,1),Phlogopite(0,2,3),Chlorite (Clinochlore Fe bearing)(1,1,4) | 3.25 |
| 21 | 34.18(3) | 2.621(2) | Amphibole(0,6,1),Phlogopite(1,3,0),Serpentine Group(2,1,0),Chlorite (Clinochlore Fe bearing)(1,3,1) | 3.09 |
| 22 | 35.421(18) | 2.5321(13) | Amphibole(2,6,0),Phlogopite(0,0,4),Serpentine Group(2,0,1) | 12.51 |
| 23 | 36.852(18) | 2.4371(11) | Amphibole(2,2,-2),Phlogopite(2,0,1),Serpentine Group(2,1,1) | 3.39 |
| 24 | 38.444(7) | 2.3397(4) | Amphibole(3,5,-1) | 1.88 |
| 25 | 38.96(6) | 2.310(3) | Amphibole(4,2,-1),Chlorite (Clinochlore Fe bearing)(0,4,1) | 1.15 |
| 26 | 41.310(15) | 2.1838(8) | Amphibole(2,4,-2),Phlogopite(2,0,2),Serpentine Group(1,1,-3) | 2.48 |
| 27 | 42.243(17) | 2.1377(8) | Amphibole(1,5,-2),Serpentine Group(1,4,0),Chlorite (Clinochlore Fe bearing)(0,2,6) | 0.96 |
| 28 | 44.672(8) | 2.0269(3) | Amphibole(3,5,1),Phlogopite(0,0,5),Chlorite (Clinochlore Fe bearing)(1,3,-5) | 36.27 |
| 29 | 45.16(4) | 2.0061(15) | Amphibole(4,0,-2),Phlogopite(1,3,3) | 2.2 |
| 30 | 54.48(3) | 1.6828(8) | Amphibole(2,6,2),Phlogopite(2,0,4) | 5.55 |
| 31 | 55.587(14) | 1.6520(4) | Amphibole(2,10,-1),Serpentine Group(3,2,-1) | 1.66 |
| 32 | 56.73(4) | 1.6214(11) | Amphibole(2,4,-3) | 0.8 |
| 33 | 59.99(4) | 1.5409(9) | Amphibole(6,4,-1),Phlogopite(3,1,2),Serpentine Group(3,2,-2),Chlorite (Clinochlore Fe bearing)(0,6,2) | 3.08 |

## Phase Data Pattern