Mineral Resources Tasmania

Mineralogical/Petrology Report

# Mineralogy and geochemical ANALYSES, Hercules mine

# Mineralogy and geochemical ANALYSES, Hercules mine

LJN2021-044

An unpublished Mineral Resources Tasmania Report for:

University of Qeensland and Mineral Resources Tasmania

An unpublished Mineral Resources Tasmania Report for:

University of Qeensland and Mineral Resources Tasmania

By:      	R S Bottrill

Date:   	17/05/2021

By:      	R.S. Bottrill, L. Unwin

Date:   17 May 2021

# Summary

The spotted rock, in H1127 has abundant carbonate spherules containing a mixture of dolomite (probably Mn rich) and kutnohorite, in a matrix of muscovite and chlorite.

The whispy foliated lenticular white/green rock, in H1034 is a quartz-sericite rock; the reason for the very low totals on the pXRF is unexplained.

A high content of Mn +/- Ca detected in other samples of these cores by portable XRF spectrometer suggests rhodochrosite and kutnohorite can be locally dominant in other parts of the cores not tested by XRD.

# Introduction & Background

Two rock samples were collected from some Hercules mine drill cores by Laura Jackson (UQ) and Ralph Bottrill (MRT). They were submitted to MRT to help determine the mineralogy of the rocks. G410195 was of interest to determine the carbonate minerals, and G410195 was tested as the pXRF gave very low totals.

# Samples

The details of the samples collected are given in Table 1 below.

Table 1: Sample details

| MRT Lab Number | Field # | Location | Sample Description | Process |
| --- | --- | --- | --- | --- |
| G410195 | H1127/50m | Hercules mine | Carbonate spotting | Xrd, pXRF |
| G410196 | H1034/35'2" | Hercules mine | Pink-white/green sericitic/cherty rock | Xrd, pXRF |

# Process

The samples were all prepared, examined by stereomicroscopy, tested by pXRF (portable X-ray Fluorescence spectrometry) for chemistry and were analysed by XRD (X-ray diffraction) for mineralogy. All preparation and testing was done in the Mineral Resources Tasmania (MRT) laboratories, Rosny Park and Mornington, Tasmania.

# Sample Descriptions

G410195	H1127/50m	Carbonate spotting

This rock is an unfoliated grey-green rock composed mostly of very pale grey carbonate spots about 5mm in diameter, in a dark green chloritic matrix. The oxidised surface shows some iron staining. There are some small carbonate-quartz-sulphide veins cross cutting it (Fig. 1).

Figure 1. G410195. Spotted carbonate-rich rock. FOV (field of view) ~120mm.

G410196	H1034/35'2"	Pink-white/green sericitic/cherty rock

This rock is a strongly foliated, mottled with white to pale pink lenticular clasts to about 20x60mm, in a grey-green sericitic matrix. The oxidised surface shows some weak iron staining (Fig. 1).

Figure 2. G410196. Sericite-chert rock. FOV (field of view) ~110mm.

# XRD analyses

The samples were prepared, examined, and analysed in the MRT laboratories, Rosny Park, Tasmania. They were run on a Rigaku Miniflex 600 X-Ray Diffractometer system: a 600W generator 150mm goniometer with a Cu tube; 40kV/15mA, sample spinner and a Scintillation counter (SC) with Be window, a graphite counter monochromator and a Kß Ni- filter. Measurement setup: 3-63° Theta/2Theta range, with a scanning speed of 0.5° /min. The analysis software used is the PDXL2 using the ICCD database.

Quantification is largely manual, using a series of prepared standards of the more common minerals to enable some semi-quantitative analysis. Quartz, if present, is used as an internal standard; and if not present, it is often added to the sample for a supplementary scan.  Our semi-quantitative results are calculated using single-peak calibration factors derived from scans of known mixtures of minerals.

The results are shown in Appendix 1 and summarised in Table 2. G410195 has carbonate spherules containing a mixture of dolomite (probably Mn rich) and kutnohorite, with a matrix of muscovite and chlorite and trace pyrite. G410196 is a quartz-sericite rock.

Table 2: XRD Summary

| Sample No | G410195 | G410196 |
| --- | --- | --- |
| Description | Spotted carbonate rock | Sericite-Chert |
| Muscovite | 36(8) | 17(5) |
| Quartz |  | 80(10) |
| Chlorite* | 8(3) |  |
| Dolomite | 43(10) |  |
| Kutnohorite | 9(3) |  |
| Siderite |  | 3(2) |
| Pyrite | 4(2) |  |

# pXRF

The sample was analysed for major and trace elements using an Olympus Vanta M Series pXRF. The instrument uses a 4-Watt X-ray tube with application optimized anode material (rhodium Rh and tungsten W): 8-50 kV with a large area Silicon Drift Detector. The instrument uses the built-in Olympus Vanta analysis software version 3.12.34.

The results are shown in Table 3 and discussed below.

Table 3: pXRF Summary

| Sample ID | DL | Hercules1 | Hercules2 | Hercules3 | Hercules4 | Hercules5 | Hercules6 |
| --- | --- | --- | --- | --- | --- | --- | --- |
| Reg No |  |  |  |  |  | G410195 | G410195 |
| Interpreted main carbonate |  | Rhc | Kut | Kut | Kut | Dol | Dol |
| SiO2 (%) | 9 | 43 | 25 | 12 | (1) | 18 | 23 |
| TiO2 (%) | 0.2 | (0.2) | (0) | (0) | (0) | 0.7 | 1.1 |
| Al2O3 (%) | 5 | 6 | (0) | (0) | (0) | 11 | 15 |
| Fe2O3 (%) | 1.0 | 2.0 | (0.5) | 1.4 | 3.1 | 2.2 | 2.5 |
| MnO (%) | 0.1 | 14.5 | 4.5 | 15.7 | 17.5 | 3.8 | 2.9 |
| MgO (%) | 1.5 | (0) | (0) | (0) | 5.2 | 5.9 | 4.7 |
| CaO (%) | 1.0 | (0.8) | 11.5 | 19.3 | 26.8 | 17.2 | 11.7 |
| K2O (%) | 2.0 | 2.8 | (0) | (0) | (0) | 5.5 | 9.2 |
| P2O5 (%) | 0.5 | (0) | (0) | (0) | (0) | (0.1) | (0.1) |
| S (%) | 1.0 | (0.4) | (0) | (0) | (0) | (0.5) | (0.6) |

| Sample ID | DL | Hercules7 | Hercules8 | Hercules9 | Hercules10 | Hercules11 | Hercules12 |
| --- | --- | --- | --- | --- | --- | --- | --- |
| Reg No |  |  |  | G410196 | G410196 | G410196 |  |
| Interpreted main carbonate |  |  | Rhc |  |  |  |  |
| SiO2 (%) | 9 | 72 | 11 | 19 | 24 | 24 | 61 |
| TiO2 (%) | 0.2 | 0.2 | (0.1) | (0.2) | (0.1) | (0.1) | (0.1) |
| Al2O3 (%) | 5 | (4) | (2) | (0) | (2) | (1) | (1) |
| Fe2O3 (%) | 1.0 | (0.5) | 5.0 | (0.8) | 3.9 | (0.5) | (0.4) |
| MnO (%) | 0.1 | (0) | 24.4 | (0.1) | 0.3 | 0.1 | 0.1 |
| MgO (%) | 1.5 | (0) | (0) | (0) | (0) | (0) | (0) |
| CaO (%) | 1.0 | (0) | 2.6 | (0.1) | (0) | (0.6) | (0.2) |
| K2O (%) | 2.0 | 2.9 | (1.7) | (1.3) | (1) | (2) | (2) |
| P2O5 (%) | 0.5 | (0) | (0) | (0) | (0) | (0) | (0) |
| S (%) | 1.0 | (0.7) | (0.7) | (0.1) | (0.1) | (0.1) | (0.1) |

The pXRF strongly suggests a mixture of Ca-Mn-Mg carbonates in these rocks, including rhodochrosite, kutnohorite and dolomite.

# Discussion and Summary

G410195 (spotted rock, H1127) has abundant carbonate spherules containing a mixture of dolomite (probably Mn rich) and subordinate kutnohorite, in a matrix of muscovite and chlorite with trace pyrite.

G410196 (lenticular white/green rock, H1034) is a quartz-sericite rock; the reason for the very low totals on the pXRF is unexplained.

PXRF suggests rhodochrosite and kutnohorite are locally dominant in parts of the core, but were not tested by XRD.

R S Bottrill 					L Unwin

Mineralogist/Petrologist	Technical Officer

Disclaimers

While every care has been taken in the preparation of this report, no warranty is given as to the correctness of the information and no liability is accepted for any statement or opinion or for any error or omission. No reader should act or fail to act on the basis of any material contained herein. Readers should consult professional advisers. As a result the Crown in Right of the State of Tasmania and its employees, contractors and agents expressly disclaim all and any liability (including all liability from or attributable to any negligent or wrongful act or omission) to any persons whatsoever in respect of anything done or omitted to be done by any such person in reliance whether in whole or in part upon any of the material in this report.

This and other data collected in MRT laboratories may enter the MRT databases but every attempt will be made to ensure it remains closed file and not be available externally, unless at your request.

Appendix 1: MRT Laboratory Report

Client:  MRT, UQ

Sample Location:  Hercules

Job Number:  LJN20201-044

Analyses:  Approximate Mineralogy

Methods: XRD

Analyst:  L Unwin

Lab Manager: R Bottrill

Date:  7/5/2021

# XRD Results-G410195-LJN2021-044-Jackson-QA1-13/5/21

## General Information

| ### Measurement date: | 7/5/2021 | ### Interpretative date: | 13/5/2021 |
| --- | --- | --- | --- |
| ### Job Number/Client: | LJN2021-44 Jackson | ### XRD | Rigaku Miniflex 600 |
| ### Registration Number: | G410195 | ### Analyst: | LUnwin |
| ### Quantitative Method: | PDXL Relative Heights | ### Process Medium: | Wholerock |
| ### Sample Holder: | Standard | ### Speed (deg/min): | 0.5 |
| ### Comment: | Shifted -0.07 |  |  |

## Analysis Results

| ### Phase name | ### Content wt% (± error) | ### Formula |
| --- | --- | --- |
| Muscovite | 36(8) | KAl2(AlSi3O10)(OH)2 |
| Dolomite | 43(10) | CaMg(CO3)2 |
| Chlorite* | 8(3) | (Fe,Mg,Al)6(Si,Al)4O10(OH)8 |
| Pyrite | 4(2) | FeS |
| Kutnohorite | 9(3) | Ca(Mn,Mg,Fe2+)(CO3)2 |

### Notes

Peak overlap may interfere with identifications and quantitative calculations.

Amorphous minerals and minerals present in trace amounts may not be detected.

Chlorite* probably Clinochlore

## Phase Data Pattern

# XRD Results-G410196-LJN2021-044-Jackson-QA1-13/5/21

## General Information

| ### Measurement date: | 7/5/2021 | ### Interpretative date: | 13/5/2021 |
| --- | --- | --- | --- |
| ### Job Number/Client: | LJN2021-044 Jackson | ### XRD | Rigaku Miniflex 600 |
| ### Registration Number: | G410196 | ### Analyst: | LUnwin |
| ### Quantitative Method: | PDXL Relative Heights | ### Process Medium: | Wholerock |
| ### Sample Holder: | Standard | ### Speed (deg/min): | 0.5 |
| ### Comment: |  |  |  |

## Analysis Results

| ### Phase name | ### Content wt% (± error) | ### Formula |
| --- | --- | --- |
| Muscovite | 17(5) | KAl2(AlSi3O10)(OH)2 |
| Quartz | 80(10) | SiO2 |
| Siderite | 3(2) | FeCO3 |

### Notes

Peak overlap may interfere with identifications and quantitative calculations.

Amorphous minerals and minerals present in trace amounts may not be detected.

## Phase Data Pattern

Appendix 2: Abbreviations

| Abbreviations | Mineral |
| --- | --- |
| Ab | Albite |
| Am- | Amphibole |
| Anh- | Anhydrite |
| Ank- | Ankerite |
| Bar | Baryte |
| Bt | Biotite |
| Cal | Calcite |
| Chl | Chlorite |
| Dol | Dolomite |
| Ep | Epidote |
| Gyp | Gypsum |
| Kut | Kutnohorite |
| Mont | Montmorillonite |
| Ms | Muscovite |
| Py | Pyrite |
| Q | Quartz |
| Rhc | Rhodochrosite |

Appendix 1: MRT Laboratory Report

Client:  MRT, UQ

Sample Location:  Hercules

Job Number:  LJN20201-044

Analyses:  Approximate Chemistry

Methods: pXRF

Analyst:  L Unwin

Lab Manager: R Bottrill

Date:  29/4/2021

| Sample ID | DL | Hercules | Hercules | Hercules | Hercules | Hercules | Hercules |
| --- | --- | --- | --- | --- | --- | --- | --- |
| Date | - | 29/4/21 | 29/4/21 | 29/4/21 | 29/4/21 | 29/4/21 | 29/4/21 |
| Time | - | 12:27:46 | 12:31:45 | 12:33:29 | 12:36:39 | 12:37:52 | 12:40:04 |
| Method | - | Geochem(2) | Geochem(2) | Geochem(2) | Geochem(2) | Geochem(2) | Geochem(2) |
| Reg No./ID |  | Rhc | Kut | Kut | Kut | G410195 | G410195 |
| SiO2 (%) | 9 | 43 | 25 | 12 | (1) | 18 | 23 |
| TiO2 (%) | 0.2 | (0.2) | (0) | (0) | (0) | 0.7 | 1.1 |
| Al2O3 (%) | 5 | 6 | (0) | (0) | (0) | 11 | 15 |
| Fe2O3 (%) | 1.0 | 2.0 | (0.5) | 1.4 | 3.1 | 2.2 | 2.5 |
| MnO (%) | 0.1 | 14.5 | 4.5 | 15.7 | 17.5 | 3.8 | 2.9 |
| MgO (%) | 1.5 | (0) | (0) | (0) | 5.2 | 5.9 | 4.7 |
| CaO (%) | 1.0 | (0.8) | 11.5 | 19.3 | 26.8 | 17.2 | 11.7 |
| K2O (%) | 2.0 | 2.8 | (0) | (0) | (0) | 5.5 | 9.2 |
| P2O5 (%) | 0.5 | (0) | (0) | (0) | (0) | (0.1) | (0.1) |
| S (%) | 1.0 | (0.4) | (0) | (0) | (0) | (0.5) | (0.6) |
| As (ppm) | 100 | (0) | (0) | (0) | (0) | (47) | (62) |
| Bi (ppm) | 200 | (0) | (0) | (0) | (0) | (0) | (0) |
| Cr (ppm) | 50 | (0) | (0) | (0) | (0) | (0) | 75 |
| Cu (ppm) | 50 | (15) | (0) | (0) | (0) | (14) | (16) |
| Mo (ppm) | 100 | (0) | (0) | (0) | (0) | (0) | (15) |
| Nb (ppm) | 30 | (10) | (0) | (0) | (0) | (15) | (18) |
| Ni (ppm) | 30 | (0) | (0) | (0) | (0) | (0) | (0) |
| Pb (ppm) | 10 | (0) | (0) | (0) | (0) | (0) | (0) |
| Rb (ppm) | 10 | 77 | (0) | (0) | (0) | 214 | 333 |
| Sb (ppm) | 100 | (0) | (0) | (0) | (0) | (0) | (0) |
| Sn (ppm) | 100 | (0) | (0) | (0) | (0) | (0) | (0) |
| Sr (ppm) | 10 | (9) | 40 | 126 | 131 | 138 | 103 |
| Th (ppm) | 100 | (0) | (0) | (0) | (0) | (0) | (0) |
| U (ppm) | 50 | (0) | (0) | (0) | (0) | (0) | (0) |
| V (ppm) | 100 | (48) | (0) | (0) | (0) | 261 | 421 |
| W (ppm) | 150 | (0) | (0) | (0) | (0) | (0) | (0) |
| Y (ppm) | 20 | (0) | (8) | 26 | 32 | 31 | 37 |
| Zn (ppm) | 20 | 1290 | (6) | 20 | 26 | 267 | 69 |
| Zr (ppm) | 50 | (29) | (0) | (0) | (0) | 226 | 326 |
| Total |  | 68 | 41 | 48 | 53 | 64 | 70 |

| Sample ID | DL | Hercules | Hercules | Hercules | Hercules | Hercules | Hercules |
| --- | --- | --- | --- | --- | --- | --- | --- |
| Date | - | 29/4/21 | 29/4/21 | 29/4/21 | 29/4/21 | 29/4/21 | 29/4/21 |
| Time | - | 12:41:39 | 12:43:17 | 12:45:10 | 12:48:39 | 12:49:33 | 12:50:56 |
| Method | - | Geochem(2) | Geochem(2) | Geochem(2) | Geochem(2) | Geochem(2) | Geochem(2) |
| Reg No./ID |  |  | Rhc | G410196 | G410196 | G410196 |  |
| SiO2 (%) | 9 | 72 | 11 | 19 | 24 | 24 | 61 |
| TiO2 (%) | 0.2 | 0.2 | (0.1) | (0.2) | (0.1) | (0.1) | (0.1) |
| Al2O3 (%) | 5 | (4) | (2) | (0) | (2) | (1) | (1) |
| Fe2O3 (%) | 1.0 | (0.5) | 5.0 | (0.8) | 3.9 | (0.5) | (0.4) |
| MnO (%) | 0.1 | (0) | 24.4 | (0.1) | 0.3 | 0.1 | 0.1 |
| MgO (%) | 1.5 | (0) | (0) | (0) | (0) | (0) | (0) |
| CaO (%) | 1.0 | (0) | 2.6 | (0.1) | (0) | (0.6) | (0.2) |
| K2O (%) | 2.0 | 2.9 | (1.7) | (1.3) | (1) | (2) | (2) |
| P2O5 (%) | 0.5 | (0) | (0) | (0) | (0) | (0) | (0) |
| S (%) | 1.0 | (0.7) | (0.7) | (0.1) | (0.1) | (0.1) | (0.1) |
| As (ppm) | 100 | (24) | (53) | (0) | (0) | (0) | (0) |
| Bi (ppm) | 200 | (0) | (0) | (0) | (0) | (0) | (0) |
| Cr (ppm) | 50 | (0) | (0) | (0) | (0) | (0) | (0) |
| Cu (ppm) | 50 | 73 | (0) | (15) | (17) | 148 | 110 |
| Mo (ppm) | 100 | (0) | (0) | (0) | (0) | (0) | (0) |
| Nb (ppm) | 30 | (0) | (7) | (4) | (4) | (8) | (5) |
| Ni (ppm) | 30 | (0) | (0) | (0) | (0) | (0) | (0) |
| Pb (ppm) | 10 | (0) | (0) | (0) | (0) | (0) | (0) |
| Rb (ppm) | 10 | 99 | 90 | 50 | 33 | 74 | 68 |
| Sb (ppm) | 100 | (0) | (0) | (0) | (0) | (0) | (0) |
| Sn (ppm) | 100 | (0) | (0) | (0) | (0) | (0) | (0) |
| Sr (ppm) | 10 | 16 | 28 | (8) | (7) | 10 | (6) |
| Th (ppm) | 100 | (0) | (0) | (0) | (0) | (0) | (0) |
| U (ppm) | 50 | (0) | (0) | (0) | (0) | (0) | (0) |
| V (ppm) | 100 | (56) | (22) | (47) | (0) | (29) | (41) |
| W (ppm) | 150 | (0) | (0) | (0) | (0) | (0) | (0) |
| Y (ppm) | 20 | (12) | 28 | (9) | (4) | (11) | (10) |
| Zn (ppm) | 20 | 3196 | 44 | 738 | 240 | 325 | 279 |
| Zr (ppm) | 50 | 83 | 67 | 74 | 57 | 80 | 64 |
| Total |  | 75 | 43 | 19 | 29 | 24 | 61 |