MINERAL RESOURCES TASMANIA

Laboratory Report

LJN2021-107

# Soil tests and analyses,

# Penna landslip

An unpublished Mineral Resources Tasmania Report for:

MRT

By:	 R.S. Bottrill, T Coyte, J Renaud and L Unwin

Date:	19 May 2022

# Summary

Eight soil samples from the Penna landslip were collected by Claire Kain in November 2021 and submitted to MRT Laboratories for soil testing and mineralogical analyses.

The Atterberg test results showed the generally clayey nature of the soils at the site and indicate soil classifications, corresponded to inorganic clays of medium to high plasticity (CH).  Sizing test also showed the samples vary from a Clay to a Sandy Loam based on the USDA soil classes.

The Emerson Class number (ECN) indicated that most samples tested had a tendency for the soil to slake with some dispersion.  E204205 tended to slake with low susceptibility for dispersion and E204206 had a low susceptibility to slake with some swelling.

XRD analyses were dominated by quartz and kaolinite, with rock sample E204203 containing mostly goethite.  Other phases identified in these samples are Illite/vermiculite, anatase, goethite and halloysite lepidocrocite and sepiolite.

# Introduction

Eight soil samples were collected in November 2021 from the Penna landslip by Claire Kain and submitted to MRT Laboratories for soil tests and mineralogical analyses. They were prepared and analysed by standard mineralogical and petrophysical techniques in the MRT laboratories, Rosny Park and Mornington.

# Samples

The details of the soil samples supplied by C Kain are given in Table 1 below and shown in Figs. 1 – 8 below. Sample E204203 is an ironstone; the remainder are reduced to slightly oxidised kaolinitic clays.

Table 1: Sample details.

| MRT Reg# | Location | Sample Description | Process |
| --- | --- | --- | --- |
| E204201 | Penna | Silty/clayey orange mottled grey sand. Bedding visible | XRD, sizing |
| E204202 | Penna | Orange/brown mottled grey plastic clay | XRD, Atterbergs, sizing |
| E204203 | Penna | Hard, orange-brown ironstone(?) | XRD |
| E204204 | Penna | Saturated grey plastic clay | XRD, Atterbergs, sizing |
| E204205 | Penna | Grey plastic clay | XRD, Atterbergs, sizing |
| E204206 | Penna | Stiff grey-brown clay | XRD, Atterbergs, sizing |
| E204207 | Penna | Silty/clayey orange mottled grey sand | XRD, sizing |
| E204208 | Penna | Grey plastic clay | XRD, Atterbergs, sizing |

Figure 1. Sample E204201. Silty/clayey orange mottled grey sand. Bedding visible. FOV ~100 mm.

Figure 2. Sample E204202. Orange/brown mottled grey plastic clay  FOV ~100 mm.

Figure 3. Sample E204203. Hard, orange-brown ironstone(?) FOV ~200 mm.

.

Figure 4. Sample E204204. Saturated grey plastic clay  FOV ~100 mm.

.

Figure 5. Sample E204205. Grey plastic clay FOV ~100 mm.

Figure 6. Sample E204206. Stiff grey-brown clay FOV ~100 mm.

Figure 7. Sample E204207. Silty/clayey orange mottled grey sand.  FOV ~100 mm.

.

Figure 8. Sample E204208.  Grey plastic clay. FOV ~100 mm.

# Sample Preparation

The samples were split into representative subsamples and analysed for mineralogy by XRD (X-Ray diffraction), in the Mineral Resources Tasmania (MRT) laboratories, Rosny.  Some samples were also subsamples for prepared for Atterberg tests, sediment and sieve size analysis, in the Mineral Resources Tasmania (MRT) laboratories, Rosny Park and Mornington, Tasmania.

# AtterBerg Limits, Dispersion and Moisture Content

The following tests were undertaken in compliance with the following Australian Standards:

- Liquid Limit (LL) AS 1289.3.1.1  [pre-dried at 105oC; see Test Note 1 (a)]

- Plastic Limit (PL) AS 1289.3.2.1

- Plasticity Index (PI) AS 1289.3.3.1

- Linear Shrinkage (LS) AS 1289.3.4.1

- Dispersion AS1289.3.8.1

Figure 9. Liquid limit (Atterberg) testing at MRT

The results of the Atterberg tests are presented below in Table 2 and on Figs 10 & 11. For Atterbergs, samples were air dried and checked for coarse particles.  Water used was distilled or demineralised. Emerson Dispersions were completed on natural samples.

All the soil samples can be classified as high plasticity (CH or OH) clays.  The relationship between Plasticity Index and Linear Shrinkage was plotted and showed some correlation indicated by a general cluster of points, this is presented below in Figure 11.

Figure 10. Plasticity chart (Australian Standard AS1726)

Table 1: USCS – inorganic fine-grained soils component only (ASTM D2487, ASTM D2488 and Casagrande, 1948)

| Liquid Limit | Plasticity Index relative to A-line | Soil class and plasticity | Code |
| --- | --- | --- | --- |
| Liquid Limit <50% (L) | On or above | Lean Clay Inorganic clays, sandy clays, silty clays, lean clays. Low to medium plasticity, no or slow dilatancy. | CL |
|  | Below | Silt Inorganic silts and very fine sands, rock flour, silty or clayey fine sands. Slight plasticity to non-plastic, slow to rapid dilatancy. | ML |
| Liquid Limit >50% (H) | On or above | Fat Clay Inorganic clays, fat clays. High plasticity, no dilatancy. | CH |
|  | Below | Elastic Silt Micaceous or diatomaceous fine sandy and silty soils, elastic silts. Low to medium plasticity, no to slow dilatancy. | MH |
| Liquid Limit <30% (L) Plasticity Index 4 to 7% | Not applicable | Silty Clay Mixed zone where both CL and ML soils plot | CL-ML |

Table 2:  Summary – Atterberg Limits, and Dispersion

|  |  | Atterberg Limits |  |  |  | Dispersion ECN |
| --- | --- | --- | --- | --- | --- | --- |
| MRT Reg. No. | Sample | LL | PL | LS | PI |  |
| E204202 | Orange/brown mottled grey plastic clay | 104% | 37% | 15% | 67% | 2 |
| E204204 | Saturated grey plastic clay | 129% | 37% | 10% | 92% | 2 |
| E204205 | Grey plastic clay | 115% | 36% | 14% | 79% | 6 |
| E204206 | Stiff grey-brown clay | 100% | 30% | 15% | 70% | 7 |
| E204208 | Grey plastic clay | 92% | 29% | 13% | 63% | 2 |

Figure 11. Relationship between Plasticity Index and Linear Shrinkage

# Particle Size analysis

Seven sample of soil were submitted for sizing analysis. The sample details are shown in Table 1.

The whole samples were wet sieved by hand sieving, using Australian standard sieves.  Each fraction was weighed and determined as a proportion of the total sample. Sedimentation Analysis was conducted on a whole sub-sample to determine the <2 micron fraction.  The results are shown in Tables 4 and Appendix 2.  Sieving was complete in accordance with AS1289.3.6.1 with some slight modifications.  Fine particle size analysis was completed using a modified AS1289.3.6.3 sedimentation method.

Table 4: Size analysis summary)

| Sample No. | <38 um (%) | ≤20 um (%) | ≤10 um (%) | ≤2 um (%) |
| --- | --- | --- | --- | --- |
| E204201 | 98.1 | 45.0 | 37.3 | 19.6 |
| E204202 | 99.6 | 86.0 | 84.3 | 80.3 |
| E204204 | 99.7 | 92.5 | 91.4 | 89.0 |
| E204205 | 97.3 | 67.4 | 66.5 | 64.7 |
| E204206 | 98.5 | 96.3 | 93.8 | 88.1 |
| E204207 | 39.0 | 32.4 | 27.0 | 14.4 |
| E204208 | 85.1 | 43.4 | 41.9 | 38.5 |

# XRD analyses

The samples were prepared, examined and analysed in the MRT laboratories, Rosny Park, Tasmania. They were run on a Rigaku Miniflex 600 X-Ray Diffractometer system: a 600W generator 150mm goniometer with a Cu tube; 40kV/15mA, sample spinner and a Scintillation counter (SC) with Be window, a graphite counter monochromator and a Kß Ni- filter. The analysis was performed using the following conditions: +3° to 63° 2Theta scanning and measuring range, with a scanning speed of 0.5 °/min with a resolution of 0.02° by step. The analysis software used is the PDXL2 using the ICCD database.

The results are shown in Appendix 1, and Table 5 and summarised below.

Table 5. Main mineral phases identified and qualitative results

| Mineral | E204201 | E204202 | E204203 | E204204 | E204205 | E204206 | E204207 | E204208 |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Kaolinite | Sub-major | 52(10) | 8(3) | 48(10) | 36(10) | 40(10) | 10(3) | Major |
| Quartz | Major | 37(10) | 6(3) | 38(10) | 27(5) | 39(10) | 88(10) | Major |
| Mixed Layer Clay | Very Minor | 9(3) |  | 13(4) | 9(3) | 7(3) |  | Trace |
| Anatase | Faint Trace | 3(2) |  |  | 2(2) | 3(2) |  | Trace |
| Halite | Trace |  |  | 1(1) |  | 1(1) | 2(2) |  |
| Goethite |  |  | 86(10) |  | 9(3) | 11(4) |  |  |
| Lepidocrocite | Sub-major |  |  |  |  |  |  |  |

E204203 (ironstone) is mostly goethite with very minor quartz and kaolinite. Quartz and kaolinite are the main mineralogical phases in the other samples, with most samples also having minor amounts of mixed-layer clays (Illite/smectite or vermiculite?), anatase and halite; some have goethite and one has lepidocrocite (E204201).

Results summary

Size analyses (sieving and sediment sizing) indicates the samples vary from a Clay to a Sandy Loam based on the USDA soil classes.  Samples are described below:

- Sample E204201is a Silt Loam, with 20% of the sample <2um

- Sample E204202 is a Clay, with 80% of the sample <2um.

- Sample E204204 is a Clay, with 89% of the sample <2um.

- Sample E204205 is a Clay, with 65% of the sample <2um.

- Sample E204206 is a Clay, with 88% of the sample <2um.

- Sample E204207 is somewhere between a Clay Loan and Sandy Loam, with 14% of the sample <2um.

- Sample E204208 is a Silty Clay, with 38% of the sample <2um.

Based on Atterberg tests, the samples E204202, E204204, E204205, E204206 and E204208 are all classified as high plasticity clays (CH) using the Unified Soil Classification Scheme.

The Emerson Class number (ECN) for soils related to the potential for a soil to slake and disperse.  Most samples tested indicated a tendency for the soil to slake with some dispersion.  E204205 tended to slake with low susceptibility for dispersion and E204206 had a low susceptibility to slake with some swelling.

The ironstone is mostly goethite with very minor quartz and kaolinite. Quartz and kaolinite are the main mineralogical phases in the other samples (Penna Clays), with most samples also having minor amounts of mixed-layer clays (Illite/smectite or vermiculite?); some have goethite and one has lepidocrocite.

R.S. Bottrill 						T Coyte, J Renaud & L Unwin

MINERALOGIST/PETROLOGIST 		TECHNICAL OFFICERS

# Disclaimers

While every care has been taken in the preparation of this report, no warranty is given as to the correctness of the information and no liability is accepted for any statement or opinion or for any error or omission. No reader should act or fail to act on the basis of any material contained herein. Readers should consult professional advisers. As a result the Crown in Right of the State of Tasmania and its employees, contractors and agents expressly disclaim all and any liability (including all liability from or attributable to any negligent or wrongful act or omission) to any persons whatsoever in respect of anything done or omitted to be done by any such person in reliance whether in whole or in part upon any of the material in this report. The MRT laboratories are not NATA registered but work to similar standards. This and other data collected in MRT laboratories may enter the MRT databases but every attempt will be made to ensure it remains closed file and not be available externally, unless at your request.

# Laboratory Details

Mineral Resources Tasmania (MRT) operates a laboratory facility at its offices at Rosny Park and Mornington, Tasmania. In the interests of full disclosure, these laboratories do not have NATA accreditation. However, all tests are performed according to relevant Australian Standards cited in the report and subject to internal peer review processes. The analytical facilities at MRT are periodically compared against other similar laboratories in other jurisdictions with favourable results.

# Appendix 1: Laboratory Report: XRD Analyses

# XRD Results-E204201

### General Information

| Measurement date: | 9/12/2021 | Interpretative date: | 19/5/2022 |
| --- | --- | --- | --- |
| Job Number/Client: | LJN2021-107 CKain | XRD | Rigaku Miniflex 600 |
| Registration Number: | E204201 | Analyst: | LUnwin |
| Quantitative Method: | Semi-Quantitative | Process Medium: | Wholerock |
| Sample Holder: | Standard | Speed (deg/min): | 0.5 |
| Comment: | Shifted -0.01, Sample dried at 30degrees |  |  |

### Analysis Results

| Phase name | Content - Estimate | Formula |
| --- | --- | --- |
| Kaolinite | Sub-major | Al2(Si2O5)(OH)4 |
| Mixed Layer Clay | Very Minor | Various |
| Quartz | Sub-major | SiO2 |
| Lepidocrocite | Sub-major | Fe3+O(OH) |
| Halite | Trace | NaCl |
| Anatase | Faint Trace | TiO2 |

### Peak List

| No. | 2-theta(deg) | d(ang.) | Phase name | Rel. int. I(a.u.) |
| --- | --- | --- | --- | --- |
| 1 | 8.83288 | 10.0032 | Mixed Layer Clay(0,0,1) | 3.74 |
| 2 | 12.372(5) | 7.148(3) | Kaolinite(0,0,1) | 36.20 |
| 3 | 14.157(3) | 6.2507(14) | Lepidocrocite(0,2,0) | 37.39 |
| 4 | 17.7276 | 4.99912 | Kaolinite(1,0,0),Mixed Layer Clay(0,0,2) | 1.18 |
| 5 | 19.8836 | 4.46167 | Kaolinite(0,2,0),Mixed Layer Clay(0,2,0) | 20.55 |
| 6 | 20.3766 | 4.35481 | Kaolinite(1,-1,0) | 9.64 |
| 7 | 20.8449 | 4.25803 | Quartz(1,0,0) | 34.44 |
| 8 | 24.90(3) | 3.572(4) | Kaolinite(1,0,1),Mixed Layer Clay(1,1,-2) | 40.65 |
| 9 | 25.259 | 3.52303 | Anatase(1,0,1) | 4.49 |
| 10 | 26.6155 | 3.34647 | Quartz(1,0,1),Kaolinite(1,1,1),Mixed Layer Clay(0,2,2) | 100.00 |
| 11 | 27.026(8) | 3.2966(9) | Lepidocrocite(0,2,1),Kaolinite(1,2,0) | 21.69 |
| 12 | 29.7562 | 3.00003 | Lepidocrocite(1,1,0) | 1.88 |
| 13 | 31.666(14) | 2.8233(12) | Kaolinite(0,2,-2),Halite(2,0,0) | 11.08 |
| 14 | 35.108(15) | 2.5540(11) | Kaolinite(2,0,-1),Mixed Layer Clay(1,3,0) | 22.62 |
| 15 | 36.32(2) | 2.4716(13) | Lepidocrocite(1,3,0),Kaolinite(1,-3,-1),Mixed Layer Clay(2,0,-2) | 32.27 |
| 16 | 36.484(5) | 2.4608(4) | Quartz(1,1,0),Kaolinite(2,-1,-1),Mixed Layer Clay(1,3,1) | 4.62 |
| 17 | 38.19(6) | 2.355(3) | Lepidocrocite(1,1,1),Kaolinite(1,0,-3),Anatase(1,0,3),Mixed Layer Clay(2,0,1) | 28.63 |
| 18 | 39.385(13) | 2.2859(7) | Quartz(0,1,2),Kaolinite(1,3,1) | 5.82 |
| 19 | 40.249(7) | 2.2389(4) | Quartz(1,1,1),Mixed Layer Clay(2,2,-1) | 2.59 |
| 20 | 42.420(15) | 2.1291(7) | Quartz(2,0,0),Kaolinite(0,2,-3),Mixed Layer Clay | 7.00 |
| 21 | 43.254(19) | 2.0900(9) | Lepidocrocite(1,3,1),Kaolinite(2,2,-2) | 1.92 |
| 22 | 45.403(11) | 1.9959(5) | Kaolinite(2,0,-3),Halite(2,2,0) | 8.11 |
| 23 | 45.732(13) | 1.9824(5) | Quartz(0,2,1),Kaolinite(1,-3,2),Mixed Layer Clay | 6.45 |
| 24 | 46.74(2) | 1.9418(9) | Lepidocrocite(1,5,0),Kaolinite(2,3,-1),Mixed Layer Clay(2,0,-4) | 17.45 |
| 25 | 49.316 | 1.84634 | Kaolinite(1,-3,-3) | 1.66 |
| 26 | 50.082(10) | 1.8199(3) | Quartz(1,1,2) | 10.71 |
| 27 | 52.69(6) | 1.7357(18) | Lepidocrocite(1,5,1),Kaolinite(2,3,1),Mixed Layer Clay(1,1,5) | 5.01 |
| 28 | 54.951 | 1.66959 | Quartz(2,0,2),Lepidocrocite(0,4,2),Kaolinite(2,4,-1),Anatase(1,0,5),Mixed Layer Clay(2,4,0) | 21.68 |
| 29 | 56.5223 | 1.62684 | Lepidocrocite(1,1,2),Kaolinite(3,-1,0),Halite(2,2,2) | 2.12 |
| 30 | 58.923(16) | 1.5661(4) | Lepidocrocite(0,8,0),Kaolinite(2,-4,1),Mixed Layer Clay(0,2,6) | 2.40 |
| 31 | 59.901(5) | 1.54290(12) | Quartz(2,1,1),Lepidocrocite(1,7,0),Kaolinite(3,1,-3),Mixed Layer Clay(1,5,-3) | 7.80 |

### Phase Data Pattern

# XRD Results-E204202

### General Information

| Measurement date: | 9/12/2021 | Interpretative date: | 19/5/2022 |
| --- | --- | --- | --- |
| Job Number/Client: | LJN2021-107 CKain | XRD | Rigaku Miniflex 600 |
| Registration Number: | E204202 | Analyst: | LUnwin |
| Quantitative Method: | PDXL Relative Heights | Process Medium: | Wholerock |
| Sample Holder: | Standard | Speed (deg/min): | 0.5 |
| Comment: | Shifted -0.03, Sample dried at 30degrees |  |  |

### Analysis Results

| Phase name | Content wt% (± error) | Formula |
| --- | --- | --- |
| Kaolinite | 52(10) | Al2(Si2O5)(OH)4 |
| Mixed Layer Clay | 9(3) | Various |
| Quartz | 37(10) | SiO2 |
| Anatase | 3(2) | TiO2 |

Notes

Peak overlap may interfere with identifications and quantitative calculations.

Amorphous minerals and minerals present in trace amounts may not be detected.

### Peak List

| No. | 2-theta(deg) | d(ang.) | Phase name | Rel. int. I(a.u.) |  |
| --- | --- | --- | --- | --- | --- |
| 1 | 8.78762 | 10.0546 | Mixed Layer Clay(0,0,1) | 10.82 |  |
| 2 | 12.352(8) | 7.160(5) | Kaolinite(0,0,2) | 85.86 |  |
| 3 | 17.816 | 4.97452 | Mixed Layer Clay(0,0,2) | 2.49 |  |
| 4 | 19.9029 | 4.45739 | Kaolinite(1,1,-1),Mixed Layer Clay(0,2,0) | 32.70 |  |
| 5 | 20.8421 | 4.25859 | Kaolinite(0,2,1),Quartz(1,0,0) | 20.85 |  |
| 6 | 21.3049 | 4.16713 | Mixed Layer Clay(0,2,1) | 17.58 |  |
| 7 | 24.91(2) | 3.571(3) | Kaolinite(0,0,4),Mixed Layer Clay(1,1,-2) | 29.83 |  |
| 8 | 25.1918 | 3.53228 | Kaolinite(1,1,-3),Anatase(1,0,1) | 16.25 |  |
| 9 | 26.616(3) | 3.3464(3) | Quartz(1,0,1),Mixed Layer Clay(0,2,2) | 100.00 |  |
| 10 | 34.93(2) | 2.5666(16) | Kaolinite(1,1,4),Mixed Layer Clay(1,3,0) | 16.75 |  |
| 11 | 35.9209 | 2.49804 | Kaolinite(1,3,-2),Mixed Layer Clay(1,1,3) | 11.48 |  |
| 12 | 36.489(11) | 2.4605(7) | Quartz(1,1,0),Mixed Layer Clay(1,3,1) | 9.17 |  |
| 13 | 37.7552 | 2.38078 | Kaolinite(0,0,6),Anatase(0,0,4),Mixed Layer Clay(2,0,1) | 10.18 |  |
| 14 | 38.3387 | 2.34588 | Kaolinite(1,3,2),Anatase(1,1,2) | 11.81 |  |
| 15 | 39.409(5) | 2.2846(3) | Quartz(1,0,2) | 12.36 |  |
| 16 | 40.22(2) | 2.2405(12) | Kaolinite(2,2,-1),Quartz(1,1,1),Mixed Layer Clay(2,2,-1) | 4.59 |  |
| 17 | 42.383(4) | 2.1309(2) | Kaolinite(2,2,1),Quartz(2,0,0),Mixed Layer Clay(1,3,-3) | 6.13 |  |
| 18 | 45.73(3) | 1.9823(12) | Kaolinite(1,1,6),Quartz(2,0,1),Mixed Layer Clay(2,2,-3) | 10.26 |  |
| 19 | 47.90(3) | 1.8977(11) | Kaolinite(2,2,3),Anatase(2,0,0),Mixed Layer Clay(2,0,3) | 2.58 |  |
| 20 | 50.066(4) | 1.82041(13) | Quartz(1,1,2) | 13.34 |  |
| 21 | 51.0299 | 1.78828 | Kaolinite(0,0,8),Mixed Layer Clay(2,2,-4) | 1.72 |  |
| 22 | 54.3232 | 1.68739 | Kaolinite(2,4,-1),Mixed Layer Clay(1,5,-1) | 3.24 |  |
| 23 | 54.8689 | 1.67189 | Kaolinite(1,3,6),Anatase(2,1,1),Quartz(2,0,2),Mixed Layer Clay(0,4,4) | 11.98 |  |
| 24 | 55.297 | 1.65996 | Kaolinite(1,5,-2),Quartz(1,0,3),Mixed Layer Clay(1,5,1) | 5.33 |  |
| 25 | 59.885(7) | 1.54328(16) | Quartz(2,1,1) | 9.08 |  |

### Phase Data Pattern

# XRD Results-E204203

### General Information

| Measurement date: | 22/12/2021 | Interpretative date: | 19/5/2022 |
| --- | --- | --- | --- |
| Job Number/Client: | LJN2021-107 CKain | XRD | Rigaku Miniflex 600 |
| Registration Number: | E204203 | Analyst: | LUnwin |
| Quantitative Method: | PDXL Relative Heights | Process Medium: | Wholerock |
| Sample Holder: | Standard | Speed (deg/min): | 0.5 |
| Comment: | Shifted -0.01, Sample dried at 30degrees |  |  |

### Analysis Results

| Phase name | Content wt% (± error) | Formula |
| --- | --- | --- |
| Kaolinite | 8(3) | Al2(Si2O5)(OH)4 |
| Goethite | 86(10) | α-Fe3+O(OH) |
| Quartz | 6(3) | SiO2 |

### Peak List

| No. | 2-theta(deg) | d(ang.) | Phase name | Rel. int. I(a.u.) |
| --- | --- | --- | --- | --- |
| 1 | 12.28(3) | 7.199(15) | Kaolinite(0,0,1) | 5.68 |
| 2 | 17.84(2) | 4.969(6) | Goethite(0,2,0) | 10.63 |
| 3 | 19.96(3) | 4.444(6) | Kaolinite(0,2,0) | 6.34 |
| 4 | 20.8441 | 4.25819 | Quartz(1,0,0) | 3.21 |
| 5 | 21.222(7) | 4.1831(13) | Kaolinite(1,1,-1),Goethite(1,1,0) | 100.00 |
| 6 | 24.8456 | 3.58072 | Kaolinite(0,0,2) | 4.67 |
| 7 | 26.36(8) | 3.379(10) | Kaolinite(1,-1,1),Goethite(1,2,0) | 10.03 |
| 8 | 26.630(3) | 3.3447(4) | Quartz(1,0,1) | 13.69 |
| 9 | 33.262(18) | 2.6914(14) | Goethite(1,3,0) | 36.43 |
| 10 | 34.784(12) | 2.5771(9) | Kaolinite(2,0,-1),Goethite(0,2,1) | 16.15 |
| 11 | 35.61(3) | 2.5191(19) | Kaolinite(1,-3,-1),Goethite(1,0,1) | 1.09 |
| 12 | 36.1155 | 2.48502 | Kaolinite(2,0,0),Goethite(0,4,0) | 11.06 |
| 13 | 36.677(16) | 2.4483(10) | Goethite(1,1,1),Quartz(1,1,0) | 77.25 |
| 14 | 38.337 | 2.34598 | Kaolinite(2,0,-2) | 5.39 |
| 15 | 39.97(3) | 2.2537(18) | Kaolinite(1,3,-2),Goethite(1,2,1),Quartz(1,1,1) | 13.60 |
| 16 | 41.27(3) | 2.1858(15) | Kaolinite(2,0,1),Goethite(1,4,0) | 14.89 |
| 17 | 42.6716 | 2.11717 | Kaolinite(0,4,1),Quartz(2,0,0) | 2.51 |
| 18 | 43.2134 | 2.09187 | Kaolinite(2,2,-2),Goethite(2,2,0) | 1.82 |
| 19 | 45.13(2) | 2.0074(10) | Kaolinite(2,0,-3),Goethite(1,3,1) | 7.20 |
| 20 | 47.38(3) | 1.9173(11) | Kaolinite(1,1,3),Goethite(0,4,1) | 5.35 |
| 21 | 50.0946 | 1.81946 | Kaolinite(1,1,-4),Goethite(1,5,0),Quartz(1,1,2) | 4.84 |
| 22 | 50.69(2) | 1.7995(7) | Kaolinite(1,-1,-4),Goethite(2,1,1),Quartz(0,0,3) | 9.74 |
| 23 | 51.6659 | 1.76775 | Goethite(1,4,1) | 2.54 |
| 24 | 53.29(3) | 1.7178(8) | Kaolinite(2,-2,2),Goethite(2,2,1) | 33.06 |
| 25 | 54.31(4) | 1.6877(12) | Kaolinite(2,4,-1),Goethite(2,4,0),Quartz(2,0,2) | 11.99 |
| 26 | 55.5129 | 1.65401 | Kaolinite(3,1,-2),Goethite(0,6,0),Quartz(1,0,3) | 4.61 |
| 27 | 57.54(3) | 1.6004(7) | Kaolinite(1,5,1),Goethite(2,3,1) | 1.94 |
| 28 | 59.09(4) | 1.5621(9) | Kaolinite(1,-5,-2),Goethite(1,5,1) | 15.85 |

### Phase Data Pattern

# XRD Results-E204204

### General Information

| Measurement date: | 9/12/2021 | Interpretative date: | 19/5/2022 |
| --- | --- | --- | --- |
| Job Number/Client: | LJN2021-107 CKain | XRD | Rigaku Miniflex 600 |
| Registration Number: | E204204 | Analyst: | LUnwin |
| Quantitative Method: | PDXL Relative Heights | Process Medium: | Wholerock |
| Sample Holder: | Standard | Speed (deg/min): | 0.5 |
| Comment: | Shifted -0.03, Sample dried at 30degrees |  |  |

### Analysis Results

| Phase name | Content wt% (± error) | Formula |
| --- | --- | --- |
| Kaolinite | 48(10) | Al2(Si2O5)(OH)4 |
| Mixed Layer Clay | 13(4) | Various |
| Quartz | 38(10) | SiO2 |
| Halite | 1(1) | NaCl |

### Peak List

| No. | 2-theta(deg) | d(ang.) | Phase name | Rel. int. I(a.u.) |
| --- | --- | --- | --- | --- |
| 1 | 8.84(2) | 10.00(3) | Mixed Layer Clay(0,0,1) | 11.83 |
| 2 | 12.268(14) | 7.209(8) | Kaolinite(0,0,2) | 70.26 |
| 3 | 17.77(5) | 4.988(13) | Mixed Layer Clay(0,0,2) | 6.76 |
| 4 | 19.877(9) | 4.463(2) | Kaolinite(1,1,-1),Mixed Layer Clay(0,2,0) | 45.71 |
| 5 | 20.822(4) | 4.2626(7) | Kaolinite(0,2,1),Quartz(1,0,0),Mixed Layer Clay(1,1,-1) | 35.56 |
| 6 | 21.3339 | 4.16152 | Mixed Layer Clay(0,2,1) | 32.70 |
| 7 | 24.91(2) | 3.571(4) | Kaolinite(0,0,4),Mixed Layer Clay(1,1,-2) | 61.08 |
| 8 | 26.621(4) | 3.3458(5) | Quartz(1,0,1),Mixed Layer Clay(0,2,2) | 100.00 |
| 9 | 31.6986 | 2.82049 | Kaolinite(0,2,4),Halite(2,0,0) | 8.70 |
| 10 | 33.31 | 2.68763 | Mixed Layer Clay(0,2,3) | 3.02 |
| 11 | 34.98(2) | 2.5630(15) | Kaolinite(1,3,0),Mixed Layer Clay(1,3,0) | 34.51 |
| 12 | 35.91(5) | 2.499(3) | Kaolinite(1,3,-2),Mixed Layer Clay(1,1,3) | 19.95 |
| 13 | 36.516(11) | 2.4587(7) | Quartz(1,1,0),Mixed Layer Clay(1,3,1) | 14.33 |
| 14 | 38.15(6) | 2.357(4) | Kaolinite(0,0,6),Mixed Layer Clay(2,0,1) | 36.23 |
| 15 | 39.4492 | 2.28236 | Kaolinite(2,0,-4),Quartz(1,0,2) | 13.68 |
| 16 | 40.3076 | 2.23572 | Kaolinite(2,2,-1),Quartz(1,1,1),Mixed Layer Clay(0,4,0) | 14.25 |
| 17 | 41.1124 | 2.19379 | Kaolinite(1,3,-4),Mixed Layer Clay(2,0,-3) | 5.53 |
| 18 | 42.430(11) | 2.1287(5) | Quartz(2,0,0),Mixed Layer Clay(1,3,-3) | 10.71 |
| 19 | 44.34(2) | 2.0414(11) | Kaolinite(2,2,-4),Mixed Layer Clay(0,4,2) | 5.00 |
| 20 | 45.69(4) | 1.9839(16) | Kaolinite(1,3,4),Halite(2,2,0),Quartz(2,0,1),Mixed Layer Clay(0,0,5) | 25.89 |
| 21 | 47.9473 | 1.8958 | Kaolinite(2,2,3),Mixed Layer Clay(2,0,3) | 6.18 |
| 22 | 50.100(8) | 1.8193(3) | Quartz(1,1,2),Mixed Layer Clay(0,2,5) | 13.71 |
| 23 | 50.73(7) | 1.798(2) | Kaolinite(0,0,8),Quartz(0,0,3),Mixed Layer Clay(2,2,-4) | 3.41 |
| 24 | 54.8619 | 1.67209 | Kaolinite(1,5,-2),Quartz(2,0,2),Mixed Layer Clay(3,1,0) | 13.44 |
| 25 | 55.2872 | 1.66023 | Quartz(1,0,3),Mixed Layer Clay(0,0,6) | 6.55 |
| 26 | 56.42(13) | 1.630(3) | Kaolinite(2,4,1),Halite(2,2,2),Quartz(2,1,0),Mixed Layer Clay(1,5,1) | 3.65 |

### Phase Data Pattern

# XRD Results-E204205

### General Information

| Measurement date: | 22/12/2021 | Interpretative date: | 19/5/2022 |
| --- | --- | --- | --- |
| Job Number/Client: | LJN2021-107 CKain | XRD | Rigaku Miniflex 600 |
| Registration Number: | E204205 | Analyst: | LUnwin |
| Quantitative Method: | PDXL Relative Heights | Process Medium: | Wholerock |
| Sample Holder: | Standard | Speed (deg/min): | 0.5 |
| Comment: | Shifted -0.02, Sample dried at 30degrees |  |  |

### Analysis Results

| Phase name | Content wt% (± error) | Formula |
| --- | --- | --- |
| Anatase | 2(2) | TiO2 |
| Halloysite-7 | 18(5) | Al2Si2O5(OH)4 |
| Goethite | 9(3) | α-Fe3+O(OH) |
| Mixed Layer Clay | 9(3) | Various |
| Quartz | 27(5) | SiO2 |
| Kaolinite | 36(10) | Al2(Si2O5)(OH)4 |

### Peak List

| No. | 2-theta(deg) | d(ang.) | Phase name | Rel. int. I(a.u.) |
| --- | --- | --- | --- | --- |
| 1 | 8.877(13) | 9.953(14) | Mixed Layer Clay(0,0,1) | 17.87 |
| 2 | 12.357(6) | 7.157(4) | Kaolinite(0,0,1),Halloysite-7(0,0,1) | 100.00 |
| 3 | 17.79(6) | 4.981(17) | Goethite(0,2,0),Mixed Layer Clay(0,0,2) | 3.05 |
| 4 | 19.8157 | 4.4768 | Kaolinite(0,2,0),Mixed Layer Clay(0,2,0),Halloysite-7 | 12.81 |
| 5 | 20.8454 | 4.25793 | Quartz(1,0,0) | 15.14 |
| 6 | 21.3188 | 4.16443 | Kaolinite(1,1,-1),Goethite(1,1,0),Mixed Layer Clay(0,2,1),Halloysite-7(1,1,-1) | 21.10 |
| 7 | 24.8887 | 3.57461 | Kaolinite(0,0,2),Mixed Layer Clay(1,1,-2),Halloysite-7 | 30.52 |
| 8 | 25.215 | 3.52908 | Anatase(1,0,1) | 13.72 |
| 9 | 26.631 | 3.34457 | Quartz(1,0,1),Mixed Layer Clay(0,2,2) | 50.13 |
| 10 | 33.403 | 2.68036 | Goethite(1,3,0),Mixed Layer Clay(0,2,3),Halloysite-7 | 1.38 |
| 11 | 34.9951 | 2.56198 | Kaolinite(1,-3,0),Goethite(0,2,1),Mixed Layer Clay(1,3,0),Halloysite-7(1,3,0) | 12.67 |
| 12 | 35.8554 | 2.50245 | Kaolinite(1,-3,-1),Goethite(0,4,0),Mixed Layer Clay(1,1,3),Halloysite-7(1,3,-1) | 5.77 |
| 13 | 36.5278 | 2.45791 | Quartz(1,1,0),Anatase(1,0,3),Goethite(1,1,1),Mixed Layer Clay(1,3,1) | 13.94 |
| 14 | 37.7442 | 2.38145 | Kaolinite(0,0,3),Anatase(0,0,4),Mixed Layer Clay(2,0,1),Halloysite-7(1,3,1) | 5.75 |
| 15 | 38.42(7) | 2.341(4) | Kaolinite(1,-3,1),Anatase(1,1,2),Halloysite-7(1,1,-3) | 7.24 |
| 16 | 39.4055 | 2.2848 | Quartz(0,1,2),Goethite(2,0,0) | 5.01 |
| 17 | 40.246 | 2.23899 | Quartz(1,1,1),Kaolinite(1,3,-2),Goethite(2,1,0),Mixed Layer Clay(0,4,0),Halloysite-7(0,4,0) | 3.66 |
| 18 | 41.34(7) | 2.182(3) | Kaolinite(2,0,1),Goethite(1,4,0),Mixed Layer Clay(0,4,1),Halloysite-7(0,2,3) | 1.74 |
| 19 | 42.38(2) | 2.1310(11) | Quartz(2,0,0),Kaolinite(0,2,-3),Mixed Layer Clay | 2.69 |
| 20 | 45.753(16) | 1.9815(7) | Quartz(0,2,1),Kaolinite(2,0,-3),Mixed Layer Clay | 3.49 |
| 21 | 46.4886 | 1.95184 | Kaolinite(2,2,1),Mixed Layer Clay(2,0,-4),Halloysite-7 | 2.03 |
| 22 | 47.9791 | 1.89462 | Kaolinite(1,3,-3),Anatase(2,0,0),Mixed Layer Clay | 1.77 |
| 23 | 50.089(8) | 1.8196(3) | Quartz(1,1,2),Goethite(1,5,0) | 5.01 |
| 24 | 50.70(9) | 1.799(3) | Quartz(0,0,3),Kaolinite(1,1,-4),Goethite(2,1,1),Mixed Layer Clay(0,2,5),Halloysite-7(2,2,-3) | 4.00 |
| 25 | 53.36(4) | 1.7155(11) | Kaolinite(2,-2,2),Anatase(1,0,5),Goethite(2,2,1),Mixed Layer Clay(2,0,-5),Halloysite-7(1,3,3) | 3.48 |
| 26 | 54.79(3) | 1.6741(7) | Quartz(2,0,2),Kaolinite(2,-4,-1),Anatase(2,1,1),Goethite(2,4,0),Mixed Layer Clay(3,1,0),Halloysite-7(2,4,-1) | 10.75 |

### Phase Data Pattern

# XRD Results-E204206

### General Information

| Measurement date: | 9/12/2021 | Interpretative date: | 19/5/2022 |
| --- | --- | --- | --- |
| Job Number/Client: | LJN2021-107 CKain | XRD | Rigaku Miniflex 600 |
| Registration Number: | E204206 | Analyst: | LUnwin |
| Quantitative Method: | PDXL Relative Heights | Process Medium: | Wholerock |
| Sample Holder: | Standard | Speed (deg/min): | 0.5 |
| Comment: | Shifted -0.03, Sample dried at 30degrees |  |  |

### Analysis Results

| Phase name | Content wt% (± error) | Formula |
| --- | --- | --- |
| Quartz | 39(10) | SiO2 |
| Anatase | 3(2) | TiO2 |
| Kaolinite | 40(10) | Al2(Si2O5)(OH)4 |
| Illite-Vermiculite | 7(3) | K0.7Al2[Al0.7Si3.3O10](OH)2 |
| Goethite | 11(4) | α-Fe3+O(OH) |
| Halite | 1(1) | NaCl |

### Peak List

| No. | 2-theta(deg) | d(ang.) | Phase name | Rel. int. I(a.u.) |
| --- | --- | --- | --- | --- |
| 1 | 8.77(2) | 10.07(3) | Kaolinite(0,1,0),Mixed Layer Clay(0,0,1) | 20.94 |
| 2 | 12.388(9) | 7.139(5) | Kaolinite(0,0,1) | 68.14 |
| 3 | 17.8088 | 4.97652 | Goethite(0,2,0),Mixed Layer Clay(0,0,2) | 5.12 |
| 4 | 19.8558 | 4.46785 | Kaolinite(0,2,0),Mixed Layer Clay(0,2,0) | 30.67 |
| 5 | 20.4168 | 4.34634 | Kaolinite(1,-1,0),Mixed Layer Clay(1,1,-1) | 15.00 |
| 6 | 20.8249(19) | 4.2621(4) | Quartz(1,0,0) | 26.68 |
| 7 | 21.258(11) | 4.176(2) | Kaolinite(1,1,-1),Goethite(1,1,0) | 19.78 |
| 8 | 24.8954 | 3.57366 | Kaolinite(0,0,2),Mixed Layer Clay(1,1,-2) | 30.00 |
| 9 | 25.3181 | 3.51494 | Anatase(1,0,1) | 17.07 |
| 10 | 26.627(4) | 3.3450(4) | Quartz(1,0,1),Kaolinite(1,0,-2),Mixed Layer Clay(0,2,2) | 100.00 |
| 11 | 27.5409 | 3.23609 | Kaolinite(1,2,-1),Halite(1,1,1) | 8.59 |
| 12 | 31.693(9) | 2.8210(8) | Kaolinite(1,2,1),Halite(2,0,0) | 5.32 |
| 13 | 33.3122 | 2.68746 | Kaolinite(1,2,-2),Goethite(1,3,0),Mixed Layer Clay(0,2,3) | 5.79 |
| 14 | 34.98(4) | 2.563(2) | Kaolinite(1,-3,0),Goethite(0,2,1),Mixed Layer Clay(1,3,0) | 27.30 |
| 15 | 35.93(6) | 2.497(4) | Kaolinite(1,-1,2),Goethite(1,0,1),Mixed Layer Clay(1,1,3) | 19.72 |
| 16 | 36.515(12) | 2.4588(8) | Quartz(1,1,0),Mixed Layer Clay(1,3,1) | 12.08 |
| 17 | 38.370(17) | 2.3440(10) | Kaolinite(2,0,-2),Anatase(1,1,2),Mixed Layer Clay | 27.89 |
| 18 | 39.450(7) | 2.2823(4) | Quartz(0,1,2),Goethite(2,0,0) | 6.76 |
| 19 | 40.2811 | 2.23712 | Quartz(1,1,1),Kaolinite(0,4,0),Goethite(1,2,1) | 3.91 |
| 20 | 41.31(3) | 2.1836(13) | Kaolinite(2,-2,0),Goethite(1,4,0),Mixed Layer Clay(0,4,1) | 3.99 |
| 21 | 42.427(12) | 2.1288(6) | Quartz(2,0,0),Kaolinite(2,-1,1),Mixed Layer Clay | 7.71 |
| 22 | 45.4209 | 1.9952 | Kaolinite(2,0,-3),Goethite(1,3,1),Halite(2,2,0),Mixed Layer Clay(0,0,5) | 7.23 |
| 23 | 45.7324 | 1.98234 | Quartz(0,2,1),Kaolinite(1,-3,2),Mixed Layer Clay | 7.15 |
| 24 | 47.8906 | 1.89792 | Kaolinite(1,3,-3),Anatase(2,0,0),Mixed Layer Clay(2,0,3) | 3.17 |
| 25 | 50.106(9) | 1.8191(3) | Quartz(1,1,2) | 11.29 |
| 26 | 51.0501 | 1.78762 | Kaolinite(0,0,4),Goethite(2,1,1),Mixed Layer Clay | 4.03 |
| 27 | 54.8548 | 1.67229 | Quartz(2,0,2),Kaolinite(2,-4,0),Anatase(2,1,1),Mixed Layer Clay(0,4,4) | 19.80 |
| 28 | 55.2998 | 1.65988 | Quartz(1,0,3),Kaolinite(1,-5,-1),Goethite(0,6,0),Mixed Layer Clay(1,5,1) | 9.08 |

### Phase Data Pattern

# XRD Results-E204207

### General Information

| Measurement date: | 9/12/2021 | Interpretative date: | 19/5/2022 |
| --- | --- | --- | --- |
| Job Number/Client: | LJN2021-107 CKain | XRD | Rigaku Miniflex 600 |
| Registration Number: | E204207 | Analyst: | LUnwin |
| Quantitative Method: | PDXL Relative Heights | Process Medium: | Wholerock |
| Sample Holder: | Standard | Speed (deg/min): | 0.5 |
| Comment: | Shifted -0.03, Sample dried at 30degrees |  |  |

### Analysis Results

| Phase name | Content wt% (± error) | Formula |
| --- | --- | --- |
| Quartz | 88(10) | SiO2 |
| Halite | 2(2) | NaCl |
| Kaolinite | 10(3) | Al2(Si2O5)(OH)4 |

### Peak List

| No. | 2-theta(deg) | d(ang.) | Phase name | Rel. int. I(a.u.) |
| --- | --- | --- | --- | --- |
| 1 | 12.3398 | 7.16708 | Kaolinite(0,0,2) | 5.70 |
| 2 | 19.8844 | 4.46149 | Kaolinite(1,1,-1) | 3.76 |
| 3 | 20.839(4) | 4.2592(8) | Quartz(1,0,0),Kaolinite(0,2,1) | 22.34 |
| 4 | 24.869(12) | 3.5774(17) | Kaolinite(0,0,4) | 2.48 |
| 5 | 25.2717 | 3.52129 | Kaolinite(1,1,-3) | 1.61 |
| 6 | 26.6267(16) | 3.3451(2) | Quartz(0,1,1) | 100.00 |
| 7 | 27.490(18) | 3.242(2) | Halite(1,1,1),Kaolinite(0,2,3) | 3.10 |
| 8 | 31.655(8) | 2.8243(7) | Halite(2,0,0) | 4.18 |
| 9 | 34.99(3) | 2.562(2) | Kaolinite(1,3,0) | 2.07 |
| 10 | 36.0229 | 2.4912 | Kaolinite(1,3,-2) | 1.10 |
| 11 | 36.499(3) | 2.4598(2) | Quartz(1,1,0) | 6.80 |
| 12 | 38.43(4) | 2.340(2) | Kaolinite(1,3,2) | 2.34 |
| 13 | 39.426(3) | 2.28367(18) | Quartz(1,0,2) | 5.90 |
| 14 | 40.238(6) | 2.2394(3) | Quartz(1,1,1) | 3.45 |
| 15 | 42.413(3) | 2.12948(16) | Quartz(2,0,0),Kaolinite(2,2,1) | 6.90 |
| 16 | 45.389(6) | 1.9965(3) | Halite(2,2,0),Kaolinite(1,3,4) | 2.59 |
| 17 | 45.749(5) | 1.98165(19) | Quartz(2,0,1) | 3.79 |
| 18 | 48.0346 | 1.89256 | Kaolinite(2,2,3) | 0.46 |
| 19 | 50.098(4) | 1.81934(14) | Quartz(1,1,2) | 12.65 |
| 20 | 54.846(5) | 1.67252(15) | Quartz(0,2,2),Kaolinite(1,3,6) | 4.96 |
| 21 | 55.291(7) | 1.6601(2) | Quartz(0,1,3),Kaolinite(1,5,-2) | 1.70 |
| 22 | 56.381(11) | 1.6306(3) | Halite(2,2,2),Kaolinite(2,2,5) | 0.85 |
| 23 | 57.181(9) | 1.6097(2) | Quartz(2,1,0) | 0.15 |
| 24 | 59.919(5) | 1.54248(11) | Quartz(1,2,1) | 9.46 |

### Phase Data Pattern

# XRD Results-E204208

### General Information

| Measurement date: | 9/12/2021 | Interpretative date: | 19/5/2022 |
| --- | --- | --- | --- |
| Job Number/Client: | LJN2021-107 CKain | XRD | Rigaku Miniflex 600 |
| Registration Number: | E204208 | Analyst: | LUnwin |
| Quantitative Method: | Semi-Quantitative | Process Medium: | Wholerock |
| Sample Holder: | Standard | Speed (deg/min): | 0.5 |
| Comment: | Shifted -0.01, Sample dried at 30degrees |  |  |

### Analysis Results

| Phase name | Content - Estimate | Formula |
| --- | --- | --- |
| Quartz | Major | SiO2 |
| Kaolinite-1A | Major | Al2(Si2O5)(OH)4 |
| Anatase | Trace | TiO2 |
| Mixed Layer Clay | Trace | Various |
| Halloysite (7Å) | Accessory | Al2Si2O5(OH)4 |

### Peak List

| No. | 2-theta(deg) | d(ang.) | Phase name | Rel. int. I(a.u.) |
| --- | --- | --- | --- | --- |
| 1 | 7.42(9) | 11.91(14) | Mixed Layer Clay(1,1,0) | 5.37 |
| 2 | 12.373(4) | 7.148(3) | Halloysite-7(0,0,1),Kaolinite(0,0,1) | 39.19 |
| 3 | 19.9129 | 4.45516 | Kaolinite(0,2,0),Mixed Layer Clay(0,6,0) | 9.29 |
| 4 | 20.3786 | 4.35439 | Kaolinite(1,-1,0) | 5.02 |
| 5 | 20.813(3) | 4.2646(5) | Quartz(1,0,0) | 18.39 |
| 6 | 24.87(2) | 3.578(3) | Halloysite-7(0,0,2),Kaolinite(0,0,2),Mixed Layer Clay | 22.45 |
| 7 | 25.2566 | 3.52337 | Anatase(1,0,1),Halloysite-7(0,2,1),Mixed Layer Clay | 6.67 |
| 8 | 26.626(2) | 3.3452(3) | Quartz(1,0,1),Kaolinite(1,-2,0),Mixed Layer Clay | 100.00 |
| 9 | 27.4419 | 3.24755 | Halloysite-7(1,1,1),Kaolinite(1,2,-1),Mixed Layer Clay(4,2,0) | 2.23 |
| 10 | 34.97(2) | 2.5640(16) | Kaolinite(2,0,-1),Mixed Layer Clay(5,3,0) | 10.33 |
| 11 | 35.9439 | 2.49649 | Kaolinite(1,-3,-1),Mixed Layer Clay(1,3,2) | 5.77 |
| 12 | 36.495(6) | 2.4601(4) | Quartz(1,1,0),Kaolinite(2,-1,-1),Mixed Layer Clay(2,0,2) | 8.61 |
| 13 | 38.4242 | 2.34086 | Anatase(0,0,4),Halloysite-7(1,3,0),Kaolinite(2,0,-2),Mixed Layer Clay(1,10,1) | 9.77 |
| 14 | 39.414(7) | 2.2843(4) | Quartz(1,0,2),Kaolinite(0,1,3),Mixed Layer Clay(0,6,2) | 10.33 |
| 15 | 40.243(6) | 2.2391(3) | Quartz(1,1,1),Kaolinite(0,4,0),Mixed Layer Clay(2,5,2) | 5.00 |
| 16 | 42.391(4) | 2.13054(18) | Quartz(2,0,0),Kaolinite(2,1,1) | 4.85 |
| 17 | 45.788(6) | 1.9800(2) | Quartz(2,0,1),Kaolinite(2,0,-3),Mixed Layer Clay(3,11,1) | 7.47 |
| 18 | 47.2042 | 1.9239 | Kaolinite(2,-1,-3),Mixed Layer Clay(0,13,1) | 1.09 |
| 19 | 47.9514 | 1.89565 | Kaolinite(1,3,-3) | 1.40 |
| 20 | 50.099(4) | 1.81929(15) | Quartz(1,1,2),Halloysite-7(1,1,-4),Kaolinite(2,-3,-2),Mixed Layer Clay(2,10,2) | 17.31 |
| 21 | 54.870(19) | 1.6719(5) | Quartz(2,0,2),Anatase(2,1,1),Kaolinite(1,-2,-4),Mixed Layer Clay(6,3,2) | 11.30 |
| 22 | 55.2851 | 1.66029 | Quartz(1,0,3),Kaolinite(2,0,-4),Mixed Layer Clay(4,14,0) | 3.23 |
| 23 | 59.906(7) | 1.54280(16) | Quartz(2,1,1),Kaolinite(2,-2,-4),Mixed Layer Clay(1,14,2) | 9.45 |

### Phase Data Pattern

Appendix 2. Sedimentation tests

Client:  C Kain, MRT

Sample Source:  Shark Point Road, Penna Landslide

MRT Job Number:  LJN2021-107

Methods:  Sedimentation sizing

Date: 31-1-2022

Analysts: J Renaud and T Coyte

MRT Reg. No.: E204201

Results:

Whole Sample

Mass: 17.2933g

Volume: 500ml

Nominal Mass per 10ml: 0.345866g

|  |  |  |  | Nominal Sedimentation (%) | Actual Sedimentation (%) | Particle Size Fractions Cumulative Weight (%) |
| --- | --- | --- | --- | --- | --- | --- |
| Time (sec) | Fall (cm) | Diameter (um) | Mass in 10ml (g) |  |  |  |
| 60 | 21.0 | 60.2 | 0.1470 | 57% | 43% | 57% |
| 120 | 20.5 | 42.0 | 0.1974 | 43% | 47% | 53% |
| 240 | 20.0 | 29.4 | 0.1537 | 56% | 51% | 49% |
| 480 | 19.5 | 20.5 | 0.1427 | 59% | 55% | 45% |
| 960 | 19.0 | 14.3 | 0.1554 |  | 59% | 41% |
| 1920 | 18.5 | 10.0 | 0.0963 | 72% | 63% | 37% |
| 3840 | 18.0 | 7.0 | 0.0969 | 72% | 67% | 33% |

Approximately 37.3% of the sample is ≤10µm in diameter

Approximately 19.6% of the sample is ≤2µm in diameter

MRT Reg. No.: E204202

Mass: 16.3428g

Volume: 500ml

Nominal Mass per 10ml: 0.326856g

|  |  |  |  | Nominal Sedimentation (%) | Actual Sedimentation (%) | Particle Size Fractions Cumulative Weight (%) |
| --- | --- | --- | --- | --- | --- | --- |
| Time (sec) | Fall (cm) | Diameter (um) | Mass in 10ml (g) |  |  |  |
| 60 | 21.0 | 62.4 | 0.2842 | 13% | 11% | 89% |
| 120 | 20.5 | 43.6 | 0.2799 | 14% | 12% | 88% |
| 240 | 20.0 | 30.4 | 0.2822 | 14% | 13% | 87% |
| 480 | 19.5 | 21.3 | 0.2793 | 15% | 14% | 86% |
| 960 | 19.0 | 14.8 | 0.2797 | 14% | 15% | 85% |
| 1920 | 18.5 | 10.4 | 0.2731 | 16% | 16% | 84% |
| 3840 | 18.0 | 7.2 | 0.2625 | 20% | 17% | 83% |

Approximately 84.3% of the sample is ≤10µm in diameter

Approximately 80.3% of the sample is ≤2µm in diameter

MRT Reg. No.: E204204

Mass: 20.0185g

Volume: 500ml

Nominal Mass per 10ml: 0.40037g

|  |  |  |  | Nominal Sedimentation (%) | Actual Sedimentation (%) | Particle Size Fractions Cumulative Weight (%) |
| --- | --- | --- | --- | --- | --- | --- |
| Time (sec) | Fall (cm) | Diameter (um) | Mass in 10ml (g) |  |  |  |
| 60 | 21.0 | 62.4 | 0.3735 | 7% | 6% | 94% |
| 120 | 20.5 | 43.6 | 0.3700 | 8% | 6% | 94% |
| 240 | 20.0 | 30.4 | 0.3709 | 7% | 7% | 93% |
| 480 | 19.5 | 21.3 | 0.3699 | 8% | 7% | 93% |
| 960 | 19.0 | 14.8 | 0.3662 | 9% | 8% | 92% |
| 1920 | 18.5 | 10.4 | 0.3640 | 9% | 9% | 91% |
| 3840 | 18.0 | 7.2 | 0.3583 | 11% | 9% | 91% |

Approximately 91.4% of the sample is ≤10µm in diameter

Approximately 89% of the sample is ≤2µm in diameter

MRT Reg. No.: E204205

Mass: 19.548g

Volume: 500ml

Nominal Mass per 10ml: 0.39096g

|  |  |  |  | Nominal Sedimentation (%) | Actual Sedimentation (%) | Particle Size Fractions Cumulative Weight (%) |
| --- | --- | --- | --- | --- | --- | --- |
| Time (sec) | Fall (cm) | Diameter (um) | Mass in 10ml (g) |  |  |  |
| 60 | 21.0 | 62.4 | 0.2666 | 32% | 31% | 69% |
| 120 | 20.5 | 43.6 | 0.2651 | 32% | 32% | 68% |
| 240 | 20.0 | 30.4 | 0.2582 |  | 32% | 68% |
| 480 | 19.5 | 21.3 | 0.2602 | 33% | 33% | 67% |
| 960 | 19.0 | 14.8 | 0.2591 | 34% | 33% | 67% |
| 1920 | 18.5 | 10.4 | 0.2572 | 34% | 33% | 67% |
| 3840 | 18.0 | 7.2 | 0.2578 | 34% | 34% | 66% |

Approximately 66.5% of the sample is ≤10µm in diameter

Approximately 64.7% of the sample is ≤2µm in diameter

MRT Reg. No.: E204206 Dup

Mass: 19.8282g

Volume: 500ml

Nominal Mass per 10ml: 0.396564g

|  |  |  |  | Nominal Sedimentation (%) | Actual Sedimentation (%) | Particle Size Fractions Cumulative Weight (%) |
| --- | --- | --- | --- | --- | --- | --- |
| Time (sec) | Fall (cm) | Diameter (um) | Mass in 10ml (g) |  |  |  |
| 60 | 21.0 | 62.4 | 0.3899 | 2% | 0% | 100% |
| 120 | 20.5 | 43.6 | 0.3866 | 3% | 1% | 99% |
| 240 | 20.0 | 30.4 | 0.3805 | 4% | 2% | 98% |
| 480 | 19.5 | 21.3 | 0.3819 | 0% | 4% | 96% |
| 960 | 19.0 | 14.8 | 0.3658 | 8% | 5% | 95% |
| 1920 | 18.5 | 10.4 | 0.3719 | 6% | 6% | 94% |
| 3840 | 18.0 | 7.2 | 0.3574 | 10% | 7% | 93% |

Approximately 93.8% of the sample is ≤10µm in diameter

Approximately 88.1% of the sample is ≤2µm in diameter

MRT Reg. No.: E204207

Mass: 24.726g

Volume: 500ml

Nominal Mass per 10ml: 0.49452g

|  |  |  |  | Nominal Sedimentation (%) | Actual Sedimentation (%) | Particle Size Fractions Cumulative Weight (%) |
| --- | --- | --- | --- | --- | --- | --- |
| Time (sec) | Fall (cm) | Diameter (um) | Mass in 10ml (g) |  |  |  |
| 60 | 21.0 | 61.6 | 0.1991 | 60% | 59% | 41% |
| 120 | 20.5 | 43.1 | 0.1628 | 67% | 62% | 38% |
| 240 | 20.0 | 30.1 | 0.1466 | 70% | 64% | 36% |
| 480 | 19.5 | 21.0 | 0.1372 | 72% | 67% | 33% |
| 960 | 19.0 | 14.7 | 0.1273 | 74% | 70% | 30% |
| 1920 | 18.5 | 10.2 | 0.1143 | 77% | 73% | 27% |
| 3840 | 18.0 | 7.1 | 0.1077 | 78% | 76% | 24% |

Approximately 27% of the sample is ≤10µm in diameter

Approximately 14.4% of the sample is ≤2µm in diameter

MRT Reg. No.: E204208

Mass: 18.9045g

Volume: 500ml

Nominal Mass per 10ml: 0.37809g

|  |  |  |  | Nominal Sedimentation (%) | Actual Sedimentation (%) | Particle Size Fractions Cumulative Weight (%) |
| --- | --- | --- | --- | --- | --- | --- |
| Time (sec) | Fall (cm) | Diameter (um) | Mass in 10ml (g) |  |  |  |
| 60 | 21.0 | 61.6 | 0.1677 | 56% | 54% | 46% |
| 120 | 20.5 | 43.1 | 0.1635 | 57% | 55% | 45% |
| 240 | 20.0 | 30.1 | 0.1670 | 56% | 56% | 44% |
| 480 | 19.5 | 21.0 | 0.1614 | 57% | 57% | 43% |
| 960 | 19.0 | 14.7 | 0.1577 | 58% | 57% | 43% |
| 1920 | 18.5 | 10.2 | 0.1554 | 59% | 58% | 42% |
| 3840 | 18.0 | 7.1 | 0.1495 | 60% | 59% | 41% |

Approximately 41.9% of the sample is ≤10µm in diameter

Approximately 38.5% of the sample is ≤2µm in diameter

Appendix 3. Sedimentation tests

Client:  C Kain, MRT

Sample Source:  Shark Point Road, Penna Landslide

MRT Job Number:  LJN2021-107

Methods:  Sedimentation sizing

Date: 27/4/2022

Analysts: L Unwin and T Coyte

| Sample No. | Original Dry Weight (g) | >38micron in size (g) | <38 um (%) | Comment |
| --- | --- | --- | --- | --- |
| E204201 | 54.01 | 1.00 | 98.1 |  |
| E204202 | 31.75 | 0.14 | 99.6 |  |
| E204204 | 83.00 | 0.27 | 99.7 | included paint chips |
| E204205 | 36.13 | 0.99 | 97.3 |  |
| E204206 | 44.54 | 0.69 | 98.5 |  |
| E204207 | 99.16 | 60.53 | 39.0 |  |
| E204208 | 89.27 | 13.34 | 85.1 |  |